# SECTION 204 – STONE FOR MASONRY, RIPRAP, POROUS BACKFILL, AND GABIONS

## 204.01 – Description

These specifications cover aggregate materials used in the construction of masonry items and stone gabions, to protect ground slopes from erosion or wave action and to facilitate drainage, generally behind a backwall or abutment.

## 204.02 – Detail Requirements

- Stone for rubble or mortar rubble masonry shall be sound, durable, and free from seams, cracks, and other structural defects and shall be minimum Grade C free from rounded, worn, or weathered surfaces.

- Stone for riprap and bedding shall be sound, durable, and free from seams, cracks, and other structural defects. Riprap stone and bedding exposed to the wave action of water shall be of igneous or metamorphic origin. Riprap bedding shall be crushed stone, minimum Grade B.

- Porous backfill shall be aggregate size No. 78 or No. 8, a minimum Grade B. Crushed glass meeting the gradation requirements specified in Section 203.02(d) may be directly substituted for size No. 78 and 8 aggregates.

- Gabion stone shall be durable and free from seams and cracks. Weathered stone shall not be used. Stone shall weigh between 4 and 30 pounds except that approximately 5 percent of the individual stones may weigh less than 4 or more than 30 pounds. At least 50 percent of the stone shall weigh more than 10 pounds.