# SECTION 205 – CRUSHER RUN AGGREGATE

## 205.01 – Description

These specifications cover crushed aggregate used for backfilling and bedding pipe and box culverts, maintaining traffic, and repairing and constructing all-weather private access pavements.

## 205.02 – Materials

Crusher run aggregate shall be crushed from stone, slag, or gravel and shall contain all of the sizes produced when the original aggregate is reduced through a series of crushers to the maximum size specified. It shall be essentially free from deleterious substances in accordance with Section 203.

- Crushed hydraulic cement concrete will be permitted for use as crusher run aggregate provided it conforms to the physical requirements of Section 203 and shows no adverse chemical reaction. It shall not be used in a subsurface drainage application in combination with perforated pipe or as a base material where geotextile fabric is to be used.

- Crushed gravel shall consist of particles of which at least 90 percent by weight of material retained on the No. 10 sieve shall have at least one face fractured by artificial crushing. Tests to verify acceptance shall be performed in accordance with VTM-15.

- Crushed glass will be permitted for use as crusher run aggregate provided it conforms to the physical requirements of Section 203.02(d). Crushed glass having the gradation specified in Section 203.02(d) may be directly substituted for size No. 25 and 26 aggregates in pipe bedding and backfilling applications only.

## 205.03 – Detail Requirements

- Grading: Grading shall conform to the following requirements when tested in accordance with AASHTO T27:

| % by Weight of Materials Passing Sieve |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Size No. | 2½ in | 2 in | 1½ in | 1 in | ¾ in | No. 4 |
| 24 | Min. 100 | 95±5 |  |  |  | 32±18 |
| 25 |  |  | Min. 100 | 95±5 |  | 32±18 |
| 26 |  |  |  | Min. 100 | 95±5 | 38±22 |

- Atterberg Limits: The liquid limit shall be not more than 25. The plasticity index shall be not more than 3. Tests to verify acceptance shall be performed in accordance with VTM-7.

- Soundness: Soundness shall conform to the requirements of Table II-4. Tests to acceptance shall be performed in accordance with AASHTO T103 or T104. The requirement for soundness test for crushed glass is waived due to its preclusion from the applications shown in Table II-4.

- Abrasion Loss: Abrasion loss shall be not more than 45 percent. Tests to verify acceptance shall be performed in accordance with AASHTO T96.

- Flat and Elongated Particles: Crusher run aggregate to be used as a temporary riding surface during construction activities or as the final riding surface after construction shall contain not more than 30 percent by mass of aggregate particles retained on and above the 3/8-inch sieve having a maximum to minimum dimensional ratio greater than 5 as determined in accordance with ASTM D4791.