# SECTION 206 – LIGHTWEIGHT AGGREGATE

## 206.01 – Description

These specifications cover lightweight aggregate used in the production of hydraulic cement concrete and asphalt surface treatment.

## 206.02 – Detail Requirements

Lightweight aggregate shall consist of clay, shale, or slate expanded through a sintering or rotary kiln.

- Lightweight aggregate used in hydraulic cement concrete shall conform to AASHTO M195.

- Lightweight aggregate used for asphalt surface treatment shall conform to AASHTO M195 except that Sections 3, 6, and 8 will not apply. Grading shall conform to Table II-3 except that the maximum percentage by weight of material passing the No. 8 sieve shall be 16 percent and passing the No. 16 sieve shall be 9 percent.