# SECTION 209 – OPEN-GRADED SHOULDER MATERIAL

## 209.01 – Description

These specifications cover the requirements for open-graded material used on roadway shoulders where designated on the plans or other Contract documents.

## 209.02 – Detail Requirements

Open-graded shoulder material shall be aggregate material No. 18 and shall consist of mixtures of natural or crushed gravel, crushed stone, or sand, without soil mortar.

- Grading: Grading shall conform to the following when tested to verify acceptance in accordance with VTM-25:

| % by Weight of Materials Passing Sieve |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| 2 in | 1 in | 3/8 in | No. 10 | No. 40 | No. 200 |
| 100 | 90 ± 10 | 55 ± 15 | 20 ± 10 | 8 ± 5 | 3 ± 3 |

- Atterberg Limits: Material shall be nonplastic, and the liquid limit shall be not more that 25 when tested to verify acceptance in accordance with VTM-7.

- Soundness: Soundness shall conform to the requirements of Table II-7 for subbase material when tested to verify acceptance in accordance with AASHTO T103 or T104.

- Abrasion Loss: Abrasion loss shall be not more than 45 percent when tested to verify acceptance in accordance with AASHTO T96.

## 209.03 – Mixing

Pugmill mixing will not be required for aggregate shoulder material No. 18. The Contractor shall provide a laboratory for Department use as specified in Section 106.07.