# SECTION 212 – JOINT MATERIALS

## 212.01 – Description

These specifications cover resilient products made from various materials that are designed to accommodate the movement of rigid structures, such as component parts of hydraulic cement concrete, and seal the joint from intrusion of water or incompressibles.

## 212.02 – Detail Requirements

- Hot-poured joint sealer shall be heated in accordance with the manufacturer’s recommendations.

  - Asphalt sealer shall conform to ASTM D6690, Type II.

  - Elastomeric joint sealer shall conform to ASTM D3406 and shall only be used for longitudinal joints.

- Silicone sealants shall be furnished in a one- or two-part formulation. The sealant shall be compatible with the surface to which it is applied. Acid-cure sealants are not acceptable for use on hydraulic cement concrete. Bond breakers shall be chemically inert and resistant to petroleum products, solvents, and primers.

Silicone sealants are identified in the following manner:

  - Class A: A low-modulus non-sag silicone for use in sealing horizontal and vertical joints in hydraulic concrete pavements and structures. Tooling is required.

  - Class B: A very-low-modulus self-leveling silicone used to seal horizontal joints in hydraulic cement concrete pavements and structures. Tooling is not normally required.

  - Class C: An ultra-low-modulus self-leveling silicone used to seal horizontal joints in hydraulic cement concrete pavements and structures. It can also be used to seal the joints between hydraulic cement concrete pavement and asphaltic concrete shoulders. Tooling is not normally required.

  - Class D: An ultra-low-modulus self-leveling rapid-curing two-part silicone used to seal expansion joints on bridge decks. It can also be used to seal joints subject to dynamic movements where rapid curing is necessary. Tooling is not normally required.

Silicone sealants shall conform to the following physical requirements:

| Properties | Test Method | Sealant Class |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | A | B | C | D |
| Tensile stress at 150% strain (max. psi) (Note 1) | ASTM C1135 | 45 | 40 | 15 | 25 |
| Durometer hardness, Shore (0º and 77º ± 3ºF) (Note 1) | ASTM D2240 | "A" 10-25 | "00" 40-80 | "00" 20-80 | "00" 40-80 |
| Bond to concrete mortar (min. psi) (Notes 1 and 3) | VTM-90 | 50 | 40 | 35 | 35 |
| Tack-free time (skin-over) (max. min) (Note 2) | VTM-90 (Note 4) | 180 | 180 | 180 | 30 |
| Extrusion rate (min. g/min) | VTM-90 | 75 | 90 | 100 | 200 |
| Non-volatile (min. %) specific gravity | VTM-90 ASTM D792 (Method A) | 90 1.1-1.5 | 90 1.1-1.5 | 90 1.1-1.5 | 90 1.2-1.5 |
| Shelf life (from date of shipment) |  | 6 mo | 6 mo | 6 mo | 6 mo |
| Movement capability and adhesion (Note 1) | VTM-90 | No adhesive or cohesive failure after 10 cycles at 0F |  |  |  |
| Ozone and UV resistance (Note 1) | ASTM C-793-75 | No chalking, cracking, or bond loss after 5,000 hr |  |  |  |
| Note 1: The cure time for these specimens shall be 21 days for Class A and 28 days for Classes B and C. Specimens shall be cured at 77 ± 3F and 50 ± 5% relative humidity. Note 2: At conditions of 77 ± 3F and 50 ± 5% relative humidity. Note 3: Class C silicone shall also attain its bond strength requirement to asphalt concrete. Note 4: In cases of dispute, ASTM D2377 shall be used as a referee test. The exposure period in Section 7, Procedure, shall be the tack-free time requirement of this specification. |  |  |  |  |  |

Bond breakers shall not stain or adhere to the sealant. Bond breakers shall be either a backer rod or tape identified and used in accordance with the following:

  - Backer Rods

Type L: A closed-cell expanded polyethylene foam backer rod. This backer rod may only be used with Class A silicone and is suitable for roadway and structure joints.

Type M: A closed-cell polyolefin foam backer rod that has a closed-cell skin over an open-cell core. This backer rod may be used with all three types of sealants and is suitable for use in roadway and structure joints.

Backer rods shall conform to the following:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Density | ASTM D1622 | Min. 2.0 lb/ft3 |
| Tensile strength | ASTM D1623 | Min. 25 psi |
| Water absorption | ASTM C509 | Max. 0.5% by volume |

  - Bond Breaking Tape Type N shall be made from extruded polyethylene and shall have a pressure-sensitive adhesive on one side. Bond breaking tape may be used with all three types of sealants but is suitable for structure joints only.

Bond breaking tape shall be not less than 0.005-inch thick.

The manufacturer of the joint sealant shall furnish certified test results on each lot of sealant furnished to a project. The certified test results shall include all test results except the bond to concrete mortar and shore durometer hardness at 0 degrees F.

The Engineer will only approve for use those silicone sealants that appear on the latest Approved Products list published by the Department’s Materials Division.

The Department will not approve silicone sealants meeting the material requirements of this specification submitted for initial approval for general use until field evaluations are completed. The material shall be installed in roadway or bridge joints and must go through two winters without failure before being approved. After such evaluation and approval, the material will be placed on the Department’s Approved Products list.

The Department will reject any sealant or bond breaker that fails to perform adequately in actual use even though a sealant or bond breaker has been previously evaluated and approved.

- Preformed expansion joint filler shall conform to AASHTO M213.

- Expanded rubber joint filler shall conform to ASTM D1056. Unless otherwise specified, Grades 2A3, 2A4, or 2A5 shall be furnished.

- Preformed neoprene (polychloroprene) seals shall conform to ASTM D1056, Grade 2B3. (Modification requires that material be manufactured from neoprene.)

- PVC and PE joint fillers shall conform to ASTM D1667. Grades VE-43 BL to VE-45 BL shall be furnished. The manufacturer shall recommend adhesives for use with this material.

- Sponge rubber joint filler shall conform to AASHTO M153, Type I. When used in conjunction with bridge bearings, the load required to compress the test specimen to 50 percent of its thickness before the test shall be not more than 100 pounds per square inch.

- Gaskets for pipe and box culvert sections shall conform to the following: Rubber gaskets for ductile iron pipe and fittings shall conform to AWWA C111. Rubber gaskets for concrete and metal pipe shall conform to ASTM C443. Rubber gaskets for plastic pipe shall conform to ASTM F 477. Flexible cellular sponge or expanded rubber gaskets for metal pipe shall conform to ASTM D1056.  Gaskets for box culvert sections shall conform to ASTM C1677. All gaskets shall conform to the ozone cracking resistance described in Section 237.02 of the Specifications.

- Preformed flexible joint sealants for concrete pipe, manholes and box culvert sections for use in storm sewers or culverts not intended to operate under pressure or subject to infiltration or exfiltration limits shall conform to ASTM C990.

- Preformed elastomeric joint sealer shall be a vulcanized elastomeric compound in which noncrystallizing neoprene is used as the sole polymer. Sealer shall be resilient and resistant to heat, oil, and ozone.

The seal shall conform to the following as evidenced by samples cut from the finished product:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Tensile strength | ASTM D412 | 2,000 psi min. |
| Elongation at break | ASTM D412 | 250% min. |
| Hardness (durometer, Shore A) | ASTM D2240 | 55 ± 5 |
| Tensile strength (change) After Oven aging (70 hr at 212F) IAW ASTM D573 | ASTM D412 | –30% max. |
| Elongation (change) After Oven aging (70 hr at 212F) IAW ASTM D573 | ASTM D412 | –40% max. |
| Hardness (points change) After Oven aging (70 hr at 212F) IAW ASTM D573 | ASTM D2240 | +10% max. |
| Ozone resistance (20% strain, 100 pphm in air, 300 hr at 104F) (wipe with solvent to remove surface contamination) | ASTM D1149 | No cracks |
| High-temperature recovery (72 hr at 212F under 50% deflection) | VTM-3 | 85% (no web adhesion or cracks) |
| Low-temperature recovery (72 hr at 14F under 50% deflection) | VTM-3 | 87% |
| Low-temperature recovery (22 hr at –20F under 50% deflection) | VTM-3 | 82% |

When tested at a temperature of 70 ± 5 degrees F, the seal shall also conform to the following:

| Use | Deflection Based on Nominal Width (%) | Pressure (psi) |
| --- | --- | --- |
| Pavement | 20 | Min. 3 |
|  | 50 | Max. 15 |
| Structure | 20 | Min. 4 |
|  | 50 | Max. 40 |

After aging at 212 degrees F for 70 hours at 50 percent deflection, the seal shall conform to the following:

| Use | Deflection Based on Nominal Width (%) | Pressure (psi) |
| --- | --- | --- |
| Pavement | 20 | Min. 1.0 |
|  | 50 | Max. 15 |
| Structure | 20 | Min. 1.5 |
|  | 50 | Max. 40 |

Lubricant adhesive shall be a one-component polyurethane compound with an aromatic hydrocarbon solvent and shall conform to the physical properties of ASTM D4070.

Lubricant for pavement seals shall conform to ASTM D2835.

- Elastomeric Expansion Dam and Tooth Expansion Joint: The elastomeric sheet gland material shall be virgin ethylene propylene diene monomer (EPDM) or virgin polychloroprene. The elastomeric material shall have the following physical properties:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Tensile strength | ASTM D412 | 1,500 psi min. |
| Elongation at break | ASTM D412 | 175% min. |
| Low-temperature brittleness | ASTM D746 | Not brittle at –40F |
| Oil deterioration (no requirement for EPDM material), volume increase after 70-hr immersion in ASTM Oil No. 3 at 212F | ASTM D471 | 120% max. |
| Ozone resistance: exposure to 100 pphm ozone in air for 70 hr at 100F under 20% strain | ASTM D1149 | No cracks |
| Hardness, Durometer A | ASTM D2240 | 50-60 |

The elastomeric strip seal gland material shall be preformed, non-reinforced, polychloroprene and shall have the following properties:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Tensile strength | ASTM D412 | 2,000 psi min. |
| Elongation at break | ASTM D412 | 250% min. |
| Hardness, Durometer A, points | ASTM D2240 (Modified)1,2 | 60 ± 5 |
| Tensile strength, loss after Oven aging, 70 hr at 212F IAW ASTM D573 | ASTM D412 | 20% max. |
| Elongation, loss after Oven aging, 70 hr at 212F IAW ASTM D573 | ASTM D412 | 20% max. |
| Hardness, Durometer A, points After Oven aging (70 hr at 212F) IAW ASTM D573 | ASTM D2240 (Modified)1,2 | 0 to +10 |
| Oil swell, ASTM Oil No. 3, 70 hr at 212F (100C), weight change | ASTM D471 | 45% max. |
| Ozone resistance, 20% strain, 300 pphm in air, 70 hr at 104F (40C) | ASTM D1149 (Modified)3 | No cracks |
| Low-temperature stiffening, 7 days at 14F(10C), hardness, Durometer A, points change | ASTM D2240 (Modified)1,2 | 0 to +15 |
| Compression set, 70 hr at 212F (100C) | ASTM D395 Method B (Modified)1 | 40% max. |
| 1The term modified relates to the specimen preparation. The use of the strip seal as the specimen source requires that more plies than specified in either modified test procedure be used. Such specimen modification shall be agreed upon by the purchaser and producer or supplier prior to testing. 2The hardness test shall be performed with the durometer in a durometer stand as specified in ASTM D2240. 3Test in accordance with ASTM D518, Procedure A. Ozone concentration is expressed in pphm. |  |  |

  - Steel portion of expansion dam shall conform to ASTM A709, Grade 36.

  - Deformed reinforcing steel bars shall conform to ASTM A615, Grade 60.

  - Lubricant adhesive shall be a one-part moisture-curing polyurethane compound conforming ASTM D4070.

  - Fabric reinforcement shall be nonwicking woven polyester material.

  - Bolts, nuts, and washers shall conform to ASTM A276, Type 304 Stainless Steel.

  - Flathead screws shall conform to ASTM F 738, Type 304 Stainless Steel.

  - Stud anchors shall conform to Section 226.02(d).

  - Special configurations such as doglegs, tees, and crosses in the elastomeric strip seal gland shall be shop fabricated in a mold under heat and pressure.

- Pressure relief joint material shall conform to ASTM D3204.

- Waterstops shall conform to the following:

  - Metal: Sheet copper shall conform to Section 230.

  - Nonmetallic Waterstops: Nonmetallic waterstops shall be manufactured from neoprene or PVC. Manufacturer’s shop splices shall be fully vulcanized.

    - Neoprene waterstops shall be manufactured from a vulcanized elastomeric compound containing neoprene as the sole elastomer and shall conform to the following:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Tensile strength | ASTM D412 | Min. 2,000 psi |
| Elongation at break | ASTM D412 | Min. 300% |
| Ozone resistance (20% strain, 100 hr at 100 ± 2oF) | ASTM D1149 (except 100 ± 20 pphm) | No cracks |
| Oil swell (ASTM No. 3 Oil, 70 hr at 212oF, volume change) | ASTM D471 | Max. 80% |

After accelerated aging in accordance with ASTM D573 for 70 hours at 212 degrees F, the elastomer shall not show a change in tensile strength of more than 15 percent or a change in the elongation at break of more than 40 percent.

    - PVC waterstops shall be manufactured from PVC conforming to the U.S. Corps of Engineers Specification CRD-C 572 and shall conform to the ozone resistance as required for neoprene waterstops. The manufacturer shall furnish a certificate verifying compliance with the performance requirements specified under paragraph 6 of CRD-C 572 with the test sample supplied.

- Traffic loop sealant material shall be an epoxy-resin system, a polyester system, or rubberized asphalt designed specifically to conform to the physical properties for sealing traffic loop pavement cuts. The system shall bond to either hydraulic cement concrete or asphalt concrete, be unaffected by environmental conditions, and have a dielectric strength sufficient to allow the traffic loop to operate as intended. The viscosity of the mixture shall be such that the mixture is easily pourable into the saw slot and sufficiently flowable to encase the electrical wiring.

  - The epoxy-resin system shall be a two-component material conforming to the following based on the epoxy without sand, except for the cure time requirement:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Pot life at 77oF | ASTM C881, Para. 11.2 | Min. 12 min |
| Initial cure time at 77oF |  | Max. 60 min |
| Hardness, Shore D | ASTM D2240 | 25-65 |
| Elongation | ASTM D638 | Min. 50% |
| Water absorption (24 hr) | ASTM D570 | Max. 0.5% |
| 3% NaCl absorption (24 hr) | ASTM D570 | Max. 0.5% |
| ASTM No. 3 Oil absorption (24 hr) | ASTM D570 | Max. 0.1% |
| Gasoline absorption (24 hr) | ASTM D570 | Max. 1.0% |

The sand used in the epoxy-resin system shall conform to the following grading requirements:

| Sieve No. | % Passing |
| --- | --- |
| 16 | 100 |
| 30 | 95 ± 5 |
| 100 | Max. 10 |
| 200 | Max. 3 |

  - The polyester system shall be a two-component material conforming to the following:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Pot life at 77oF | ASTM C881, Para. 11.2 | Min. 12 min |
| Initial cure time at 77oF |  | Max. 45 min |
| Hardness, Shore D | ASTM D2240 | 25-65 |
| Elongation | ASTM D638 | Min. 15% |
| Water absorption (24 hr) | ASTM D570 | Max. 0.2% |
| 3% NaCl absorption (24 hr) | ASTM D570 | Max. 0.2% |
| ASTM No. 3 Oil absorption (24 hr) | ASTM D570 | Max. 0.02% |
| Gasoline absorption (24 hr) | ASTM D570 | Max. 0.8% |

  - Rubberized asphalt (two-component) shall conform to the following:

| Property | Test Procedures | Physical Requirements |
| --- | --- | --- |
| Pot life at 77oF |  | Min. 25 min |
| Initial cure time at 77oF |  | Max. 60 min |
| Hardness, Shore A | ASTM D2240 | Max. 20 |
| Flow at 140oF (5 hr) | ASTM D1851 | No flow |
| Bond at 0oF (3 cycles) | ASTM D1851 | Min. 50% of original width |
| Water absorption (72 hr) |  | Max. 0.1% |
| ASTM No. 3 Oil absorption (24 hr) |  | Max. 0.1% |