# SECTION 213 – DAMP-PROOFING AND WATERPROOFING MATERIALS

## 213.01 – Description

These specifications cover materials, generally asphalt based, that are intended to prevent or delay the passage of water, usually through a section of hydraulic cement concrete.

## 213.02 – Detail Requirements

- Asphalt shall conform to ASTM D312 Type II and shall be free of asbestos. Primer shall conform to AASHTO M140, Types SS-1h, QS-1H, or AASHTO M208, Types CSS-1h, CQS-1h.

- Fabric shall conform to AASHTO M288. When cotton fabric is used, it shall be saturated with asphalt. Glass fiber shall conform to ASTM D1668.

- Joint sealers for horizontal joints shall be a viscosity grade, AC-40 asphalt cement, conforming to Section 210. Sealers for vertical joints shall have fiber added, 20 percent by weight. The manufacture shall provide a factory mixed vertical joint sealer to ensure a uniform mixture.

- Membrane shall conform to ASTM D6153.