# SECTION 214 – HYDRAULIC CEMENT

## 214.01 – Description

These specifications cover cements that harden when mixed with water. The various types have special characteristics to be used as denoted in other parts of these specifications and on the plans or in other Contract documents.

## 214.02 – Detail Requirements

- Blended hydraulic cement shall conform to AASHTO M240 and only used as approved by the Engineer.

- Portland cements shall conform to AASHTO M85 except as follows:

  - The Department will permit SO3 content as specified in AASHTO M85 provided supporting data specified in AASHTO M85 are submitted to the Department for review and acceptance prior to use of the material.

  - Type I and Type II cement shall contain not more than 1.0 percent alkalies (% Na2O + % 0.658K20).

- Expansive hydraulic cement shall conform to ASTM C 845, Type K.