# SECTION 218 – HYDRAULIC CEMENT MORTAR AND GROUT

## 218.01 – Description

These specifications cover hydraulic cement mortar and grout used in bonding units together, filling voids, and making surface repairs.

## 218.02 – Materials

- Hydraulic cement shall conform to Section 214.

- Fine aggregate shall conform to Section 202.

- Water shall conform to Section 216.

- Admixtures shall conform to Section 215.

## 218.03 – Detail Requirements

Hydraulic cement mortar and grout shall consist of a mixture of hydraulic cement, fine aggregate, water, and admixtures as specified herein.

Hydraulic cement mortar and grout shall contain from 3 to 7 percent entrained air. Air-entrained hydraulic cement may be used. The Contractor or supplier shall mix hydraulic cement mortar and grout with the minimum amount of water necessary to obtain the required consistency.

- Hydraulic cement mortar shall consist of 1 part hydraulic cement, 2 1/2 parts fine aggregate by weight, and sufficient water to produce a stiff mixture. Grading C fine aggregate shall be used.

- Nonshrink mortar shall consist of 1 part hydraulic cement, 2 parts fine aggregate by weight, a set retarder or other admixture that will reduce the amount of required mixing water, and sufficient water to produce a stiff mixture. Grading C fine aggregate shall be used.

- Hydraulic cement grout shall consist of 1 part hydraulic cement, 2 parts fine aggregate by weight, and sufficient water to produce a free-flowing mixture. Grading A or C fine aggregate shall be used.

- High-strength grout and mortar shall consist of a commercially produced prepackaged, non shrink, hydraulic cement mixture conforming to ASTM C1107 modified by the following:

The grout/mortar shall develop a 7-day compressive strength of at least 4,000 pounds per square inch when tested in accordance with ASTM C109, and a 7-day bond strength of at least 1,000 pounds per square inch when tested in accordance with VTM-41, except that epoxy shall not be used to develop the bond.