# SECTION 219 – RIGHT-OF-WAY MONUMENTS

## 219.01 – Description

These specifications cover concrete and metal markers used to designate right-of-way boundaries.

## 219.02 – Detail Requirements

Right-of-way monuments shall be manufactured from reinforced concrete or metal conforming to the dimensions and details shown in the Standard Drawings, and in accordance with these specifications.

- Concrete Monuments: Concrete shall be Class A3 conforming to Section 217, except that the Department will allow the use of Type I cement and a change in the aggregate size.

Steel reinforcement shall conform to Section 223 and shall be placed as shown on the Standard drawings.

Monuments shall be cast in one piece with smooth and uniform surfaces.

Monuments shall withstand a cracking load of at least 4,000 pounds and a destruction load of 5,000 pounds when tested transversely on a 24-inch span and shall have an absorption value of not more than 10 percent. Tests will be performed in accordance with AASHTO T177.

- Metal Monuments: Material for steel pins shall conform to Section 223.

Material for locator posts shall conform to Section 226 or Section 229.

Steel posts or pins shall be galvanized in accordance with ASTM A123.