# SECTION 222 – MASONRY UNITS

## 222.01 – Description

These specifications cover masonry units manufactured of regular or lightweight concrete or brick made from clay or shale in a plant specifically designed for such a purpose.

222.02 – Detail Requirements

- Wall Units:

  - Hollow load-bearing units shall conform to ASTM C90, Grade N-I.

  - Hollow non-load bearing units shall conform to ASTM C129, Type I.

  - Solid load-bearing units shall conform to ASTM C145, Grade N-I.

  - Building bricks shall conform to either:

    - ASTM C62 Grade SW, or

    - ASTM C55, except that the average compressive strength of 5 bricks shall be a minimum 3000 psi and no individual brick shall be less than 2500 psi.

- Catch Basins and Manholes:

  - Masonry blocks shall conform to ASTM C139.

  - Bricks shall conform to either:

    - ASTM C32, Grade MS, or

    - ASTM C55, except that the average compressive strength of 5 bricks shall be a minimum 3000 psi and no individual brick shall be less than 2500 psi.

- Sewer Bricks shall conform to ASTM C32, Grade SM.