# SECTION 225 – STEEL FORGINGS AND STEEL SHAFTING

## 225.01 – Description

These specifications cover steel items specifically designed for a particular bridge structure and generally used where movement of a part of the structure is involved.

## 225.02 – Detail Requirements

- Steel forgings shall conform to ASTM A668, Class D, for use with structural carbon steel and Class F for use with high-strength low-alloy steel.

- Steel shafting shall conform to ASTM A108, Grades 1016 through 1030.