# SECTION 227 – STEEL GRID FLOORING

## 227.01 – Description

These specifications cover plant-fabricated steel for use as a portion of a bridge deck.

## 227.02 – Materials

- Steel shall conform to ASTM A709, Grade 36, except that material which is not galvanized shall have a copper content of at least 0.2 percent.

- Concrete for filling steel grid floors shall conform to Section 217 for Class A3, maximum aggregate size No. 7.

## 227.03 – Detail Requirements

- Open flooring shall be galvanized in accordance with ASTM A123.

- Painting, when specified or permitted by the Engineer, shall be performed in accordance with Section 411 except that the Department will allow dipping to coat the flooring.