# SECTION 228 – STEEL PILES

## 228.01 – Description

These specifications cover steel fabricated to a shape that will act as a foundation for a structure. The Contractor shall ensure one copy of each applicable mill analysis accompanies the corresponding steel piles shipped to the project and shall supply the Engineer three additional copies of the mill analysis.

## 228.02 – Detail Requirements

- H-piles: H-piles shall be structural carbon steel conforming to ASTM A709, Grade 36.

- Shell Piles: Welded shells shall be fabricated with butt welds only.

End plates and other fittings shall be fabricated from the same material used for the shell or from steel conforming to ASTM A709, Grade 36.

  - Steel for Type A shells shall be classification SAE 1010 with a yield point of at least 50,000 pounds per square inch. Shells shall be fluted and consist of a cylindrical upper section(s) and a lower section having a diameter diminishing at the rate of at least 1/8 but not more than 1/4 inch per foot. The lower section shall have a welded point with a diameter of at least 8 inches.

  - Steel for Type B shells shall conform to ASTM A252, Grade 1, 2, or 3. Shells shall be straight pipe having bottoms closed with end plates at least 3/4 inch in thickness and a diameter not more than 1/2 inch greater than the outside diameter of the shell.

  - Steel for Type C shells shall conform to ASTM A569 or A366. Shells shall be helically corrugated and cylindrical in the section and shall diminish in diameter toward the point by stepping at regular intervals at the rate of approximately 1 inch per step or at an average rate of at least 1/8 but not more than 1/4 inch per foot. The lower section shall have a welded point with a diameter of at least 8 inches.

  - Steel for Type D shells shall be classification SAE 1010 with a yield point of at least 50,000 pounds per square inch. Shells shall be helically corrugated and of a constant cylindrical section or shall diminish uniformly in diameter at the rate of at least 1/8 but not more than 1/4 inch per foot. Bottoms shall have ends closed with plates at least 3/4 inch in thickness and not more than 1/2 inch greater in diameter than the outside diameter of the shell. Shells diminishing in diameter shall have welded points with a diameter of at least 8 inches.

- Steel Sheet Piles: Steel sheet piles shall conform to ASTM A328.