# SECTION 233 – GALVANIZING

## 233.01 – Description

These specifications cover the use and repair of zinc coatings (galvanizing) on a variety of materials.

## 233.02 – Detail Requirements

Galvanizing of fabricated items shall be performed after fabrication.

Galvanized items shall be stored off the ground in a manner that will allow free drainage of water from galvanized surfaces.

- Galvanizing of iron and steel hardware shall conform to ASTM A153 for the hot-dip process or ASTM B695, Class 50, for the mechanical process.

- Galvanizing of rolled, pressed, and forged steel shapes, plates, bars, and strips shall conform to ASTM A123.

## 233.03 – Repair of Galvanized Surfaces

Galvanizing surfaces that have been damaged or have uncoated areas shall be repaired in accordance with ASTM A780 except that repair materials shall not contain lead or cadmium.