# SECTION 234 – GLASS BEADS FOR REFLECTORIZING TRAFFIC MARKINGS

## 234.01 – Description

This specification covers glass beads applied on the surface or incorporated into traffic-marking materials so as to produce a retroreflective surface.

## 234.02 – Detail Requirements

Beads shall be manufactured from glass of a composition designed to be highly resistant to traffic wear and weather. Glass beads shall conform to AASHTO M247, Type 1-5, except that at least 80 percent of the beads shall be round when tested in accordance with ASTM D 1155, Procedure B.

The Contractor shall provide a written certification that each batch of glass beads used in or on VDOT pavement markings conforms to AASHTO M247 including the total concentration limit of Lead and Arsenic.