# SECTION 241 – FLY ASH

## 241.01 – Description

These specifications cover fly ash (burnt coal residue) used as an additive in hydraulic cement concrete or as a soil stabilizer.

## 241.02 – Detail Requirements

- Fly ash used in hydraulic cement concrete shall conform to ASTM C618, Class F, or Class C.

- Fly ash used in lime stabilization shall conform to ASTM C593. The Engineer may approve the use of bulk material if requested.