# SECTION 245 – GEOSYNTHETICS AND LOW PERMEABILITY LINERS

## 245.01 – Description

These specifications cover artificial fiber textile products to be used in transportation construction work, and low permeability liners for stormwater management facilities.

## 245.02 – Shipping, Handling, and Storage Requirements

Geosynthetic shall be permanently marked with a clearly legible print showing manufacturing plant or plant Identification Code number, located on the roll edge at least every 16 feet. Rolls shall be labeled at both ends of the outside of the roll outer wrapping and both ends of the inside of the geotextile roll core, and labels shall list the roll number, production date, AASHTO M288 class(es) the product meets, and the product name; if the permanent marking contains this information, the labels may be omitted.

Each geosynthetic roll shall be wrapped or otherwise packaged in a manner that will protect the geosynthetic, including the ends of the roll, from damage due to shipment, water, sunlight, and contaminants. The protective wrapping shall be maintained during periods of shipment and storage.

During storage, geosynthetics rolls shall be elevated off the ground and adequately covered to protect them from the following: site construction damage; precipitation; extended ultraviolet radiation including sunlight; strong acids or strong bases; flames including welding sparks; temperatures in excess of 160 degrees F; and other environmental conditions that may damage the physical property values of the geosynthetic. Geosynthetics that are not properly protected may be subject to rejection.

245.03—Testing and Documentation

Each geosynthetic material provided to the project shall have a manufacture date within its current NTPEP product 3-year evaluation cycle. The manufacturer and any subsequent private labeler facility shall be listed as compliant by NTPEP within the current calendar year, or immediate past calendar year with an application for audit for the current calendar year.

The Department may sample and test product from a facility or project at any time to verify compliance with specification requirements. Failure may result in the product being rejected or removed from the Approved List.

Property values in these specifications represent minimum average roll values (MARV) in the weakest principal direction unless direction is otherwise specified; permittivity values specified are minimum; AOS and panel vertical strain values are maximum; mass per unit area, UV degradation, and asphalt retention values are typical.

Product acceptance is determined by comparing the manufacturer test data against these specifications and using independent assurance testing, verification sampling and testing, and facility audits.

- Geotextile Fabric for Use in Silt Fences: Geotextile shall be a woven fabric and function as a vertical, permeable interceptor designed to remove suspended soil from overland water flow. Fabric shall filter and retain soil particles from sediment-laden water to prevent eroding soil from being transported off the construction site by water runoff.

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Filtering efficiency | ASTM D5141-11 and NTPEP Erosion Control Products Committee Work Plan | Min. 75% |
| Flow rate | ASTM D5141-11 and NTPEP Erosion Control Products Committee Work Plan | Min. 0.2 gal/ft2/min |

In addition to these requirements, the geotextile shall comply with the requirements of AASHTO M288, Table 7, Temporary Silt Fence Property Requirements, for grab strength and ultraviolet stability.

- Geotextile for Use as Riprap Bedding Material: Geotextile shall comply with the requirements of AASHTO M288, Table 3-Separation Geotextile Property Requirements, for apparent opening size and ultraviolet stability and Table 1-Geotextile Strength Property Requirements, Class 2, for grab strength and puncture strength.

- Geotextile Fabric for Use in Drainage Systems (Drainage Fabric): Drainage fabric shall be nonwoven and clog resistant, suitable for subsurface application, and thermally and biologically stable.

Polypropylene material is acceptable in environments with pH values between 3 and 12 inclusive; polyester material between 3 and 9 inclusive.

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Permittivity | ASTM D4491 | Min. 0.5 sec-1 |
| Apparent opening size | ASTM D4751 | Max. No. 50 sieve |

In addition to these requirements, the geotextile shall comply with the requirements of AASHTO M288 Table 1-Geotextile Strength Property Requirements, Class 3, for grab strength.

- Geotextile for Use in Stabilization: These are geotextiles used in saturated and/or unstable conditions to provide the functions of separation and reinforcement.

  - Subgrade Stabilization Fabric:

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Apparent opening size | ASTM D 4751 | Max. No. 20 sieve |

In addition to this requirement, the geotextile shall comply with the requirements of AASHTO M288 Table 1-Geotextile Strength Property Requirements, Class 3, for grab strength, tear strength, and puncture strength.

  - Embankment Stabilization Fabric Up to 6 Feet High:

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Apparent opening size | ASTM D 4751 | Max. No. 20 sieve |
| Seam strength | ASTM D 4632 | 90% specified grab strength |

In addition to this requirement, the geotextile shall comply with the requirements of AASHTO M288 Table 1-Geotextile Strength Property Requirements, Class 1 for grab strength, tear strength, and puncture strength.

- Prefabricated Geocomposite Pavement Underdrain: Prefabricated geocomposite pavement underdrain shall consist of a polymeric drainage core encased in a nonwoven filter fabric envelope having sufficient flexibility to withstand bending and handling without damage. Prefabricated geocomposite pavement underdrain shall conform to the following:

  - Core: The drainage core shall be made from an inert, polymeric material resistant to commonly encountered chemicals and substances in the pavement environment and shall have a thickness of not less than 3/4 inch. Outer surfaces shall be smooth to prevent excessive wear of bonded filter fabric.

| Physical Properties | Test Method | Requirements |
| --- | --- | --- |
| Compressive strength panel vertical strain and core area change | ASTM D1621/ D2412/D6364 | Min. 40 psi at 20% deflection after 24 hrs at 0 deg F and at 125 deg F |
| Water flow rate (after 100 hr at 10 psi normal confining pressure gradient of no more than 0.1) | ASTM D4716 | Min. 15 gal/min/ft width for 12-in specimen length |

  - Filter Fabric geotextile shall be bonded to and tightly stretched over the core. Geotextile shall not sag or block the flow channels, shall have a life equivalent to that of the core material, and shall conform to the requirements of (c) herein, except that grab strength shall meet AASHTO M288 Table 1, Class2.

- Geocomposite Wall Drains: Prefabricated geocomposite wall drain shall consist of a polymeric drainage core encased in a nonwoven filter fabric envelope having sufficient flexibility to withstand bending and handling without damage. Geocomposite wall drains shall conform to the following:

  - Core: The drainage core shall be made from an inert, polymeric material resistant to commonly encountered chemicals and substances in the roadway. Outer surfaces shall be smooth to prevent excessive wear of bonded filter fabric.

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Compressive strength at 20% deflection | ASTM D1621/ D2412/D6364 | Min. 40 psi after 24 hrs at 0 degree F and at 125 degree F |
| Water flow rate (after 100 hr at 10 psi normal confining pressure and gradient of no more than 1.0) | ASTM D4716 | Min. 15 gal/min/ft width (for 12-in specimen length) |

  - Filter Fabric: Geotextile shall be bonded to and tightly stretched over both sides of the core. Geotextile shall not sag or block the flow channels, shall have a life equivalent to that of the core material, and shall conform to the requirements of (c) herein, except that grab strength requirement shall meet AASHTO M288 Table 1, Class 2.

- Geomembrane Moisture Barrier: Geomembrane moisture barrier shall be resistant to biological attack. geomembrane shall be constructed of PVC and shall conform to the requirements of the PVC Geomembrane Institute 1104 material specification for PVC geomembrane (Revision #1 effective April 15, 2008) and shall meet the following additional or more stringent requirements:

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Thickness | ASTM D5199 | Min. 30 mils |
| Tensile (1-in strip) | ASTM D882 | Min. 0.80 kip/ft (ultimate) |
| Tear Strength (Die C) | ASTM D1004 | Min. 8 lbf |
| Seam Seal Strength | ASTM D1004 | Min. 0.18kip/ft |

- Dewatering Bag: A nonwoven geotextile sewn together to form a bag that can be used in lieu of a de-watering basin for the purpose of filtering out suspended soil particles. The bag shall be capable of accommodating the water flow from the pump without leaking at the spout and seams.

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Grab strength @ Elongation >50%(CRE/Dry) | ASTM D4632 | Min. 250 lb (min) |
| Seam strength | ASTM D4632 | 90% Specified grab strength |
| Puncture | ASTM D6241 | Min. 150 lb |
| Flow rate | ASTM D4491 | Min. 0.189 ft3/sec/ft2(min) |
| Permittivity | ASTM D4491 | Min. 1.2 sec-1 |
| UV resistance | ASTM D4355 | Min. 70% at 500 hr |
| AOS | ASTM D4751 | Max. 100 sieve |

- Pavement Interlayer products shall be listed on the Materials Division Approved List No. 63. All interlayer material shall be from National Transportation Product Evaluation Program (NTPEP)-compliant manufacturers, and shall be evaluated through NTPEP; tests not covered by the NTPEP Geosynthetics Work Plan shall be performed by independent, certified laboratories and submitted to the State Materials Engineer. Testing for products not covered by NTPEP shall be on a minimum 3-year cycle also. Terms defined by ASTM D4439 shall apply herein, except when they conflict with terms defined by Section 101.

For Paving Fabric, Paving Mat, Paving Grid, and Composite Paving Grid, the Contractor shall provide asphalt retention rates (ASTM D6140), material properties specified herein, and manufacturer’s recommendations for tack application to the Engineer at the preconstruction meeting. The total minimum tack coat application rate sprayed in the field shall meet the manufacturer’s recommendations, but shall be clearly totaled at the preconstruction meeting as the components of the asphalt retention rate and the additional rate based on the anticipated surface condition of the pavement.

  - Paving Fabric, Type I & II:  All paving fabrics shall meet the requirements of the table below, and have 50% retained strength after 500 hours of UV exposure when tested in accordance with ASTM D4355.

| Property | Test Method | Type I | Type II |
| --- | --- | --- | --- |
| Mass per unit area, min (oz/yd2) | ASTM D5261 | 4.5 | 4.1 |
| Grab Tensile Strength, min (lbs.) | ASTM D4632 | 120 | 101 |
| Grab Tensile Elongation, min (%) | ASTM D4632 | 50 | 50 |
| Melting point, min (F) | ASTM D276 | 3201 | 3201 |
| 1320 is the softening/melt point of polypropylene. See Section 318.03 for more on placement temperature. |  |  |  |

  - Paving Mat; Type I, II, and III: Materials used for paving mat shall be a hybrid of two or more of the following material types: fiberglass, polyester, or polypropylene.  Paving mat shall meet the requirements of the table below.

| Property | Test Method | Type I | Type II | Type III |
| --- | --- | --- | --- | --- |
| Tensile Strength, min (lb/in) | ASTM D5035 | 280 | 140 | 45 |
| Ultimate Elongation, max (%) | ASTM D5035 | 5 | 5 | 5 |
| Melting Point, min (°F) | ASTM D276 | 3201 | 3201 | 3201 |
| Mass/Unit Area, min (oz/yd2) | ASTM D5261 | 7.0 | 4.0 | 4.0 |
| 1320 is the softening/melt point of polypropylene, which is lower than either polyester or fiberglass. See Section 318.03 for more on placement temperature. |  |  |  |  |

  - Paving Grid: Type I, II, & III:  Materials used for paving grids shall be comprised of fiberglass and shall meet the requirements of the table below.  Some paving grids are self-adhesive and some require nails for installation.  Tack coat required for the installation of the overlay shall be specified with the paving grid.  Refer to manufacturer’s recommendations for tack coat type and application rate.

| Property | Test | Type I | Type II | Type III |
| --- | --- | --- | --- | --- |
| Tensile Strength, min (lbs/in)1 | ASTM D6637, Method A, modified | 560 x 1,120 | 560 | 280 |
| Aperture size, min (in) | Calipered | 0.5 | 0.5 | 0.5 |
| Elongation, max (%) | ASTM D6637 | 3 | 3 | 3 |
| Mass per area, min (oz/yd2) | ASTM D5261 | 16 | 10 | 5.5 |
| Melting Point, min (°F) (fabric component – if applicable) | ASTM D276 | 4202 | 4202 | 4202 |
| 1For Type I, machine and cross direction respectively. Strengths for Type II and III are in both directions |  |  |  |  |

  - Composite Paving Grids: Type I, II, & III: Composite paving grids shall consist of a fiberglass, polyester, or polyvinylacetate (PVA) paving grid integrated with a nonwoven geotextile and meet the requirements of the table below.

| Property | Test | Type I | Type II | Type III |
| --- | --- | --- | --- | --- |
| Tensile Strength, Min (lbs/in)1 | ASTM D6637, Method A, modified | 560 x 1,120 | 560 | 280 |
| Aperture size, Min (in) | Calipered | 0.5 | 0.5 | 0.5 |
| Elongation, Max (%) | ASTM D6637 | 5 | 5 | 10 |
| Mass per area, Min (oz/yd2) | ASTM D5261 | 16 | 10 | 5.5 |
| Melting Point, Min (°F) (fabric component) | ASTM D276 | 3202 | 3202 | 3202 |
| 1For Type I, machine and cross direction respectively. Strengths for Type II and III are in both directions. 2320 is the assumed softening/melt point of PVA. See Section 318.03 for more on placement temperature. |  |  |  |  |

  - Pavement Repair and Bridge Deck Waterproofing Strip Membrane: Materials used for strip membranes shall be comprised of composite self-adhering rubberized asphalt attached to a pavingfabric, a paving mat, or a paving grid and meet the requirements of the table below.

| Property | Test Method | Type I |
| --- | --- | --- |
| Strip Tensile Strength, min (lb/in) | ASTM D882 | 50 |
| Puncture Resistance, min (lbs) | ASTM E154 | 200 |
| Permeance-Perms, max | ASTM E-96 Method B | 0.05 |
| Pliability - 1/4" Mandrel 180⁰ Bend at -25 ⁰F | ASTM D146 | No cracks in fabric or rubberized asphalt |

- Low Permeability Liners for Stormwater Management Facilities: SWM liner soil shall be classified as CL, CH or MH in accordance with ASTM D2487 and shall have a maximum coefficient of permeability of 1 x 10-6 cm/sec in accordance with ASTM D5084, after compaction. The maximum particle size shall be three inches in its largest dimension. Natural soils, which do not meet these specifications, may be blended with bentonite to provide the specified permeability characteristics.

Geosynthetic Clay Liner shall have a maximum coefficient of permeability of 1 x 10-8 cm/sec in accordance with ASTM D5887.

This specification is not intended for dam embankment material or clay core cut-off trench material.

- Fabric for Use in Turbidity Curtains shall consist of synthetic fabric coated with suitable elastomeric or polymeric compound. The coating shall have a high resistance to weathering, hydrocarbons, fresh and salt water, and temperature extremes. The curtain shall form a continuous vertical and horizontal barrier for the entire width and length of each section. Seams, if required, shall be either vulcanized welded or sewn and shall develop the full strength of the fabric.

The curtain fabric shall meet the minimum requirements noted below:

| Physical Properties of Turbidity Curtain Fabric |  |
| --- | --- |
| Physical Property | Requirement |
| Weight (oz/yd2) |  |
| Type I | 18 |
| Type II | 22 |
| Type III | 22 |
| Grab Tensile Strength (ASTM D 4632) | 300 lbs |
| UV Inhibitor | Required |