# SECTION 250 – CARBON FIBER MESH

## 250.01 – Description

These specifications cover carbon fiber mesh used along with EP-7 epoxy to seal joints in between box beam bridges and other bridge joints.

## 250.02 – Materials

- Carbon Fiber Mesh Materials shall conform to the following:

The carbon fiber mesh is comprised of high tensile strength carbon fiber strips 4 inches in width. The mesh is not impregnated, wets out with the epoxy, and cured in place in epoxy resin overlay.

| General Information |  |
| --- | --- |
| Constituent Materials: | 6K Carbon Fiber unidirectional tows |
| Primary Fiber Directions | Closed knit 0° X 90° |
| Color | Black |

| Carbon Material Properties | Requirement | Test Method |
| --- | --- | --- |
| Nominal Thickness | 0.030 inch |  |
| Nominal Tensile Strength per unit width | 400,000 psi | ASTM D3039 |
| Nominal Tensile Modulus | 33,000,000 psi | ASTM D3379 |
| Failure Strain | 1.3% | ASTM D3379 |
| Grid Spacing | 1/4” x 1/4” (inch) (longitudinal x transverse) |  |