# SECTION 252 – GRAVITY-FILL POLYMER CRACK SEALERS

## 252.01 – Description

These specifications cover polymers used for gravity-filling sealing cracks in hydraulic cement concrete surfaces.

## 252.02 – Materials

Gravity-fill polymer crack sealers shall be a high molecular weight methacrylate, epoxy, or urethane conforming to the following:

| Properties of Gravity-filled Polymers |  |  |
| --- | --- | --- |
| Property @ 75 ± 5 °F | Test Method | Requirement |
| Gel Time, 50 ml sample | ASTM C881 | 6 hrs. max. |
| Tensile Strength | ASTM D638 | 1,500 psi min. |
| Sand Penetration, MX-45 sand | VTM 101 | 80% min. |