# SECTION 417 – DAMP-PROOFING

## 417.01 – Description

This work shall consist of furnishing and applying damp-proofing material to concrete surfaces in accordance with the plans and these specifications.

## 417.02 – Materials

Materials shall conform to Section 213 as applicable.

## 417.03 – Procedures

- Surface Preparation: Surfaces shall be cleaned of loose, foreign material or other substances, materials, etc. than may inhibit or prohibit successful continuous application and shall be dry. The Engineer may require the surface to be scrubbed with water and a stiff brush, after which it shall be allowed to dry before application of primer.

- Application: The cleaned surface shall be brush painted or spray painted with at least two coats of primer, using at least 1/8 gallon per square yard of surface area per coat. On the primed surface, one application of an asphalt seal coat shall be applied by brush, using at least 1/10 gallon per square yard.

Asphalt shall be confined to areas to be damp-proofed and shall not be dripped or spread on any other parts of the structure. The Contractor shall take protective measures and exercise care to prevent asphalt from being applied to non-designated areas.

## 417.04 – Measurement and Payment

Damp-proofing, when a pay item, will be measured in square yards and will be paid for at the contract unit price per square yard. The price shall include damp-proofing materials, surface preparation, protective measures, and application. When not a pay item the cost of damp-proofing shall be included in the price for other appropriate pay items.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Damp-proofing | Square yard |