GUIDELINES — Use when requested by the Designer.{2007-S208B00}

SP208-DB0100-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

SECTION 208—SUBBASE AND AGGREGATE BASE MATERIAL

Crushed Hydraulic Cement Concrete (CHCC)

January 10, 2019

SECTION 208—SUBBASE AND AGGREGATE BASE MATERIAL of the Specifications is amended as follows:

Section 208.02—Materials is replaced with the following:

(a)	Subbase material may consist of any mixture of natural or crushed gravel, crushed stone or slag, crushed hydraulic cement concrete (CHCC), and natural or crushed sand; with or without soil mortar. Subbase material may be used in a stabilized or unstabilized form.

(b)	Aggregate base material may be designated as Type I or Type II as follows:

Type I shall consist of crushed stone, crushed slag, crushed hydraulic cement concrete (CHCC), crushed gravel or any combination of these materials: with or without soil mortar or other admixtures. Crushed gravel shall consist of particles of which at least 90 percent by weight of the material retained on the No. 10 sieve shall have at least one face fractured by artificial crushing.

Type II shall consist of gravel, stone, or slag screenings; fine aggregate and crushed coarse aggregate; sand-clay-gravel mixtures; crushed hydraulic cement concrete; or any combination of these materials; with or without soil mortar or other admixtures. Aggregate base materials Type I or II may be used in a stabilized or unstabilized form.

(c)	Crushed Hydraulic Cement Concrete shall not be used as Subbase or aggregate base material when any subsurface drainage system, such as standard underdrains (UD-4 or UD-5) and /or a stabilized open graded aggregate drainage layer (OGDL) is present, except when the CHCC is cement stabilized.

Section 208.03(b) Atterberg Limits is amended to include the following:

Plasticity: Subbase and aggregate base materials shall be either non-plastic (PI=0) or shall conform to Table II-11 of the Specifications when tested according to VTM-7. If the material is classified as non-plastic (PI=0), according to VTM-7, the Liquid Limit requirement will be waived. Exceptions to this provision are noted as follows:

1.	100% CHCC and 20% or less CHCC Blends will be tested and subject to penalty as noted in Table II-11 of the Specifications for the plasticity index, excluding Liquid Limit penalties.

2.	Greater than 20% CHCC Blends will follow testing guidelines as set forth in Section 208.06 (b) for Atterburg limits.

Section 208.03 is amended to add the following:

(h)	Deleterious Material: The quantity of deleterious materials present in stockpiles of Crushed Hydraulic Cement Concrete, to be used in blending with virgin aggregates or as 100 percent CHCC, shall not exceed the following values:

| MATERIAL | PERCENT BY WEIGHT (MASS) |
| --- | --- |
| Asphalt Concrete | 5.0 |
| Glass and Metals | 5.0 |
| Wood, Plastic, Brick and other foreign matter | 0.5 |

Section 208.04—Job-Mix Formula is replaced by the following:

(a)	The Design-Builder shall submit, or shall have the source of supply submit, for the Engineer’s approval, a job-mix formula for each mixture to be supplied for the project prior to starting work. The formula shall be within the design range specified in Table II-9 of the Specifications. If unsatisfactory results or other conditions make it necessary, the Design-Builder shall prepare and submit a new job-mix formula for approval.

(b)	A job mix formula shall be submitted for the Engineer’s approval for each category of CHCC mixture used. Designated categories shall indicate the mixture percentage of CHCC used according to the following criteria:

1.	Category 1: 100% CHCC

Category 2: 20% or less CHCC ( 20%)

Category 3: greater than 20% CHCC but less than 100% CHCC (>20%<100%)

2.	The quantity of CHCC in the mix shall be expressed as a percentage of the total mix.

Section 208.06—Acceptance is amended to include the following:

The following applies specifically to the use of Crushed Hydraulic Cement Concrete (CHCC) mixtures in addition to the acceptance criteria specificed in this section:

1.	100% CHCC shall conform to this special provision.

2.	20% or Less CHCC Blends shall conform to this special provision.

3.	Greater than 20% CHCC Blends shall conform to the following:

a.	The virgin aggregate portion of the blend will be tested for Atterberg limits, prior to CHCC blending.

b.	Price adjustments for Liquid Limit and the Plasticity Index of the virgin aggregates used in the blend with CHCC shall be according to Table II-11 of the Specifications.

c.	No additional testing for Liquid Limit or Plasticity Index will be required on the final blended product.

4.	All shipments of products containing CHCC must be designated on the shipping ticket (scale ticket) by the use of the letter “R”. Examples: [22R, 21AR and 21BR] for: Aggregate Base material, Type I or Subbase materials.