GUIDELINES — For use on Asphalt Schedule Work - Plant Mix projects.  Include SP315-000100-02. {2007-S211HP0}

SP211-000100-02

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

SECTION 211—ASPHALT CONCRETE

March 28, 2022

SECTION 211—ASPHALT CONCRETE of the Specifications is amended as follows:

Section 211.03(a) SUPERPAVE mixes is amended by inserting the following:

For SM-9.5 and SM-12.5 mixes, the minimum asphalt contents shall be based on the following unless otherwise approved by the Engineer:

| Bulk Specific Gravity of the Total Aggregate | Minimum Design AC Content Mix Type (%) |  |
| --- | --- | --- |
|  | SM-9.5 | SM-12.5 |
| Less Than 2.65 | 5.5 | 5.3 |
| 2.65 - 2.74 | 5.4 | 5.2 |
| 2.74 - 2.85 | 5.3 | 5.1 |
| Greater Than 2.85 | 5.2 | 5.0 |

Section 211.09—Adjustment System is amended to replace the third paragraph with the following:

If the total adjustment for a lot is greater than 25 points, the Contractor shall remove the failing material from the road.  If the total adjustment is 25 points or less and the Contractor does not elect to remove and replace the material, the unit price for the material will be reduced by 3% for SM, IM, and BM Superpave mixes, and by 1% for all other mixes, for each adjustment point the material is outside of the process tolerance.  The Engineer will apply this adjustment to the tonnage represented by the samples. If the Engineer applies adjustment points against two successive lots, the Contractor shall ensure plant adjustment is made prior to continuing production.

Section 211.09—Adjustment System is amended to replace the last paragraph with the following:

The Engineer will reduce the unit bid price for SM, IM, and BM Superpave mixes by  1.0%, and for all other mixes by 0.5%, for each adjustment point applied for standard deviation.

The Engineer will increase the unit bid price for SM, IM, and BM mixes by 5% if the following criteria are met: 1) the standard deviation of the AC content is within the ranges of 0.0 – 0.15; 2) there are no adjustment points assigned for any sieve sizes as noted in Table II-16; and 3) the average AC content is no less than 0.10% below and no more than 0.20% above the approved mix design AC content.