GUIDELINES: Use when requested by the Designer for asphalt projects. Include SP315-000400-01.

SP211-000400-01

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

COLD CENTRAL PLANT RECYCLING MATERIAL

March 10, 2020

- DESCRIPTION

These specifications cover the requirements for Cold Central Plant Recycling Material (CCPRM). Cold Central Plant Recycling (CCPR) is a process in which recycled asphalt concrete pavement is processed and stabilized using foamed asphalt or emulsified asphalt at a plant and then placed using conventional asphalt paving equipment. CCPRM shall not be used as a final riding surface.

- MATERIALS

  - Stabilizing Agents (Emulsified or Foamed Asphalt) shall be emulsions or PG binders (conforming to Section 210 of the Specifications; liquid asphalts shall be a neat (i.e., not modified) asphalt that conforms to Section 211.02 of the Specifications.

  - Water used for mixing shall conform to Section 216 of the Specifications.

  - Crushed Reclaimed Asphalt Pavement (RAP) Material shall conform to Section 211.02(j)4 of the Specifications and Table 1.

| Table 1 Crushed RAP Properties |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Deleterious Materials: Clay Lumps and Friable Particles in Aggregate | AASHTO T 112 | 0.2% maximum |
| Maximum Sieve Size, 1.5 in | AASHTO T 27 | 100% Passing |

  - Aggregate: Based on the results of the Job Mix Formulae (JMFs) or other requirements of this provision, the Contractor shall determine if additional aggregate is required. If the Contractor determines additional aggregate is needed any additional aggregate shall conform to Section 203 of the Specifications and Table 2, and shall be graded to conform to Table 3. The percentage of additional aggregate used in the mixture shall not exceed 50%.

  - Additional Additives may be used to meet the requirements in Table 4. In the case where an additional additive is used, the type and dosage must be described in the JMFs submitted to the Department.

| Table 2 Aggregate Properties |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Los Angeles Abrasion Value | AASHTO T 96 | 45% maximum loss |
| Sand Equivalent | AASHTO T 176 | 45% minimum |
| Maximum size, 100% Passing, Sieve Size | AASHTO T 27 | 1.5 inches |
| Water absorption | AASHTO T 85 | 3% maximum |

- Job-Mix Formula

A JMF for CCPRM shall be submitted to the District Materials Engineer for approval at least 30 Days before the start of CCPRM operations. More than one JMF may be required. The gradation of each JMF shall fall within the bands shown in Table 3.

| Table 3 CCPRM Design Range |  |  |
| --- | --- | --- |
| Sieve Size | Percentage by Weight Passing Square Mesh Sieves1 |  |
|  | Lower | Upper |
| 1.5” | 100 | 100 |
| 3/4" | -- | -- |
| 3/8” | -- | -- |
| No. 4 | -- | -- |
| No. 2002 | 2 | 9 |
| 1Values based on AASHTO T 27 using washed, pulverized materials, prior to stabilization. 2For CCPRM using Foamed Asphalt, cement can be used as a portion of the material passing the No. 200 sieve. |  |  |

The Contractor shall establish, as part of the JMF, a target percent passing for the 1.5”, 3/4", 3/8”, No. 4 and No. 200 sieves. The JMFs shall be created using either existing materials obtained directly from the project site (prior to the start of construction) or from an existing stockpile of Reclaimed Asphalt Pavement (RAP). The Contractor may add additional aggregate to material from the project site or RAP stockpile to establish the JMF. Sampling shall be conducted at least once per 2500 lane-feet when sampled from the road. When sampling from a stockpile, material shall be taken from various locations around the stockpile and combined to produce a representative sample. Each JMF shall provide as a minimum the following mix design parameters:

- Maximum Dry Density at Optimum Moisture Content

- Percent by weight of all stabilizing agents to be added to the recycled mix

- Percent by weight of water (at room temperature) required

- Expansion ratio and half-life characteristics and temperature of asphalt binder at the time of dosage into foaming chamber (for mixtures using foamed asphalt), minimum curing time or set time for the emulsified asphalt and temperature of emulsified asphalt at the time of dosage into the mixture (for mixtures using emulsified asphalt)

- Target gradation for sieve sizes 1.5”, ¾”, 3/8”, No. 4 and No. 200 (including any aggregate to be added).

Within the first production lot, the Contractor may revise the approved JMF using the production materials from lot 1. The revised JMF shall include the Moisture Density Relations according to AASHTO T 180 Method D, percentage by weight of stabilizing agent content, Target gradation for sieve sizes 1.5”, ¾”, 3/8”, No. 4 and No. 200 (including any aggregate to be added),and shall meet the CCPRM Mix Design criteria of Table 4 at the approved stabilizing agents content. The revised design shall be submitted to the District Materials Engineer by the end of the first lot of production for approval prior to use.

If a change in source materials is made during construction, the Contractor shall create new JMFs and submit them to the District Materials Engineer for approval before use. The JMFs shall conform to Tables 4A or 4B at the approved stabilizing agent content.

- QUALITY CONTROL PLAN

The Contractor shall develop and implement a Quality Control Plan to ensure that operational techniques and activities are controlled to provide a homogeneous and finished material of acceptable quality meeting this Special Provision.  The Contractor shall provide the Quality Control Plan and Job Mix Formulae to the Department for approval at least 30Days before the start of CCPRM operations.

| Table 4A CCPRM Mix Design Criteria Emulsified Asphalt Stabilized Materials |  |  |  |
| --- | --- | --- | --- |
| Item | Property | Test Method | Criteria |
| 1 | Moisture Density Relations | AASHTO T 180, Method D | Determined by Design |
| 2 | Marshall Stability Test (min)1, 2 | ASTM D5581 or AASHTO T 245 | 2945 lbs (ASTM) 1475 lbs (AASHTO) |
| 3 | Retained Stability1, 3 | ASTM D5581 or AASHTO T 245 | 70% of results from Item 2 |
| 4 | Raveling Stability4 | ASTM D7196 | Maximum 6% |
| 5 | Materials Gradation Test prior to stabilization | AASHTO T 27 | Gradation to control field production. |
| 1The Contractor may test this property using either ASTM D5581 or AASHTO T 245 and compare to the criteria corresponding to that test. 2Three specimens shall be produced at 75 blows per side (or 30 gyrations per AASHTO T 312), cured at 140ºF to constant mass, and held at 104ºF for 2 hours in a forced draft oven immediately before testing. 3An additional three specimens shall be produced at cured at 140ºF to constant mass. Specimens shall then be vacuum saturated to 55-65%, in a 77ºF water bath for 23 hours and 104ºF water bath for an additional hour immediately before testing 4Specimens shall be produced using a gyratory at 20 gyrations and cured at 50ºF for 4 hours at 50% humidity. |  |  |  |

| Table 4B CCPRM Mix Design Criteria Foamed Asphalt Stabilized Materials |  |  |  |
| --- | --- | --- | --- |
| Item | Properties | Test Method | Criteria |
| 1 | Moisture Density Relations | AASHTO T 180, Method D | Determined by Design |
| 2 | Dry Indirect Tensile Strength (ITS)1 | AASHTO T 283 Section 11 | 53 psi minimum |
| 3 | Retained Indirect Tensile Strength2 | AASHTO T 283 Section 11 | Min 70% of the Dry ITS |
| 4a | Expansion Ratio (Aggregate temperature 50ºF to 77ºF) | Wirtgen 2012 Cold Recycling Manual | 10 times |
| 4b | Expansion Ratio (Aggregate temperature greater than 77°F) | Wirtgen 2012 Cold Recycling Manual | 8 times |
| 5 | Half-Life | Wirtgen 2012 Cold Recycling Manual | 6 second minimum |
| 6 | Materials Gradation Test, prior to stabilization | AASHTO T 27 | Gradation to control field production. |
| 1Three (3) specimens shall be produced using 75 blows per side (or 30 gyrations per AASHTO T 312) compacted at or below Optimum Moisture Content and oven dried at 104ºF (40°C) for 72 hrs and cool to ambient temperature for 24 hrs. 2An additional three (3) specimens shall be produced and cured according to Item 2 Dry Indirect Tensile Strength. Specimens shall be oven dried at 104ºF (40ºC) for 72 hrs, and then submerged in 77ºF (25ºC) water bath for 24 hours prior to testing. |  |  |  |

For each CCPRM project, a project specific Quality Control Plan is required, and shall include the following (minimum) information:

  - A description of the Contractor’s Quality Control organization, including the number of full-time equivalent employees or Sub-Contractors with specific Quality Control responsibilities and an organizational chart showing lines of authority and reporting responsibilities.

  - 2.	. A list of Cold Asphalt Recycling Plant and Field Technicians conforming to Section 200.06 of the Specifciations who will work on the Project.

  - A Quality Control Sampling, Testing and Analysis Plan with methods that include a description of how random locations for testing and sampling are determined. All samples will be taken at the plant unless otherwise directed by the Engineer.

  - Identification and description (including any accreditation) of the laboratories to be used for each type of testing. Lab shall conform to Section 106.07 of the Specifications.

  - Specify documentation for Quality Control activities.

  - Procedures to meet Contract requirements for corrective action when Quality Control criteria are not met.

  - Procedures to protect stabilized material from receiving excessive moisture from weather events (e.g. rain, fog, etc.) and corrective actions when criteria are not met.

  - Contingency Plan including:

      - Inclement weather

      - Equipment breakdowns

      - Materials shortages

      - Deficient density of installed CCPRM

      - Material doesn’t break or cure in timely manner

      - Gradation is outside tolerances

      - Production modifications based on changes in ambient or material temperature.

- ACCEPTANCE

  - Gradation: CCPRM acceptance for gradation will be based on a mean of the results of eight tests performed on pre-stabilized samples taken in a stratified random manner from each 4,000-ton lot (8,000-ton lots may be used when the normal daily production of the source from which the material is being obtained is in excess of 4,000 tons).

A lot will be considered to be acceptable for gradation if the mean of the test results obtained is within the tolerance allowed for the JMF as specified in Table 5. If a lot does not conform to the acceptance requirements for gradation, the Department will determine variability and adjustment points in accordance with Section 211.09 of the Specifications.

If gradation fails to meet the requirements, the Department at its discretion reserves the right to require appropriate measures that may include stopping the work.

  - Stabilizing Agent Content: The Contractor will provide a computer printout of the stabilizing agent content percentage of the plant at the time of sampling with each gradation sample. If the dosage rate varies by more than 0.20 percentage points from the approved JMF target, then paving and production shall stop and the Contractor shall take corrective measures to bring the dosage rate within tolerance of the approved JMF. In addition, a daily summary of the stabilizing agent content percentage shall be provided to the Department.

  - Moisture Content will be reported for each Asphalt Content test.  After drying in accordance with Section VI-1, the following equation shall be used:

% Moisture=Original Mass-Final MassFinal Mass×100

  - Marshall Stability – The compaction method used for design to produce the specimens shall be used during production. When emulsified asphalt is used as the stabilizing agent, acceptance for Marshall Stability will be based on results of samples taken in a stratified random manner at a frequency of at least one per day or one per 1,000 tons per mix per day if more than 1,000 tons are produced daily.   The following pay adjustment will be applied for the tonnage represented by the sample result:

| Marshall Stability (6 inch specimen) | Marshall Stability (4 inch specimen) | % of Payment |
| --- | --- | --- |
| 2945 lbs or greater | 1475 lbs or greater | 100 |
| 2500 to 2944 lbs | 1250 to 1474 lbs | 95 |
| Less than 2500 lbs1 | Less than 1250 lbs1 | Remove and Replace |
| 1The Contractor shall immediately cease production and notify the Department when results fall below 2500 lbs (6 inch) or 1250 lbs (4 inch). The Contractor shall make any necessary corrective actions to the mix and provide verification to the Engineer that it conforms to the approved job-mix formula before resuming production. |  |  |

  - Dry Indirect Tensile Strength: The compaction method used for design to produce the specimens shall be used during production. When foamed asphalt is used as the stabilizing agent, acceptance for Dry Indirect Tensile Strength will be based on results of samples taken in a stratified random manner at a frequency of at least one per day or one per 1,000 tons per mix per day if more than 1,000 tons are produced daily. The following pay adjustment will be applied for the tonnage represented by the sample result:

| Dry Indirect Tensile Strength | % of Payment |
| --- | --- |
| 53 psi or greater | 100 |
| 45 psi to 52 psi | 95 |
| Less than 45 psi1 | Remove and Replace |
| 1The Contractor shall immediately cease production and notify the Department when results fall below 45 psi. The Contractor shall make any necessary corrective actions to the mix and provide verification to the Engineer that it conforms to the approved job-mix formula. |  |  |

  - Half-Life and Expansion Ratio: The Contractor shall verify and provide reports to the Department confirming that each load of asphalt binder used for foaming conforms to Table 4B.

| Table 5 Process Tolerance |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Tolerance on Each Laboratory Sieve and Asphalt Content: Percent Plus and Minus |  |  |  |  |  |
| No. Tests | 1 ½” | 3/4" | 3/8” | No. 4 | No. 200 |
| 1 | 0.0 | 8.0 | 8.0 | 8.0 | 2.0 |
| 2 | 0.0 | 5.7 | 5.7 | 5.7 | 1.4 |
| 3 | 0.0 | 4.4 | 4.4 | 4.4 | 1.1 |
| 4 | 0.0 | 4.0 | 4.0 | 4.0 | 1.0 |
| 5 | 0.0 | 3.6 | 3.6 | 3.6 | 0.9 |
| 6 | 0.0 | 3.3 | 3.3 | 3.3 | 0.8 |
| 7 | 0.0 | 3.0 | 3.0 | 3.0 | 0.8 |
| 8 | 0.0 | 2.8 | 2.8 | 2.8 | 0.7 |
| 12 | 0.0 | 2.3 | 2.3 | 2.3 | 0.6 |

  - Testing Records: The Contractor shall prepare separate test reports meeting the requirements of AASHTO R 18. Records documenting the test results from Tables 4A and 4B shall be provided to the Engineer.

- TESTING

  - Asphalt Content:  The Contractor shall perform Asphalt Content testing and report the results as extractable asphalt or weight after ignition in accordance with VTM 102. The Contractor shall determine a RAP correction factor according to VTM 102. For production samples, testing shall be conducted at a rate of 1 sample per 1,000 tons and the material shall be cured to constant weight in an oven at 225°F until the weight loss in a two hour period does not exceed 0.02% by weight (e.g., for a 5000 gram sample, the sample does not lose more than 1 gram in a two hour period). There will be no price adjustment for asphalt content.

  - Retained Stability and Retained Indirect Tensile Strength: The Contractor shall calculate and report the retained stability or retained indirect tensile strength for each Marshall Stability or Dry Indirect Tensile Strength test performed.

- EQUIPMENT

  - CCPRM Plant shall be capable of homogeneously incorporating all stabilizing agents and materials up to the sizes shown in Table 3. The plant shall be capable of delivering the amount of additives to within +/- 0.2% of the required amount by weight of the pulverized bituminous material, except that a capability of adding up to 5% water by weight of the pulverized bituminous material is mandatory. Automated systems shall be used to regulate the application of stabilizing agents and water and shall adjust automatically to the mass of the material being processed. When using foamed asphalt, the plant shall also be outfitted with a test or inspection nozzle at one end of the spray bar that can produce a representative sample. The plant shall be capable of maintaining the temperature of the liquid asphalt at a minimum of 300°F. The plant shall be equipped with the means for the operator to verify the stabilizing agents and water are being evenly distributed and that the correct dosage rates of each are being applied. The plant shall have the ability to print out stabilizing agents and water quantities used during production. The equipment shall be operated according to the manufacturers’ recommendations.

  - Plant Scales:  Scales shall be approved according to Section 109.01 of the Specifications.

  - Trucks, Truck Scales and Automatic Printer System:  Shall conform to Section 109.01 of the Specifications.

- WEATHER LIMITATIONS

CCPRM shall be produced when both the atmospheric temperature and material to be processed (measured in the shade and away from artificial heat) is at least 50°F.  CCPRM production shall not begin when the weather forecast calls for freezing temperatures within 48 hours after placement of the CCPRM on any portion of the project.