Guidelines: For use in projects where plans specify VHPC for use in VA Adjacent Member (voided slabs and box beams typically) Connection block-outs and Shear Keys.

SP217-000100-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

VERY HIGH PERFORMANCE CONCRETE (VHPC)

February 8, 2021

- DESCRIPTION

This work shall consist of furnishing and placing Very High Performance Concrete (VHPC) described herein as shown on the Plans, and directed by the Engineer.

- MATERIALS

VHPC is used to fill shear keys and Virginia Adjacent Member Connection block outs between prestressed concrete elements and other locations as shown on the Plans. It shall conform to Tables 1 or 2 or provide deflection hardening such that the ultimate strength is at least 5% higher than the first crack strength when tested in accordance with ASTM C1609 at 28 days.

The mixtures shall be self-consolidating as shown in Table 3.

| Table 1 Mixture proportions using fly ash and silica fume in lbs/yd3 (except where noted) |  |  |
| --- | --- | --- |
| Mix Component1 | VHPC FA w CA | VHPC FA w sand |
| Type I/II Cement | 1,120 | 1,120 |
| Silica Fume | 240 | 240 |
| Fly Ash | 240 | 240 |
| Slag Cement | --- | --- |
| Sand, Grading A2 | 1,450 | 2,000 |
| No. 8 or 8P Stone | 620 | --- |
| Max. w/c3 | 0.25 | 0.25 |
| Steel fibers4 | 265 | 265 |

- Mix components are subject to the tolerances indicated in Section 217.04 of the Specifications. - Relative densities of 2.57 for sand, 2.25 for silica fume, 2.25 for fly ash, 2.90 for slag cement, and 2.70 for No. 8 or 8P stone are used in the calculations. Sand amount may need to be adjusted to yield a 1 cubic yard material based on actual relative densities of ingredients. Air content is assumed to be 2%. - w/c = water-cementitious materials ratio. - Steel fibers shall conform to ASTM A820 with a length ranging from 1 to 1.4 in and have hooked ends. Steel fiber used shall require documentation using Form C-76. This form documents that the steel fibers are domestic or, if foreign, allows for documentation of a minimal use exclusion if applicable. It is the Contractor’s responsibility to ensure one of these two requirements are met or payment for the fibers will not be permitted

| Table 2 Mixture proportions using fly ash or slag cement in lb/yd3 (except where noted) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Mix Component1 | VHPC FA w CA | VHPC FA w sand | VHPC S w CA | VHPC S w sand |
| Type I/II Cement | 1,120 | 1,120 | 800 | 800 |
| Silica Fume2 | ---- | ---- | --- | --- |
| Fly Ash 2 | 480 | 480 | --- | --- |
| Slag Cement2 | --- | --- | 800 | 800 |
| Sand, Grading A2 | 938 | 1,680 | 939 | 1,817 |
| No. 8 or 8P Stone | 934 | --- | 942 | --- |
| Max. w/cm3 | 0.25 | 0.25 | 0.25 | 0.25 |
| Steel fibers4 | 265 | 265 | 265 | 265 |
| 1Mix components are subject to the tolerances indicated in Section 217.04 of the Specifications. 2Relative densities of 2.57 for sand, 2.25 for silica fume, 2.25 for fly ash, 2.90 for slag cement, and 2.70 for No. 8 or 8P stone are used in the calculations. Sand amount may need to be adjusted to yield a 1 cubic yard material based on actual relative densities of ingredients. Air content is assumed to be 2%. 3w/c = water-cementitious materials ratio. 4Steel fibers shall conform to ASTM A820 with a length ranging from 1 to 1.4 in and have hooked ends. Steel fiber used shall require documentation using Form C-76. This form documents that the steel fibers are domestic or, if foreign, allows for documentation of a minimal use exclusion if applicable. It is the Contractor’s responsibility to ensure one of these two requirements are met or payment for the fibers will not be permitted. |  |  |  |  |

The components of VHPC shall conform to Section 217 of the Specifications.

Batches may be produced using pre-packaged (bag) VHPC materials identified in the VHPC section of Approved List 54 for the specified application in the Plans. Use of pre-packaged VHPC materials does not alleviate the requirements for acceptance testing of the trial and production batches.

Self-consolidating concrete (SCC) requires high-range water-reducing agent (HRWRA); dosage rate can range from 10 oz/cwt to 60 oz/cwt depending on the ingredients and the efficiency of the mixer. Air entraining admixture is not required.

- MIXING PROCEDURES

Batch size should not exceed one-third of the mixer capacity for both small and large batches.  The Contractor may submit alternate mixing procedures that evenly distribute the fibers throughout the mix to the Engineer for approval. Self-consolidating concretes, such as VHPC, require longer mixing times to achieve the consistency for placement compared to normal concrete mixes.

  - Small Batches (1 cubic feet to 1 cubic yard) shall be mixed using a mortar mixer with rotating paddles and the following mixing sequence, unless otherwise approved by the Engineer:

- Wet mixer and pour out excess water.

- Mix the sand and limestone in the mixer with half of the water in order to control the dust until the materials are dispersed evenly.

- Add the fibers and mix until they are dispersed evenly throughout the mixture.

- Add the cement, fly ash and silica fume. Slowly pour the remaining water into the mixer.

- Add the high-range water reducer in increments until the desired consistency is achieved and then perform the inverted slump cone test and measure spread. Spread shall be in accordance with Table 3, with no evidence of segregation. Add additional HRWRA as needed to achieve required spread.

If pre-packaged (bag) materials are used, they shall be mixed in accordance with the manufacturer’s recommendations.

  - Large Batches (1 cubic yard or larger) shall be mixed using a mortar mixer with rotating paddles, stationary mixers at the concrete plant or ready mixed concrete trucks and the following mixing sequence, unless otherwise approved by the Engineer:

- Mix the sand and limestone in the mixer with half of the water until the materials are dispersed evenly.

- Add the silica fume and fibers and mix at high RPM for at least 5 minutes or until the material is homogeneous, whichever is longer.

- Add the cement and fly ash.

- Add remaining water to wash the drum fins and mix at high RPM for at least 5 minutes or until the material is homogeneous, whichever is longer.

- Add the high-range water reducer in increments until the desired consistency is achieved.

- Perform the inverted slump cone test and measure spread. Spread shall be in accordance with Table 3, with no evidence of segregation. Add additional HRWRA as needed to achieve required spread.

If pre-packaged (bag) materials are used, they shall be mixed in accordance with the manufacturer’s recommendations.

- TRIAL BATCHING

At least 14 days before the planned trial batch date the Contractor shall notify the Engineer and the District Structure and Bridge Engineer in writing of the planned trial batch date and planned production start date. The trial batch date shall be at least 28 days prior to production.

At least 28 days prior to production, the Contractor shall prepare a minimum 1 cubic foot trial batch of  the mix to demonstrate compliance with mixing requirements. The pre-production mix shall be used to prepare test specimens.  All mix specimens regardless of aggregate size shall be tested in accordance with ASTM C39 for compressive strength and ASTM C496 for splitting tensile strength, and shall attain the properties listed in Table 3, before production placement begins.

The Contractor shall prepare the trial batch with the same equipment to be used during production on the project. The Contractor shall perform the trial batch testing in accordance with the test methods in Table 3. Test results shall be furnished to the Engineer for review. The Contractor will not be authorized to proceed with production until the test results verify conformance with the requirements stated herein.

| Table 3 Properties of VHPC |  |  |
| --- | --- | --- |
| Property | Test | Value |
| 7-day compressive strength | ASTM C39 | ≥ 9,000 psi |
| 28-day compressive strength | ASTM C39 | ≥ 11,500 psi |
| 7-day splitting tensile strength | ASTM C496 | ≥1,200 psi |
| 28-day splitting tensile strength | ASTM C496 | ≥ 1,500 psi |
| Slump flow | ASTM C1611 | 18 in to 22 in |

- SAMPLING AND TESTING DURING PRODUCTION

The Contractor shall use the same equipment during production that was used to prepare the trial batch. The Contractor shall produce a sample from the first batch. Where the number of batches exceeds 3, a second batch shall be sampled. Where the number of batches exceeds 10, a third batch shall be sampled. The Engineer may require additional sampling to determine the variation in the product and where the consistency of the mix appears to have changed or the Contractor may choose to discard the batch. The Contractor shall produce all samples in accordance with Section 217 of the Specifications large enough to perform all acceptance tests. All samples of VHPC will be tested for slump flow, 7-day splitting tensile strength, and 7-day compressive strength in accordance with Table 3 regardless of aggregate size. Test results shall conform to Table 3. The Contractor shall prepare test specimens in accordance with Section 217.11(e) of the Specifications. Material represented by samples not conforming to Table 3 will be accepted in accordance with Table II-17A of the Specifications.