Guidelines: For projects where the plans specify ECC for use in shear keys, or where ECC is specified for use in culvert repairs.

SP217-000110-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

ENGINEERED CEMENTITIOUS COMPOSITE (ECC)

March 16, 2021

- DESCRIPTION

This work shall consist of furnishing and placing fiber-reinforced Engineered Cementitious Composite (ECC), as shown on the Plans, and directed by the Engineer.

- MATERIALS

The Contractor shall produce ECC using a mix design that conforms to Table 1 or provides deflection hardening such that the ultimate strength is at least 5% higher than the first crack strength when tested in accordance with ASTM C1609 at 7 days.

| Table 1 Mixture Design for ECC-Culvert and ECC-Shear Keys |  |
| --- | --- |
| Mix Component1 | lbs/yd3 (except where noted) |
| Cement | 960 |
| Class F Fly Ash | 1150 |
| Mortar or Concrete Sand | 6702 |
| Maximum water/cementitious ratio | 0.27 |
| Synthetic Fiber, (1.8% by volume) | 40 |
| High Range Water Reducing Admixture (HRWRA) | As needed 3 |
| 1Mix components are subject to the tolerances in Section 217.04 of the Specifications. 2A relative density of 2.57 for sand and 2.25 for Class F fly ash is used in these calculations. Mortar sand amount may need to be adjusted to yield a 1 yd3 material based on actual relative densities of ingredients. Air content is assumed to be 2% (no air entrainment is required). 3For self-consolidating concrete (SCC) a dosage rate of HRWRA at 6 to 10 oz/cwt may be sufficient. Workability retaining admixtures or hydration stabilizing admixtures may be used to maintain the workability of the mixture. If a shrinkage reducing admixture at 1.5 gal/yd3 is added, dosage may be as low as 2 oz/cwt. For ECC culvert, a lower dosage of admixture is needed or the water content can be reduced. Air entraining admixture is not required in ECC. |  |

  - The components of ECC shall conform to Section 217 of the Specifications.

  - Fibers shall be polyvinyl alcohol conforming to ASTM C1116. They shall be 8 Denier or less in diameter and 8 mm long.

Alternatively, batches may be produced by using pre-packaged (bag) ECC materials identified in the ECC section of Approved List 54 for the specified application in the Plans. Use of prepackaged ECC materials does not alleviate the requirements for acceptance testing of the trial and production batches.  Trial batching shall be required if this is the first application for the Contractor or the concrete plant.

- MIXING PROCEDURES

Batch size should not exceed one-third of the mixer capacity for both small and large batches.  The Contractor may submit alternate mixing procedures that evenly distribute the fibers throughout the mix to the Engineer for approval. Self-consolidating concretes, such as ECC, require longer mixing times to achieve the consistency for placement compared to normal concrete mixes.

  - Small batches (1 cubic foot to 1 cubic yard) shall be mixed using a mortar mixer with rotating paddles and the following procedure, unless otherwise approved by the Engineer: The Engineer may approve an alternate procedure if the Contractor shows that the mixer can produce a uniform product at the specified workability.

- Mix the solid materials (cement, Class F fly ash, and mortar sand) in the mixer.

- Add water along with the HRWRA to ensure appropriate consistency (9 to 13 inch spread when tested with the conical mold of ASTM C230 before addition of fibers).

- Add fibers and mix until they are evenly distributed throughout the mixture.

- The final mixture shall display SCC characteristics (i.e., flow without the need for mechanical consolidation).

If pre-packaged (bag) materials are used, they shall be mixed in accordance with the manufacturer’s recommendations.

  - Large batches (1 cubic yard or larger) shall be mixed using stationary mixers at the concrete plant or ready mix concrete trucks, and the following procedure, unless otherwise approved by the Engineer:  It is difficult to disperse the fibers in truck mixers.  The Engineer may approve an alternate procedure if the Contractor shows that the mixer can produce a uniform product at the specified workability.

- Add all sand.

- Add 90 to 95% of the water and all of the admixtures.

- Add all Class F fly ash, add Portland cement.

- Add remaining water to wash the drum fins, mix at high speed for at least 5 minutes or until the material is homogeneous, whichever is longer.

- Add fibers and mix at high speed for at least 5 minutes or until the material is homogeneous, whichever is longer.

- The final mixture shall display SCC characteristics (i.e., flow without the need for mechanical consolidation).

If pre-packaged (bag/sack) materials are used, they shall be mixed in accordance with the manufacturer’s recommendations.

- TRIAL BATCHING

At least 14 days before the planned trial batch date, the Contractor shall notify the Engineer and the District Structure and Bridge Engineer of the planned trial batch date and planned production start date. The trial batch date shall be at least 28 days prior to production.

At least 28 days prior to production, the Contractor shall prepare a minimum 1 cubic foot trial batch of the mix to demonstrate compliance with mixing requirements. The pre-production mix shall be used to prepare test specimens in accordance with Section 217.11(e) of the Specifications. The specimens shall be tested in accordance with ASTM C109 or ASTM C39, and shall attain a 28-day compressive strength of 4,000 pounds per square inch for shear keys and 3,000 pounds per square inch for culvert repair; the results of the 28-day test shall be provided to the Engineer before production placement begins. To open a bridge structure to traffic, the 4,000 pounds per square inch shall be achieved. For culvert repairs, stiffening of the ECC mixture is sufficient for opening to traffic.

The Contractor shall prepare the trial batch with the same equipment to be used during production on the project. The Contractor shall perform the trial batch testing in accordance with the test methods listed herein. Test results shall be furnished to the Engineer for review. The Contractor will not be authorized to proceed with production until the test results verify conformance with the requirements stated herein.

- SAMPLING AND TESTING DURING PRODUCTION

The Contractor shall use the same equipment during production that was used to prepare the trial batch. The Contractor shall produce a sample from the first batch. Where the number of batches exceeds 3, a second batch shall be sampled.  Where the number of batches exceeds 10, a third batch shall be sampled.  All samples shall be in accordance with Section 217 of the Specifications and large enough to perform all acceptance tests. Mixes shall conform to Table 2.

| Table 2 ECC Properties Based on Type |  |  |  |
| --- | --- | --- | --- |
| Property | Test Method | ECC Type |  |
|  |  | ECC- Shear Keys | ECC- Culverts |
| Compressive Strength, psi, @28 days | ASTM C109 or ASTM C39 | 4,000 | 3,000 |
| Slump Flow, inches, min | ASTM C1611 | 18 | -- |
| Slump, inches | ASTM C143 | -- | 2-6 |

Slump flow of ECC- Shear Keys shall be without segregation. For ECC-culverts, slump shall not flow down the vertical or inclined surfaces.

The Contractor shall prepare test specimens for compressive strength in accordance with Section 217.11(e) of the Specifications. The specimens shall be tested in accordance with ASTM C109 or ASTM C39, and shall attain a compressive strength meeting the requirements of Table 2.