Guidelines: For use on all projects with cast-in-place mass concrete. Does not cover precast mass concrete.

SP217-000120-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

MASSIVE CONSTRUCTION HYDRAULIC CEMENT CONCRETE (“MASS CONCRETE”) OPERATIONS

March 19, 2020

- DESCRIPTION

This work shall consist of furnishing and placing hydraulic cement concrete for massive cast-in-situ concrete bridge components, which shall be any concrete element designated on the plans as mass concrete. If the plans do not address mass concrete, then any concrete element for which the smallest dimension according to the Plans exceeds 5 feet shall be designated mass concrete. This shall include footings, drilled shaft caps, piers, abutments, and other work that meet this criterion. Work shall be performed in accordance with this Special Provision, the Plans, and as directed by the Engineer.

Unless otherwise specified, the 28-day compressive strength (f’c) used in the design calculations and specified in Table II-17 of the Specifications shall be attained in 56 days instead of 28 days.

- DEFINITIONS

Match-Cured. A process where concrete test specimens are cured at the same temperature as the product by monitoring the concrete temperature in both the product and the test specimens and applying heat to the test specimens to match the temperature of the concrete.

- MATERIALS

  - Mass Concrete shall contain at least 30% Class F fly ash or at least 65% blast-furnace slag, measured by mass of cementitious materials, but not both.

  - High-early-strength (Type III) cement, calcium chloride, and accelerating type admixtures shall not be used.

  - A retarding admixture may be allowed, if approved by the Engineer, for the following conditions: to prevent cold joints due to the quantity of concrete placed, to permit re-vibration of the concrete, to offset the effects of high concrete temperature, or to reduce the maximum temperature and rate of temperature rise. The admixture shall be pretested with job materials under job conditions, to include approximate dimensions.

  - The Class of Concrete used in mass concrete placements shall conform to Table II-17 of the Specifications and shall not be higher quality than Class A4 General unless specified otherwise on the Plans.

- PROCEDURES

  - ACI Specifications. This work shall be performed in accordance with the following ACI publications, except as modified by this Special Provision:

    - “Guide to Mass Concrete”, ACI 207.1R.

    - “Report on Thermal and Volume Change Effects on Cracking of Mass Concrete”, ACI 207.2R.

    - “Control of Cracking in Concrete Structures”, ACI 224R.

    - “Specifications for Structural Concrete”, ACI 301, Section 8.

  - Submittals

The Contractor shall submit the following to the Engineer for review and approval according to the procedures in Section 105.10(c) of the Specifications.

    - Working Drawings. Describe the intended concrete placing sequence in the mass concrete components. Indicate proposed locations of all temperature sensors.

    - Shop Drawings. Show reinforcing steel to be placed in the elements if different size, spacing, or depth of reinforcing bars to be used than those given in the Plans.

    - Placement Plans. For each proposed concrete mix design, the following information shall be submitted:

      - Methods. Describe the methods to be used to construct the mass concrete  components within the criteria set forth herein. Include graphics that illustrate the dimensions of proposed mass concrete placements. Mass concrete placements shall be laid out to minimize surface area for a given volume. Individual placements that combine elements considered mass concrete and non-mass concrete shall not be permitted.

      - Design calculations prepared to document that the methods chosen to install the mass concrete components are in accordance with the ACI publications referenced above as modified by this Special Provision. Calculations shall include:

- A table of calculated peak temperatures for the range of expected air, concrete, and soil or ground (if applicable) temperatures at time of placement.

- A calculation of maximum temperature differences within the element during the curing period.

- A calculation of time to peak temperature.

- A curve of maximum allowable temperature difference vs. concrete strength for each element under consideration, calculated for the allowable crack widths shown on the Plans. The Contractor shall use allowable crack widths shown in Table 4.1 of ACI 224R when not shown on the Plans. At the Engineer’s discretion, this analysis can be waived for elements where all of the following conditions are met:

  - the smallest dimension is less than 10 ft.

  - at least 40% Class F Fly Ash or at least 75% granulated iron blast-furnace slag cement is used in the concrete mix

  - the total maximum cementitious content is 600 lbs/yd3 except with Self-Consolidating Concrete.

- Insulation requirements for the forms and exposed portions of the concrete to keep the thermal differences within allowable limits.

- A calculation of the time to reach the peak temperature difference, as well as the estimated time to cool to the allowable differential temperature specified in Section IV-4C.

      - Mix design showing proportions and sources for all components, and results of strength tests of sample cylinders. Mix designs shall also include the heat of hydration of the cementitious materials in the mix, as well as the thermal expansion coefficient of the concrete in accordance with AASHTO T 336 if the allowable temperature difference curve will be used.

      - Admixtures. Catalogue information on any admixtures proposed to be added to the concrete mix.

      - Temperature control. Proposed methods to reduce concrete temperatures and temperature differentials, such as pre-cooling of concrete or insulation. Internal cooling pipes shall not be permitted.

    - All submittals must be signed and sealed by a Professional Engineer licensed to practice engineering in the Commonwealth of Virginia.

  - Placing

The maximum temperature of the concrete for mass components when deposited shall be 95°F. The minimum temperature limit of the concrete for mass components when deposited shall be 50°F.

  - Curing and Protection

    - The minimum curing period shall be 7 Days. Curing methods shall be in accordance with Section 404 of the Specifications, and shall not result in temperature differentials exceeding the limits in Sections IV-2C(2) and IV-4C. With the Engineer’s approval, the forms may be stripped prior to the end of the curing period, provided the curing continues for the remaining time.

    - The maximum allowable temperature in any portion of the mass concrete shall be 160F for slag cement mixes and fly ash mixes, in the prescribed proportions. The Engineer may direct that concrete which has exceeded these temperatures be removed, or otherwise mitigated, at no cost to the Department.

    - The maximum allowable thermal gradient between the core and skin temperatures of a placement is limited to 35F.

    - Temperature sensors shall be installed in each mass concrete pour and placement. A pair of two temperature sensors (a primary and backup), shall be at the centroid of the placement, or wherever the point of expected maximum temperature is anticipated.  If there is any doubt as to the location of the predicted maximum temperature, then additional temperature sensors shall be placed as required or as directed by the Engineer.

    - For elements cast on the ground or in a horizontal position such as footings, slabs, or pier caps: in addition to the pair of temperature sensors located at the point of maximum temperature, one pair each of temperature sensors shall be cast 3 inches from the surface and each pair of temperature sensors shall be vertically in line with the temperature sensors placed at the centroid as required by Section IV-4D. The temperature sensors pairs located at the elevations of the top and bottom mats shall have the same concrete cover as the reinforcing mats in those locations.

    - For elements cast in a vertical position such as columns and walls: in addition to the temperature sensors located at the point of maximum temperature, one pair each of temperature sensors on the north face and on the south face shall be cast in line with the temperature sensors cast at the centroid. These temperature sensors shall be located in the same vertical plane as the reinforcing steel mats and shall have the same concrete cover as the reinforcing mats.

    - The Engineer may direct that additional temperature sensors be placed if the area of maximum thermal gradient cannot be readily determined.

    - Both temperature sensors from each pair shall be connected to a data logger or other recording device. The data logger shall record the temperatures at each temperature sensor at least once every hour from the time the temperature sensor is covered with concrete until 3 days after the peak temperature is reached, or as directed by the Engineer. The data logger shall have a printed tape or electronic data storage capability. The Engineer may discontinue monitoring of mass concrete elements deemed to be similar to previously monitored elements and placed under similar temperature conditions.

    - To determine concrete strength for stripping and allowable thermal differences, the Contractor shall use Match-Cured cylinders. A separate analysis shall be provided for each approved mass concrete design mix.

    - Match-Cured cylinders shall follow the coolest surface temperature sensor in the placement. Sufficient number of cylinders shall be cast to allow an accurate plot of the strength development of the concrete. At a minimum, 9 pairs of cylinders shall be cast, with two cylinders each broken at the end of 1, 2, 3, 4, 5, 6, 7, 10, and 14 days.  Additional cylinders shall be cast if it is anticipated that the concrete will not reach peak temperature until after 10 days from the placement.

    - The forms may be stripped when the concrete strength is high enough (as determined by the Match-Cured cylinders) to withstand the anticipated thermal difference between the core temperature and the 48-hour average air temperature, or as directed by the Engineer. In no event will form stripping be allowed before the surface concrete reaches at least 80 percent of its design strength. After form striping, concrete shall be protected from freezing temperatures for 48 hours by the use of insulating blankets or other methods approved by the Engineer.

  - Remedial Measures

If temperature differentials are exceeded and cracking occurs or if other damage is evident, the Contractor shall core or otherwise test the concrete elements as directed by the Engineer to determine the extent of damage.

The Contractor shall submit a proposed remediation plan for the approval of the Engineer. The Engineer may direct that all or a portion of the damaged or unacceptable concrete be removed and replaced without additional compensation.

For concrete left in place, all cracks widths over 0.2 mm shall be epoxy injected. Epoxy bonding compounds shall be in accordance with Section 243 of the Specifications. All ports and mastic compound shall be removed from portions of the structure that will remain visible when construction is complete.

All remedial work required, including coring and crack sealing, shall be incidental to the unit bid price for Concrete (Class).

- MEASUREMENT AND PAYMENT

Measurement and payment will be in accordance with Section 404 of the Specifications. All work required to install mass concrete bridge components as specified herein shall be considered incidental to the work required in Section 404 of the Specifications and will not be measured for separate payment.