GUIDELINES: Use this spec where the Contractor has recommended Number 10 Screenings for use on certain items as a Value Engineering Proposal, or where Number 10 Screenings are specified as an alternate bid item. If the Plans specifically require Number 10 Screenings, contact the State Specifications Engineer for clarification before use.

SP303-DB0210-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

USE OF NUMBER 10 SCREENINGS

November 14, 2018

- DESCRIPTION

This Special Provision cover the use of No. 10 Screenings in various applications on the Project. No. 10 Screenings shall be used in locations designated in the Contract.

- MATERIALS

  - No. 10 Screenings (also known as quarry dust, rock dust, quarry screenings, rock screenings and quarry byproduct) may be used as an acceptable source of borrow material for the applications described herein. No. 10 Screenings shall conform to the requirements herein and elsewhere in the Contract. For the purpose of this Special Provision, No. 10 Screenings shall be defined as any material that is a byproduct of rock crushing processes, and either has a gradation of 100% passing the 3/8” Sieve and less than 20% passing the No. 200 Sieve, or meets the No. 10 coarse aggregate gradation. No. 10 Screenings shall also have a minimum CBR value of 15 and be either non-plastic or have liquid limit less than 25 and a plasticity index less than 9.

  - Low-plasticity clay or silt shall conform to classification CL or ML according to ASTM D2487.

- PROCEDURES

  - Embankment

No. 10 Screenings shall be compacted to 95% of Standard Proctor dry density, and shall be compacted in the field within a water content range of 2 percentage points either side of the optimum water content. For laboratory optimum water contents greater than 9%, a field optimum water content target of 8.5% shall be used. Both dry density and optimum water content shall be obtained according to VTM-1.

When landscaping is required in areas of No. 10 Screenings use, the Design-Builder shall make accommodations for landscaping as trees and larger shrubs will not be able to root properly in No. 10 Screenings.

The top and sides of unconfined areas consisting solely of No. 10 Screenings shall be capped with low-plasticity clay or silt material to deter water from penetrating into and saturating embankments constructed of No. 10 Screenings. Fills less than 10 feet in height shall be capped on the sides and top with a minimum 2 feet of low-plasticity clay or silt. At a minimum, fills greater than 10 feet in height shall be capped with 3 feet of low-plasticity clay or silt.

In low-lying areas, drainage areas or areas identified as active or potential wet zones during construction, a separation layer between the bottom of the placed fill and original ground shall be placed to mitigate the potential destabilization of a No. 10 Screenings embankment. The separation layer should be at least 8-inches thick and composed of No. 1 or No. 57 aggregate or another open graded aggregate wrapped in drainage fabric. Riprap bedding fabric meeting the requirements of Section 245 of the Specifications shall be placed between the separation layer and the No. 10 Screenings.

If an embankment greater than 10 feet in height is constructed, survey points shall be taken after the fill is complete at bi-weekly intervals until 2 consecutive measurements are each less than ¼ inch to ensure that settlement is not occurring. If settlement issues are identified, the Design-Builder shall mitigate the causes of settlement as needed (e.g., additional asphalt, ground improvement techniques, removing and replacing settled locations if isolated, etc.).

  - Structure backfill, building foundation soil, road subgrade, undercut replacement, fill under approach slabs

No. 10 Screenings used for these purposes shall have a CBR of at least 30, shall be compacted to 95% of Standard Proctor dry density (100% under approach fills), and shall be compacted in the field within a water content range of 2 percentage points either side of the optimum water content. For laboratory optimum water contents greater than 9%, a field optimum water content target of 8.5% should be used. Both dry density and optimum water content shall be obtained using VTM-1.

These applications should typically be in confined areas. Where there is no confinement, capping of the unconfined sides shall be as in Paragraph 1 above.

In low-lying areas, drainage areas or areas identified as active or potential wet zones during construction, the No. 10 Screenings shall be wrapped in drainage fabric.

  - Pipe Backfill

Pipe backfill shall be performed in accordance with Standard Drawing PB-1 and Section 302.03(a)2g of the Specifications unless noted herein. No. 10 Screening may be used as either Regular Backfill or Class I Backfill, as shown in Standard Drawing PB-1. Regular Backfill material within the limits of roadway embankments and under existing or proposed roadway shall meet a minimum CBR value of 15.0 as determined by VTM-8. Ground line shall be considered the top of trench at the time of pipe installation. When pipe does not project above ground line, Regular Backfill shall extend to the top of the pipe trench in fills or subgrade in cuts. Outlet pipes for storm water management basins shall be installed as noted on the plans.

- Reinforced Fill for Mechanically Stabilized Earth Walls

No. 10 Screenings used for these purposes shall have a friction angle of at least 34 degrees, with up to 60% passing the No. 40 sieve. They shall be compacted to 95% of Standard Proctor dry density, and shall be compacted in the field within a water content range of 2 percentage points either side of the optimum water content. For laboratory optimum water contents greater than 9%, a field optimum water content target of 8.5% should be used. Both dry density and optimum water content shall be obtained using VTM-1. If the use of No. 10 Screenings conflicts with any other Contract requirement for reinforced fill for MSE walls, No. 10 Screenings shall not be used for this purpose.

  - Soft ground stabilization

No. 10 Screenings may be used as a replacement or stabilizing agent for soft or unsuitable soils in parking areas, under building pads or foundations, or under roadways. In the event soft or unsuitable soils are identified, No. 10 Screenings may replace or be mixed into the soil in a prescribed percentage to improve the bearing capacity of the soil. Replacement shall require confinement by surrounding ground. For mxing, the percentage of screenings to be used shall be determined by sampling the soft/unsuitable soil and mixing with varying percentages of No. 10 Screenings in the laboratory. Proctor samples and CBR samples of each mixture shall be prepared in accordanceVTM-1 and VTM-8, respectively. The mixture resulting in the desired minimum CBR will determine the minimum amount of No. 10 Screenings to be used. Field mixing of the No. 10 Screenings shall be accomplished by layering the appropriate amount of screenings on top of the soft/unsuitable soil followed by blending to a depth of 8 inches to achieve the blend percentage determined in the laboratory. Mixing shall be accomplished by means of a self-propelled or self-powered machine equipped with a mechanical rotor or other approved type of mixer that will thoroughly blend the No 10 Screenings with the soil.