SP307-000100-01

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

CEMENT TREATED AGGREGATE (CTA) BASE

June 18, 2020

- Description

This work shall consist of constructing a base course of the pavement structure using a plant mixture of approved aggregates, hydraulic cement, and water on a prepared surface in accordance with the requirements of this Special Provision and in conformity with the lines, grades, typical sections, and cross sections shown on the Plans or as directed by the Engineer.

- Materials

  - Cement shall conform to the requirements of Section 214, Type I, IL, IP, or II. Cement shall be transported, stored, and otherwise protected in accordance with the requirements of Section 217.03 of the Specifications.

  - Water shall conform to the requirements of Section 216 of the Specifications.

  - Asphalt used for curing or priming shall conform to the requirements of Emulsified Asphalt in Section 210 of the Specifications.

  - Aggregate shall conform to Section 208 of the Specification or other Contract requirements. Aggregate Base, Type 1, Size No. 21A shall be used conforming to the following requirements:

    - Optimum Water Content: Material shall be delivered at a water content of not less than optimum or more than optimum plus 2 percentage points determined by AASHTO T 134, Method B.

    - Compressive Strength: Tests for compressive strength shall be performed in accordance with the requirements of ASTM D1633, Method A for conformance to the specified value (a 7-day compressive strength of 650 psi).

    - Durability: Neither the wet-dry weight loss nor the freeze-thaw weight loss shall exceed 14% in accordance with AASHTO T 135 Method B and AASHTO T 136 Method B, respectively.

- Job-Mix Formula

If unsatisfactory results or other conditions make it necessary, the Contractor shall submit a new job-mix formula for approval. CTA shall not be delivered to the Project until the submitted job mix formula has been approved by the Engineer.

  - Mix Design: The job mix formula shall use a cement content that, when tested in the laboratory per ASTM D1633 Method A, produces a 7-day compressive strength of 650 psi.

  - Submittals: The Contractor shall submit for the Engineer’s approval a proposed job-mix formula through the “Producer Lab Analysis and Information Details” (PLAID) website https://plaid.vdot.virginia.gov and certified test reports at least 30 calendar days before the CTA production. Tests older than 12 months shall not be used except for durability (wet-dry and freeze-thaw weight loss) tests. Test results for the durability tests will be valid for 3 years. The certification shall show the ASTM or AASHTO specifications or tests for the material, the name of the company performing the tests, the date of the tests, the test results, and a statement that the material did or did not comply with the applicable specification. The submittal package shall include the following:

- Job Mix Identification Number

- Sources of materials (Aggregate, Cement)

- Aggregate gradation

- Target cement content with associated plot

- Compressive strength at seven days determined in accordance with ASTM D1633, Method A (Minimum three specimens per cement content)

- Laboratory compaction characteristics with associated plot (maximum dry density and optimum water content) determined in accordance with AASHTO T 134, Method B

- Wet-Dry weight loss determined in accordance with AASHTO T 135, Method B

- Freeze-Thaw weight loss determined in accordance with AASHTO T 136, Method B

Target cement content shall be determined using the following procedures:

    - Conduct a Proctor test (AASHTO T 134, Method B) on a sample containing 4.5% cement.

    - Prepare sets of three specimens each at 2%, 4.5%, and 7% cement and test for compressive strength in accordance with ASTM D1633, Method A. Compact all specimens to maximum dry density (± 3pcf) and optimum water content (± 1 percentage point).

    - Plot a compressive strength versus cement content graph using the average strength values at each cement content by connecting the points with a straight line.

    - Select a target cement content from the graph at 650 psi. An example is shown in Figure 1. A different gradation or source shall be used if the strength of 650 psi is not reached within the 2-7% cement content range.

Figure 1: Example compressive strength versus cement content graph

- Construction Method

  - Weather Limitations

CTA shall not be placed when aggregate or the surface on which the course will be placed is frozen. The Contractor shall not start placing CTA until the air temperature is at least 40°F in the shade and rising.

CTA shall not be placed in the rain. If unexpected rain occurs during placement, placement shall be halted, and the layer shall be quickly compacted, tested, and protected. CTA that becomes wet by rain during transport or placement shall be evaluated by the Engineer, and may be rejected.

  - Procedures

    - Preparing Existing Surface: The Contractor shall prepare the surface of the roadbed in accordance with Section 305.03 of the Specifications.

    - Preparing Materials: Aggregate shall be proportioned and mixed with cement and water in an approved central mixing plant. The plant shall be equipped with feeding and metering devices that will introduce materials into the mixer in the specified quantities. Mixing shall continue until a uniform mixture has been obtained.

CTA shall be transported from the plant to the job site in trucks or other hauling equipment having beds that are smooth, clean, and water-tight. Truck bed covers shall be provided and used to protect the CTA from rain or drying out. CTA shall be spread on a moistened surface (no standing water) in a uniform layer by a self-propelled spreader or other approved method. Not more than 60 minutes shall elapse between the start of mixing at the plant and the start of compacting the CTA on the prepared subgrade. Retarder may be allowed at the discretion of the Engineer.

The Contractor shall determine cement content by the titration method as described in VTM-40. Sampling and testing for determining cement content shall be performed at the plant. However, nothing herein shall be construed as waiving the requirements of Sections 106.06 and 200.02 of the Specifications. The Department may sample and prepare specimens at a plant or project at any time to verify compliance with strength requirement.

The Engineer’s acceptance for cement content will be based on the mean of the results of tests performed on samples taken in a stratified random manner from each lot. The rate of sampling will be four samples per lot. A lot of material is defined as 2000 tons, or 4000 tons for Contract items in excess of 50,000 tons. If the Project requires less than 2000 tons or the job-mix formula for the aggregates is modified within a lot, then that amount shall be defined as a lot. If a portion of the lot is rejected on the basis of individual test results, the remainder shall be defined as a lot.

A lot will be considered acceptable for cement content if the mean result of the tests is within the following process tolerances of the job-mix formula for the number of tests taken. However, no one sample shall have a cement content more than 1.6 percentage points below the design cement content.

| Table 1 Process Tolerances for Cement Content |  |
| --- | --- |
| No. of Tests | Tolerance |
| 1 | -1.6 |
| 2 | -1.1 |
| 3 | -0.9 |
| 4 | -0.8 |

If an individual test result indicates that the cement content of the material represented by the test is deficient by more than 1.6 percentage points from the design cement content, the portion of the material represented by the sample shall be removed from the road.

If the average value of the test results for a lot falls below the allowable process tolerance, a payment adjustment will be applied to the contract unit price at the rate of 1.0 percent for each 0.1 percent the material is outside the process tolerance. If the total adjustment is 8.0 percent or less and the Contractor does not elect to remove and replace the material, the Contract unit price paid for the material will be reduced at the rate specified herein. The adjustment will be applied to the tonnage included in the entire lot.

    - Compacting and Finishing: Prior to the beginning of compaction, the CTA shall be brought to a uniformly loose condition for its full depth and compacted thoroughly. At compaction, the CTA shall have a water content of not less than optimum or more than optimum plus 2 percentage points. Compaction equipment shall be subject to the approval of the Engineer, and the number of such units shall be sufficient to ensure the specified density and completion of the processed section within 3 hours from the time the water is added to the mixture. No section shall be left undisturbed for longer than 30 minutes during the compaction operation. The compacted thickness of any one layer shall be not more than 6 inches, except that the Engineer may approve increasing the compacted depth of a single layer of the CTA course to 10 inches when vibrating or other approved types of special compacting equipment are used. In multiple layer construction, the surface of the compacted material shall be kept moist until covered with the next layer. Successive layers shall be placed and compacted so that the required total thickness of the CTA course is completed in the same shift.

The CTA base course will be tested in place for depth and density. Field density determinations shall be performed with a portable nuclear field density testing device, using a density control strip as specified in Section 304 and VTM-10 except that the density shall be a minimum 95% of the theoretical maximum dry density as determined by AASHTO T 134, Method B when direct transmission testing is performed upon the completion of the control strip to verify the compaction.

As compaction nears completion, the surface shall be shaped to the required lines, grades, and cross sections. The water content of the surface material shall be maintained at not less than the specified optimum during finishing operations. Compaction and finishing operations shall be completed within the specified time and carried out in a manner that will produce a smooth and dense surface free of ruts, cracks, ridges, and loose material. The total time ( from the time water is added to the mixture at the plant to final grade) may be increased at the discretion of the Engineer if retarder is used due to longer haul times, however, the time will not be allowed to exceed 4 hours in any case.

    - Construction Joints: At the end of each shift’s construction, a transverse construction joint shall be formed that is a vertical face, perpendicular to the centerline, and is free of loose material.

Longitudinal construction joints (parallel to the centerline) shall be formed to a consistent, well-defined vertical edge that is free of loose material. The longitudinal joints shall be located so there is a 2-foot minimum offset from planned joints in any overlying layer.

While forming construction joints, the Contractor shall ensure the material in the joint area is adequately compacted and that the joints are finished level and even with the remainder of the CTA course.

    - Tolerances: The finished CTA course shall conform to the specified thickness and density, subject to the following tolerances:

      - Density: Density for test section shall be determined in accordance with VTM-10. Five readings shall be made on each test section for density using the same method of test used on the Roller Pattern and Control Strip. None of the five readings shall be less than 95% of the Control Strip density, and any portion on which density is less than 95% of the Control Strip density shall be removed and replaced. The Contractor has the option ofre-compacting the material if the time since water was added at the plant has not exceeded 4 hours if a retarder was used or 3 hours without a retarder. The average of the five readings shall be equal to or greater than 98% of the Control Strip density. If the average density does not meet this requirement, the Contractor may elect to leave the lot in place at a reduced unit price determined in accordance with Table 2.

| Table 2 Payment Schedule for Density |  |
| --- | --- |
| Average Dry Density (%) | Payment (%) |
| 98.0 and greater | 100 |
| 97.0-97.9 | 95 |
| 96.0-96.9 | 90 |
| 95.0-96.0 | 75 |

      - Thickness: Thickness will be determined in accordance with VTM-38B except that maximum lot size shall be 1 mile for each paver application width. Sample shall be taken from the lot at the following rate:

| Table 3 Lot Size and No. of Samples required for Thickness |  |
| --- | --- |
| Lot size | No. of samples required |
| 0-0.5 Mile | 2 |
| 0.5-0.75 Mile | 3 |
| 0.75-1 Mile | 4 |

Acceptance of the course will be based on the requirements of Section 308.04 of the Specifications except when the depth is deficient by more than 1 inch. The Contractor shall correct sections on CTA base courses that are deficient in depth by more than 1 inch by   applying asphalt concrete at their own expense if approved by the Engineer, or by removing and replacing the affected areas.

    - Curing: The completed CTA course shall be cured with an emulsified asphalt seal applied as soon as possible and in no case later than 24 hours after completion of the finishing operations. The surface of the base CTA course shall be kept continuously moist using an application of water that shall not erode the CTA (e.g. a fog-type water spray or equivalent) until the emulsified asphalt is applied.

Emulsified asphalt shall be uniformly applied at the rate of approximately 0.25 gallon per square yard or as shown on the Plans. Application of the emulsified asphalt shall produce full coverage without excessive runoff. At the time the emulsified asphalt is applied, the CTA course shall be tightly knit and free from loose and extraneous material.

Should it be necessary for construction equipment or other traffic to use the emulsion-covered surface before the emulsified asphalt has cured sufficiently to prevent pickup, sufficient sand blotter cover shall be applied before such use.

The CTA course shall be protected from freezing for at least 7 days after its construction.

    - Traffic: CTA course may be opened immediately to low-speed lightweight local traffic (less than 10 tons; no tandem axle or tractor trailer trucks) and to construction equipment provided the emulsified asphalt is not impaired and the CTA is sufficiently stable to withstand marring or permanent deformation (<1/4”). Construction equipment shall be limited to that used in applying emulsified asphalt and placing subsequent layers. The section can be opened to all traffic after a period of 7 days or the CTA has received a subsequent layer, and is sufficiently stable to withstand marring or permanent deformation.

    - Surfacing: Subsequent pavement layers (asphalt concrete or Portland cement concrete) may be placed any time after finishing, as long as the CTA is sufficiently stable to support the required construction equipment without marring or permanent distortion (<1/4”) of the surface.

If a subsequent pavement layer is placed within 24 hours of the CTA placement, the CTA may be moist cured until the next pavement is placed. The emulsified asphalt seal may not need to be applied in such case.

    - Maintenance: Maintenance in accordance with Section 105.14(c) of the Specifications shall include immediate repairs of defects, which work shall be performed by the Contractor and repeated as often as necessary to keep the course continuously intact. Repairs to the CTA course shall be performed in a manner that will ensure the restoration of a uniform surface and stability of the area repaired. If it is necessary to replace any processed material, the replacement shall be for the full depth, with vertical cuts, using either fresh cement-treated material or concrete. No skin patches will be permitted.

- Measurement and Payment

Cement-Treated Aggregate Base Material will be measured in tons and will be paid for at the Contract ton price. This price shall include furnishing and installing cement-treated aggregate; emulsified asphalt, cover material, water for curing and maintenance; and restoring shoulders and ditches when grading is not a pay item.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Cement Treated Aggregate Base Material | Ton |