Guidelines: For use on paving Construction Projects designated by the District Materials Engineer.  Use in areas with very soft material.  Gradation in Section II-1 is approximate and should only be inspected visually.  Used for years in Staunton District.

SP309-DB0100-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

SELECT MATERIAL – TYPE OGB (OPEN GRADED BASE)

WITH TYPE I NO. 21B AGGREGATE MATERIAL

November 14, 2018

- DESCRIPTION

This work shall consist of furnishing and placing Select Material Type OGB including aggregate no. 21B in accordance with the Plans, Specifications, and as directed by the Design-Build Design Manager.

- MATERIALS

  - Select Material Type OGB shall consist primarily of crusher run and shall be free from seams, cracks, and other structural defects. The rock shall contain no more than 3% foreign and deleterious materials per visual examination, and have a gradation in accordance with the table below based on Visual Inspection.

| Seive | Percent Passing (%) |
| --- | --- |
| 8” | 100 |
| 4” | 40-50 |
| 2” | <1 |

  - Aggregate no. 21B shall conform to Section 208 of the Specifications.

- PROCEDURES

The Select Material Type OGB shall be placed, shaped, and tracked-in at locations shown in the Plans or as directed by the Design-Build Design Manager. Tracking-in shall consist of 2-4 passes over the material with a bulldozer or other tracked equipment. After placement of the Select Material Type OGB, aggregate no. 21B shall be placed and compacted in accordance with Section 309 of the Specifications to block the voids in the upper 2 inches of the Select Material Type OGB.