GUIDELINES – Asphalt surface treatment projects. {2007-S314DM1}

SP314-000120-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

MACRO-TEXTURE SURFACE TREATMENT

November 6, 2009; Reissued 7-12-16

I.	DESCRIPTION

This work shall consist of the production and placement of a polymer modified macro-texture surface treatment according to the Contract, as specified herein, and as directed by the Engineer.

II.	MATERIALS

A.	Asphalt: The asphalt emulsion shall be polymer modified conforming to Section 210 of the Specifications except as noted herein:

| Tests | Method | Minimum | Maximum |
| --- | --- | --- | --- |
| Sieve Test, 20 mesh, percent | AASHTO T 59 |  | 0.5 |
| Storage Stability Test, 24 hour, percent | AASHTO T 59 |  | 1.0 |
| Viscosity, Sayboult Furol @ 1220F, sec. | AASHTO T 59 | 50 | 600 |
| Particle Charge | AASHTO T 59 | Positive |  |
| Classification Test | AASHTO T 59 | Pass |  |
| Distillation: |  |  |  |
| Oil distillate by volume of emulsion, percent | AASHTO T 55 |  | 2 |
| Residue from distillation, percent | Note 1 | 65 |  |
| Tests on Residue from Distillation: |  |  |  |
| Penetration, 770F, 100g., 5 sec. | AASHTO T 59 | 60 | 140 |
| Ductility, 39.20F, 5cm/min., cm | AASHTO T 51 | 30 |  |
| Softening Point, Ring & Ball, degrees F | AASHTO T 53 | 38 |  |
| Elastic Recovery, 500F | Note 2 | 60 |  |
| Note 1: AASHTO T 59 modified to maintain a 3500F maximum temperature for 15 minutes. |  |  |  |
| Note 2: AASHTO T 301 Elastic Recovery Test: Condition the ductilometer and samples to be treated at 500F. Prepare the brass plate, mold and briquette specimen according to AASHTO T 51. The molds shall be the non-tapered type used for Force Ductility Testing. Keep the specimen at the specified test temperature for 85-90 minutes. Immediately after conditioning, place the specimen in the ductilometer and proceed to elongate the sample to 20 cm at a rate of pull of 5cm/min. After the 20 cm elongation has been reached, stop the ductilometer and hold the sample in it’s elongated position for five minutes. After five minutes, clip the sample approximately in half by means of scissors or other suitable cutting device. Let the sample remain in the ductilometer in an undisturbed condition for one hour. At the end of this time period, retract the half sample specimen until the two broken ends touch. At this point note the elongation (E) in cm. Calculate the percent recovery by the following formula: % Recovery =; 20 - E; x 100. 20. |

Modifiers shall not be post-added to the finished emulsion.  All modifiers shall be incorporated into the base asphalt prior to the emulsification process at the manufacturing facility.  The emulsion, upon standing undisturbed for a period of 24 hours shall show no milky white colored substance on its surface.  It shall have a homogeneous brown color throughout.  The emulsion used for the sweep test shall be the same as that used on the jobsite.

B.	Aggregate:  Aggregate shall conform to Section 203 of the Specifications except as noted herein.

| 1. | All aggregate shall be crushed. |  |  |  |
| --- | --- | --- | --- | --- |
| 2. | Moisture shall be maintained so that the surface is visibly moist by using methods as needed. The aggregate shall not be excessively moistened. If water is free draining from aggregate haul trucks, moisture will be considered excessive. |  |  |  |
| 3. | Fractured Faces – (ASTM D 5821) |  |  |  |
|  |  | One Fractured Face |  | 98% minimum |
|  |  | Two or more Fractured Faces |  | 95% minimum |
| 4. | Flakiness Index – (FLH T 508) 17% maximum |  |  |  |
|  | Federal Land Highways (FLH) Test Method T 508 |  |  |  |
| 5. | Grading – (AASHTO T 27) |  |  |  |
|  | Sieve Size |  | Percent Passing |  |
|  | 1/2 inch |  | 100 |  |
|  | 3/8 inch |  | 90-100 |  |
|  | No. 4 |  | 12 max. |  |
|  | No. 200 |  | 1.0 max. |  |

C.	Macro-Texture Surfacing Design.  At least 3 weeks before beginning this work, the Contractor shall submit a macro-surfacing wearing course design to the Engineer for review.  The Contractor shall indicate on the design all material sources, emulsion and aggregate application rates, and certify that the emulsion and aggregate, when tested according to the Macro-Surfacing Sweep Test available from the Central Office Materials Division, Pavement Design and Evaluation Section, results in a maximum aggregate mass loss equal to or less than 15 percent.

III.	PROCEDURES

A.	Weather Limitations shall conform to Section 314.03 of the Specifications.

B.	Surface Preparation:  Immediately prior to application of the macro-surfacing wearing course, clean the surface of vegetation, loose materials, dirt, mud, and other objectionable items.  When sealing open cracks any over-banding of crack sealant shall not be left on either side of the crack.  Thermoplastic and tape pavement markings shall be removed prior to placement.  Protect existing raised/recessed pavement markers by methods acceptable to the Engineer.

C.	Macro-Texture Application:  Emulsion and aggregate shall be uniformly applied in a continuous variable width.  Emulsion shall be applied with a self-propelled, front feed, continuous-loading vehicle.  Emulsion shall be applied so that no more than 48 inches of emulsion is exposed without aggregate cover.  The Contractor shall apply both the emulsion and aggregates in a single pass within + 10 percent of the design application rates.  Damp or moist aggregates may be used if no free water is evident in the support vehicles.

The emulsion shall be maintained at a minimum temperature of 140 degrees F in the transport vehicles. No emulsion shall be stored in the application or support units overnight.  Material not used within 48 hours of initial delivery to the job site shall be returned to the production facility at no additional cost to the Department.

Transfer of emulsion and aggregates shall be done without spillage.  Immediately stop application of the macro-texture if spillage occurs and remove the loose aggregate and/or emulsion.

The Contractor shall daily provide the Engineer with the gallons of emulsion applied and tons of aggregate and the area covered at the end of each day’s work.

For inaccessible areas, portable pressurized units shall be used to spray the emulsion uniformly over the surface.  Gage quantity of material placed at one time, according to facilities for handling, spreading, and rolling coarse aggregate, as well as the temperature of the surface and the bituminous material.  Insure uniformity at the junction of the two applications both transversely and longitudinally.

Within 2 minutes of application, roll the entire surface of the macro-texture wearing course with a minimum of one pass of a roller.  Use a sufficient number of rollers to keep pace with the continuous application operation.  Complete additional passes of the roller, as needed, within 10 minutes of application.

Complete all rolling before sweeping.  Use a sufficient number of sweepers to keep pace with the continuous application operation.  When the surface temperature is less than 125 degrees F and the relative humidity no more than 75 percent, sweep the entire surface of the macro-texture to remove excess aggregate, without damage, within 1 hour after application.  When the surface temperature is greater than 125 degrees F and the relative humidity is greater than 75 percent, sweep the macro-texture to remove excess aggregate when recommended by the bituminous material producer.  Sweep the entire surface of the macro-texture a minimum of three times.

IV.	PROTECTION OF SURFACE

Traffic will not be allowed on the newly completed surface until adequate stability and adhesion has been attained and the material is sufficiently cured to prevent distortion, flushing of bituminous material to the surface, or loss of aggregate.  Do not allow vehicular traffic on the newly completed surface until excess aggregate is removed.

V.	EQUIPMENT

A.	Asphalt Distributor:  Shall be calibrated by the Contractor in the presence of the Engineer prior to placement to ensure an even and accurate spray.  Calibration will be considered acceptable when the spray rate is within 0.02 gallon per square yard of the design application rate.

The asphalt distributor shall have an insulated tank with access for cleaning, a functional volume measuring device or calibrated tank, and a thermometer for measuring emulsion temperature in the tank.  It shall have dual, full circulation spray bars that are adjustable laterally and vertically and spray nozzles, including end nozzles that have individual control valves for adjustment.  The asphalt distributor shall be capable of synchronizing the emulsion spray bar width to the aggregate spreader width to prevent exposed emulsion.

B.	Aggregate Distributor:  Shall be calibrated by the Contractor in the presence of the Engineer prior to placement to ensure an even and accurate distribution of material.  Calibration will be considered acceptable when the application rate is within 1.0 pound per square yard of the design application rate.

The aggregate distributor shall have an integrated, aggregate hopper and variable width spreader, including power-driven augers and spread rolls to uniformly deliver the aggregate to the spreader gate openings.  It shall also have a continuous conveyor to feed the hopper, and full-width screen to reject oversize aggregate and foreign objects from entering the hopper.

C.	Rollers:  The Contractor shall use either a steel wheel or pneumatic-tire roller or combination of rollers to seat the aggregate.  The pneumatic-tire roller shall have a minimum contact pressure of 80 pounds per square inch and maximum speed of 5 miles per hour.  The steel wheel roller weight shall be between 6 and 8 tons for the tandem type.

D.	Sweeper:  Shall be vehicle mounted with variable speed, angle, and contact pressure.  Sweepers shall have rotary brooms with bristles of not less than 5 inches in length.  Other types of sweeping devices may be used if acceptable to the Engineer.  No sweeping vehicles equipped with tractor tires shall be used.

E.	Support Vehicles:  Use support vehicles as necessary to continuously load emulsion and aggregates to allow for a continuous, non-stop operation.

F.	Flagger Service and Pilot Vehicles:  When needed, the Contractor shall provide according to Section 512 of the Specifications.

VI.	TEST SECTION

At the start of this work, unless waived by the Engineer, the Contractor shall construct at least a 400-foot test section at no cost to the Department.  Construct the test section at a location designated by the Engineer.  Construct the test section using the same equipment, and the same material sources and application rates indicated on the design and that will be used on the project.  During construction of the test section, demonstrate that the macro-texture wearing course is capable of final sweeping, without damage, within one hour after application.  If the demonstration is unsuccessful, corrective actions shall be taken until results are acceptable to the Engineer.  Additional test section(s) shall be placed at no cost to the Department until the demonstration is satisfactory to the Engineer.

VII.	DEFECTIVE WORK

Where the Engineer deems work defective, the Contractor shall remove and replace, apply additional applications of macro-texture, or repair such areas using methods acceptable to the Engineer at no cost to the Department.

VIII.	MEASUREMENT AND PAYMENT

Macro-texture surface treatment will be measured and paid for at the contract unit price per square yard on a plan quantity basis, complete-in-place, which price bid shall include furnishing and applying aggregate and modified polymer asphalt emulsion, protection of the macro-texture surface treatment and all incidentals necessary to complete the work.

Sweeping shall be included in the price bid for other appropriate items.

| Pay Item | Pay Unit |
| --- | --- |
| Macro-Texture Surface Treatment | Square Yard |