GUIDELINES — For use with Asphalt Schedule Work - Plant Mix projects.  Include SP211-000100-02. {2007-S315HP1}

SP315-000100-02

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

DENSITY DETERMINATION

September 21, 2018

SECTION 315—ASPHALT CONCRETE PAVEMENT of the Specifications is amended as follows:

Section 315.04—Placement Limitations is amended to add the following:

Density: Methods for acceptance and payment of in-place density will be determined according to Table III-2A, and performed as described herein.

| TABLE III-2A Density Acceptance Methods |  |  |  |
| --- | --- | --- | --- |
| Density Acceptance Method to be used | Route type | Traffic Group | Minimum roadway pavement width |
| Method ‘A’ (plugs or cores) | - All intersate & limited access primary - Primary & secondary with minimum traffic & width | X and higher (>=2,000 ADT) | 20’ |
| Method ‘B’ (nuclear guage) | - Primary & secondary not meeting minimum traffic & width | IX and lower (< 2,000 ADT) | n/a |

Section 315.05(e)1 is amended to replace the first and second paragraphs with the following:

Contractor Quality Control – roller patterns, control strips, and test sections

The Contractor shall perform roller pattern and control strip density testing on surface, intermediate, and base courses in accordance with the requirements of VTM-76.  The Contractor shall have a certified Asphalt Field Technician II perform all density testing.

Density shall be determined with a thin-lift nuclear gauge conforming to VTM-81 or from the testing of plugs/cores taken from the roadway where the mixture was placed.  Density test locations shall be marked and labeled according to VTM-76.  When acceptance testing is performed with a nuclear gauge, the Contractor shall have had the gauge calibrated within the previous 12 months by an approved calibration service.  In addition, the Contractor shall maintain documentation of such calibration service for the 12-month period from the date of the calibration service.  The required density of the compacted course when tested with a nuclear gauge shall not be less than 98.0 percent and not more than 102.0 percent of the target control strip density.

Table III-3 – Density Requirements is replaced with the following:

| TABLE III-3 Minimum Control Strip Density Requirements |  |
| --- | --- |
| Mixture Type | Min. Control Strip Density (%)1 |
| SM-9.5A, 12.5A | 92.5 |
| SM-9.5D, 12.5D | 92.5 |
| SM-9.5E, 12.5E | 92.5 |
| IM-19.0A, IM-19.0D, IM-19.0E | 92.2 |
| BM-25.0A, BM-25.0D | 92.2 |
| 1The control strip density requirement is the percentage of theoretical maximum density of the job-mix formula by SUPERPAVE mix design or as established by the Engineer based on two or more production maximum theoretical density tests. |  |

Table III-4 – Payment Schedule for Lot Densities is replaced with the following:

| TABLE III-4 Payment Schedule for Failing Control Strips |  |
| --- | --- |
| % TMD | % of Payment |
| Greater than 96.5 | 95 |
| 92.2/92.51– 96.5 | 100 |
| 90.0-92.1/92.41 | 90 |
| 88.0-89.9 | 80 |
| Less than 88.0 | 75 |
| 1For SM-9.5 and SM-12.5 mixes, the minimum density value is 92.5% per Table III-3. For IM-19.0 and BM-25.0 mixes, the minimum density value is 92.2 per Table III-3. |  |

Section 315.05(e)1a Control Strip is amended to replace the last paragraph with the following:

The control strip shall be considered a lot.  If the control strip density conforms to the requirements specified in Table III-3, the Engineer will consider the control strip to be acceptable and the control strip density shall become the target control strip density.

If the Engineer determines that the control strip requirements in Table III-3 cannot be met due to in-situ pavement conditions, Method ‘B’ will be used for acceptance and payment and density adjustments will be waived.

Otherwise, if the density does not conform to the requirements specified in Table III-3, the tonnage placed in the control strip and any subsequent paving prior to construction of another control strip will be paid for in accordance with Table III-4.  The Contractor shall take corrective action to comply with the density requirement specified in Table III-3.

Section 315.05(e)1b Test section (lot) is replaced with the following:

Test section (lot):  For the purposes of both contractor quality control and for determining acceptance, the Engineer will consider each day’s production as a lot unless the paving length is less than 3,000 linear feet or greater than 7,500 linear feet, irrespective of the method of acceptance (Method ‘A’ (cores/plugs) or Method ‘B’ (nuclear gauge)).  When paving is less than 3,000 feet, that day’s production will be combined with the previous day’s production or added to the next day’s production to create a lot as described below.

The standard size of a lot will be 5,000 linear feet (five 1,000 foot sublots) of any pass 6 feet or greater made by the paving train for the thickness of the course.  If the Engineer approves, the lot size may be increased to 7,500 linear foot lots with five 1,500 foot sublots when the Contractor’s normal daily production exceeds 7,000 feet.  Pavers traveling in echelon will be considered as two passes.  When a partial lot occurs at the end of a day’s production or upon completion of the project, the lot size will be redefined as follows:

●	If the partial lot contains one or two sublots, the sublots will be added to the previous lot.

●	If the partial lot contains three or four sublots, the partial lot will be redefined to be an entire lot.

The Contractor shall test each lot for density by taking a nuclear density gauge reading from two random test sites selected by the Engineer within each sublot.  When saw plugs or cores are used to determine acceptance, a single test site per sublot will be selected by the Engineer.  Test sites will not be located within 12 inches of the edge of any application width for surface and intermediate mixes or within 18 inches of the edge of any application width for base mixes.

The Engineer will compare the average of the sublot density measurements to the target nuclear density, or for plugs and cores, to the target percent of theoretical maximum density achieved on the control strip to determine the acceptability of the lot.  The Contractor shall immediately institute corrective action if two consecutive sublots produce density results less than 98% or more than 102% of the target control strip density.

Longitudinal joints shall also be tested for density using a nuclear density gauge at each test site in the sublot.  For surface and intermediate mixes, the edge of the gauge shall be placed within 4 inches of the joint.  For base mixes, the edge of the gauge shall be placed within 6 inches of the joint.  The Contractor shall not place the gauge over top of the joint.  The joint density value shall be recorded.  The Contractor shall report to the Engineer and institute corrective action if a single longitudinal joint density reading is less than 95 percent of the target control strip density..  The Engineer will not use the values obtained from the joint readings in payment calculation.  The Contractor shall furnish the test data developed during the day’s paving to the Engineer by the end of the day’s operations.

Table III-4A – Payment Schedule for Surface, Intermediate and Base Courses is inserted as follows:

| TABLE III-4A Payment Schedule for Method A Lot Densities |  |
| --- | --- |
| % TMD | % of Payment |
| Greater than 96.5 | 95 |
| 92.21/92.52 – 96.5 | 100 |
| 90.0 – 92.11/92.42 | 90 |
| 88.0 – 89.9 | 80 |
| Less than 88.0 | 75 |
| 1For Intermediate and Base Mixes, the minimum TMD percentage is 92.2 per Table III-3 2For Surface Mixes, the minimum TMD percentage is 92.5% per Table III-3 |  |

Table III-4B – Payment Schedule for Lot Densities is inserted as follows:

| TABLE III-4B Payment Schedule for Method B Lot Densities |  |
| --- | --- |
| % of Target Control Strip Density | % of Payment |
| Greater than 102.0 | 95 |
| 98.0 to 102.0 | 100 |
| 97.0 to less than 98.0 | 95 |
| 96.0 to less than 97.0 | 90 |
| Less than 96.0 | 75 |

Section 315.05(e)3 Density Acceptance & Payment is inserted as follows:

Density Acceptance & Payment

a.	Method ‘A’ (plugs or cores)

For all interstate and limited access routes, and for primary and secondary routes in Traffic Group X or greater (ADT 2,000) and a minimum of 20’ in width, field density will be determined for acceptance and payment using plugs or cores.

The Contractor shall perform acceptance testing for density for each sublot by obtaining one plug, defined as a sawed 4 inch by 4 inch specimen, or one 4-inch-diameter core, at a single random test site selected by the Engineer.  (note: more than one plug or core can be taken in the event the original sample is damaged)

The sub-lot site shall be marked as described in VTM-76. The bulk specific gravity of the plugs or cores shall be determined in accordance with VTM-6. The density of the plugs or cores shall be determined in accordance with VTM-22, excepting that the daily Rice values obtained by the contractor for the mix will be used for calculating percent density (instead of using the 5-day running average as noted in VTM-22).

Plugs or cores shall be taken from the pavement and bulked in the presence of the Engineer unless otherwise approved.  The Department reserves the right to have the plugs or cores bulked on the project site.  In the event of any uncertainty around the bulking procedures or results, the Department further reserves the right to re-bulk the samples.  The Contractor will have the right to witness the re-bulking. The Contractor will be responsible for maintaining the cores until approved for disposal by the Department.

The Contractor shall number sublot test sites sequentially per lot, mark these on the pavement, fill them with the paving mixture, and compact them prior to the completion of each day of production.

The Contractor shall clean and straighten any irregular edges prior to filling and compacting. Liquid tack material shall be applied so it visibly covers all plug or core hole surfaces (sides, bottom, etc.). Hot mix asphalt paving mixture available on the same day of paving, or other permanent patching material as approved by the Engineer, shall be placed into the plug or core hole and compacted with a minimum of a 10-lb weighted hand tool or greater compactive effort with rollers or other equipment available on-site and approved by the Engineer.

The tonnage of each lot will be based on the lot’s width and length and the mixture application rate as designated in the Contract or as revised by the Engineer.  Payment will be made in accordance with the requirements of Table III-4A.

If a minimum of 80% of each lot’s core/plug samples is no lower than 92.5% of TMD for Surface Mixes and 92.2% of TMD for Intermediate and Base Mixes and the lot average results in 100% payment, then the Engineer will increase the unit bid price for AC  mixture by five (5) percent.

The Engineer at any time on any project may perform lot density verification testing.  Lot density verification is performed by testing plugs or cores.  The Contractor shall be responsible for taking plugs or cores for testing.  The Engineer will perform verification testing of the plugs or cores  per the VDOT Manual of Instructions Section 503.03 – Verification Density Testing.  If the Contractor disputes either the density of the plugs or cores determined or the resulting pay factor does not provide for at least 100% payment of the unit bid price, then the Contractor may request additional sampling to be invoked as outlined in Section 503.03(a)(1) of the Manual of Instructions.  Payment for that lot will be in accordance with Table III-4A.

Longitudinal joints shall also be tested for density using a nuclear density gauge at each test site in the sublot.  For surface and intermediate mixes, the edge of the gauge shall be placed within 4 inches of the joint.  For base mixes, the edge of the gauge shall be placed within 6 inches of the joint.  The Contractor shall not place the gauge over top of the joint.  The joint density value shall be recorded.  The Contractor shall report to the Engineer and institute corrective action if a single longitudinal joint density reading is less than 95 percent of the target control strip density.  The Engineer will not use the values obtained from the joint readings in payment calculation.  The Contractor shall furnish the test data developed during the day’s paving to the Engineer by the end of the day’s operations.

b.	Method ‘B’ (nuclear gauge)

For all primary and secondary routes in Traffic Group IX and below (ADT less than 2,000) or width less than 20’, field density will be determined for acceptance and payment using a nuclear gauge.

The Contractor shall test each lot for density by taking a nuclear density gauge reading from two random test sites selected by the Engineer within each sublot.  Test sites will not be located within 12 inches of the edge of any application width for surface and intermediate mixes or within 18 inches of the edge of any application width for base mixes.

The Engineer will compare the average of the sublot density measurements to the target nuclear density, or for cores, to the target percent of theoretical maximum density achieved on the control strip to determine the acceptability of the lot.  Once the average density of the lot has been determined, the Engineer will not allow the Contractor to provide additional compaction to raise the average.  The Contractor shall immediately institute corrective action if two consecutive sublots produce density results less than 98% or more than 102% of the target control strip density.

Longitudinal joints shall also be tested for density using a nuclear density gauge at each test site in the sublot.  For surface and intermediate mixes, the edge of the gauge shall be placed within 4 inches of the joint.  For base mixes, the edge of the gauge shall be placed within 6 inches of the joint.  The Contractor shall not place the gauge over top of the joint.  The joint density value shall be recorded.  The Contractor shall report to the Engineer and institute corrective action if a single longitudinal joint density reading is less than 95 percent of the target control strip density.  The Engineer will not use the values obtained from the joint readings in payment calculation.  The Contractor shall furnish the test data developed during the day’s paving to the Engineer by the end of the day’s operations.

The tonnage of each lot will be based on the lot’s width and length and the mixture application rate as designated in the Contract or as revised by the Engineer.  Payment will be made in accordance with the requirements of Table III-4B.

The Engineer at any time on any project may perform lot density verification testing.  Lot density verification is performed by testing plugs or cores.  The Contractor shall be responsible for taking plugs or cores for testing.  The Engineer will perform verification testing of the plugs.

On surface, intermediate, and base mixes, the Contractor shall take two plugs or cores per Verification, Sampling and Testing (VST) lot at locations selected by the Engineer.  If the Engineer determines the density of the plugs or cores does not conform to the requirements for the lot in question or the same payment percentage determined by the Contractor’s testing for that lot, then the Contractor may request additional sampling to be invoked.  The Contractor shall take one additional plug or core from the remaining sublots.  Payment for that lot, based on the results of the initial two plugs or cores or referee procedure, will be in accordance with the Table III-4A for Method A on the basis of the percentage of the theoretical maximum density or Table III-4B for Method B on the basis of the percentage of the control strip bulk density achieved.