SP315-000120-02

GUIDELINES — Projects requiring asphalt concrete type SM-4.75.{2007-S315U03}

SP315-000120-02

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

DENSE GRADED ASPHALT MIX TYPE SM-4.75

September 20, 2016

I.	DESCRIPTION

This work shall consist of the production, placement and acceptance criteria of the thin asphalt concrete material designated as type SM-4.75 according to the Contract requirements, this provision, and as directed by the Engineer.  SM-4.75 mix types are specified as one of the types listed as follows:

| Mix Type | Asphalt Performance Grade |
| --- | --- |
| SM-4.75A | 64S-22 |
| SM-4.75D | 64H-22 |
| SM-4.75E | 64E-22 |

II.	MATERIALS

A.	Asphalt: The asphalt cement shall be performance graded asphalt (PG) 64S-22, 64H-22 or 64E-22 meeting the requirements of Section 210 of the Specifications or as designated by the Engineer.

B.	RAP: Recycled asphalt pavement material will be permitted according to Table II-14A in Section 211 of the Specifications.

C.	Coarse aggregate shall conform to Section 203 of the Specifications, except for grading, or as directed by the Engineer.

D.	Fine aggregate shall conform to Section 202 of the Specifications, except for grading.  The uncompacted void content shall not have a value less than 40 percent when tested according to AASHTO T 304 Method A and the sand equivalent value shall not be less than 40 percent when tested according to AASHTO T 176.

E.	Anti-stripping Additive shall be hydrated lime at a rate of one percent of the total mix or a chemical anti-stripping agent, which has a proven performance in asphalt concrete using the same aggregate sources as approved by the Engineer.

III.	MIX GRADATION LIMITS

The Contractor shall submit for the Engineer’s approval, a job mix formula within the following design ranges of percent passing each sieve size as noted:

| Table 1 - Design Ranges |  |  |
| --- | --- | --- |
| Sieve Size | Percent By Weight Passing Square Mesh Sieves (in) |  |  |
|  | Maximum | Minimum |  |
| 1/2” | - | 100 |
| 3/8” | 100 | 95 |
| #4 | 100 | 90 |
| #16 | 55 | 30 |
| #200 | 13 | 6 |

IV.	MIX VOLUMETRICS

The Contractor shall submit for the Engineer’s approval, a job mix formula within the following design ranges of volumetrics as noted:

| Table 2 - Mix Design and Production Criteria |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mix Type | VTM (%) Production (Note 1) | VFA (%) Design | VFA (%) Production (Note 2) | Min. VMA (%) | Fines/Asphalt Ratio (Note 3) | Number of Gyrations |
|  |  |  |  |  |  | N Design |
| SM-4.75 Notes 1,2,3 | 3.0-6.0 | 70-75 | 70-80 | 16.5 | 1.0 – 2.0 | 50 |

Note 1:  Asphalt content should be selected at 5.0 percent Air Voids.

Note 2:  During production of an approved job mix, the VFA shall be controlled within these limits.

Note 3:  Fines-Asphalt Ratio is based on effective asphalt content.

V.	MIX PERMEABILITY

For mix design approval, permeability test data shall be submitted according to VTM 120 using the regression method.  The pill height shall be one inch.  If the regression method predicts a permeability exceeding 150 x 10-5 cm/sec at 7.5 percent voids, the Contractor shall redesign the mixture to produce a permeability number less than 150 x 10-5 cm/sec.

VI.	PLANT ACCEPTANCE

A lot will be considered acceptable for gradation and asphalt content according to Section 211 of the Specifications with process tolerances as defined Table 3 applied to the design sieves in Table 1.  One adjustment point will be applied for each 1 percent that the material is out of the process tolerance for the No. 16 Sieve, applied in 0.1 percent increments, all other adjustments will be applied according to Section 211.09 of the Specifications.

| TABLE 3 Process Tolerance |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Tolerance on Each Laboratory Sieve and Asphalt Content: Percent Plus and Minus |  |  |  |  |  |  |  |  |  |  |
| No. Tests | Top Size1 | 1 ½” | 1” | ¾” | ½” | 3/8” | No. 4 | No. 16 | No. 200 | A.C. |
| 1 | 1.0 | 8.0 | 8.0 | 8.0 | 8.0 | 8.0 | 8.0 | 8.0 | 2.0 | .60 |
| 2 | 1.0 | 5.7 | 5.7 | 5.7 | 5.7 | 5.7 | 5.7 | 5.7 | 1.4 | 0.43 |
| 3 | 1.0 | 4.4 | 4.4 | 4.4 | 4.4 | 4.4 | 4.4 | 4.4 | 1.1 | 0.33 |
| 4 | 1.0 | 4.0 | 4.0 | 4.0 | 4.0 | 4.0 | 4.0 | 4.0 | 1.0 | 0.30 |
| 5 | 1.0 | 3.6 | 3.6 | 3.6 | 3.6 | 3.6 | 3.6 | 3.6 | 0.9 | 0.27 |
| 6 | 1.0 | 3.3 | 3.3 | 3.3 | 3.3 | 3.3 | 3.3 | 3.3 | 0.8 | 0.24 |
| 7 | 1.0 | 3.0 | 3.0 | 3.0 | 3.0 | 3.0 | 3.0 | 3.0 | 0.8 | 0.23 |
| 8 | 1.0 | 2.8 | 2.8 | 2.8 | 2.8 | 2.8 | 2.8 | 2.8 | 0.7 | 0.21 |
| 12 | 1.0 | 2.3 | 2.3 | 2.3 | 2.3 | 2.3 | 2.3 | 2.3 | 0.6 | 0.17 |
| 1Defined as the sieve that has 100% passing as defined in Table II-13. |  |  |  |  |  |  |  |  |  |  |

In the event the Department or Contractor determines that the mixture being produced does not conform to the approved job-mix formula based on the Department’s or Contractor’s test results, the Contractor shall immediately make corrections to bring the mixture into conformance with the approved job-mix formula or cease paving with that mixture. Subsequent paving operations using either a revised or other job-mix formula that has not been verified for acceptance as described herein shall be limited to a test run of 300 tons maximum.  No further paving using that specific mixture shall occur until the acceptability of the mixture being produced has been verified using the 300-ton constraint.

VII.	PLACING, FINISHING AND COMPACTION

The application rates of SM-4.75 will be specified in the Contract or as directed by the Engineer.

The Contractor shall plan his operation so a continuous paving operation provides for a constant steady movement of the paver.  The placement of the SM-4.75 shall be as continuous as possible and shall be scheduled such that the interruption occurring at the completion of each day’s work will not detrimentally affect the partially completed work.

Immediately after the mixture has been spread and struck off, it shall be thoroughly and uniformly rolled and compacted.  Breakdown rolling shall be accomplished with steel wheel roller(s) with a minimum weight of 10 tons.  The mixture shall receive a minimum of three breakdown roller passes prior to intermediate and finish rolling.

Should visual examination by the Engineer reveal that the material in any load, or portion of the paved roadway is contaminated, segregated, or flushed with asphalt cement, that load, or portion of the paved roadway may be rejected without additional sampling of the material.

The minimum laydown temperatures for SM-4.75A and SM-4.75D shall not be less than 270°F. For SM-4.75E, the minimum laydown temperature shall not be less than 290°F.

VIII.	Weather Restrictions

SM-4.75 mixture shall be placed only when the ambient and surface temperature are 50 degree F or above.  The Contractor shall employ a Material Transfer Vehicle (MTV) during the placement of SM-4.75 mixtures for the ambient and/or surface temperature between 50-60 degree F.

IX.	FIELD ACCEPTANCE

Lot Density, roller pattern and control strip density testing shall be performed per VTM-76.  However, sawn cores/plugs will not be required to determine the field percentage of the maximum theoretic density for the mixture.  The required density of the compacted mixture shall not be less than 98.0 percent and not more than 102.0 percent of the target control strip for the test section.  Payment schedules for lot density will be according to Table III-4 in Section 315.05 of the Specifications.

X.	MEASUREMENT AND PAYMENT

Asphalt concrete type SM-4.75A will be measured in tons and paid for at the contract unit price per ton, which price shall include surface preparation; and all materials, additives, labor, testing and equipment necessary to complete the work.

Asphalt concrete type SM-4.75D will be measured in tons and paid for at the contract unit price per ton, which price shall include surface preparation; and all materials, additives, labor, testing and equipment necessary to complete the work.

Asphalt concrete type SM-4.75E will be measured in tons and paid for at the contract unit price per ton, which price shall include surface preparation; and all materials, additives, labor, testing and equipment necessary to complete the work.

Tack Coat will be measured and paid in accordance with Section 310.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete Type SM-4.75A | Ton |
| Asphalt Concrete Type SM-4.75D | Ton |
| Asphalt Concrete Type SM-4.75E | Ton |