GUIDELINES – Use when requested by the designer for asphalt projects. Include SP211-000400-01.

SP315-000400-01

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

COLD CENTRAL PLANT RECYCLING MATERIAL PLACEMENT

March 10, 2020

- Description

This specification covers the furnishing, installation and acceptance criteria for Cold Central Plant Recycling (CCPR) pavement.

- Materials

  - Cold Central Plant Recycling Material (CCPRM) shall conform to the Special Provision for Cold Central Plant Recycling Material.

  - Asphalt for tack coat shall conform to Section 310 of the Specifications.

  - Fog Seal shall be a CSS-1h or CQS-1h conforming to Section 210 of the Specifications.

  - Fine Aggregate used for Grit application shall conform to Section 202 of the Specifications.

- Equipment

  - Hauling Equipment shall conform to Section 315.03(a) of the Specifications.

  - Asphalt Pavers shall conform to Section 315.03(b) of the Specifications.

  - Rollers shall conform to Section 315.03(c) of the Specifications. At least one pneumatic roller shall have a minimum gross operating weight of at least 50,000 pounds. Pneumatic rollers shall have properly working scrapers and water spraying systems. At least one double drum vibratory roller shall have a gross operating weight of at least 24,000 pounds and a width of 78 inches.

- Weather Limitations

Placement of CCPRM shall be completed when both the atmospheric temperature and material to be processed (measured in the shade and away from artificial heat) is a minimum 50°F.  CCPRM placement shall not begin when the weather forecast calls for freezing temperatures within 48 hours after placement of the CCPRM on any portion of the project.

- Placing and Finishing

  - Emulsified Asphalt, used as a stabilizing agent, shall not be used when placement occurs during night time hours and will be opened to traffic the next morning.

  - The vibratory setting on rollers shall be at the highest frequency and lowest amplitude setting. The Contractor shall establish a rolling pattern and control strip to determine the maximum achievable density. The testing shall be conducted using a nuclear gauge in backscatter mode for CCPRM layer depth of 3.0 inches or less, or the direct transmission mode for CCPRM layer depth greater than 3.0 inches .  Final rolling to eliminate pneumatic tire marks and to achieve density shall be done by double drum steel rollers, either operating in a static, oscillating, or vibratory mode at the highest frequency and lowest amplitude. Oscillating and vibratory modes should only be used if it is shown to not damage the pavement.

Rolling shall start no more than 30 minutes after initiation of paving. Finish rolling shall be completed no more than one hour after paving is completed, unless otherwise approved by the Engineer. When possible, rolling shall not be started or stopped on uncompacted material, but performed with rolling patterns established so that they begin or end on previously compacted material or the existing pavement.

  - If CCPRM is subjected to traffic, after compaction of the CCPRM but before asphalt overlay, a fog seal and grit application shall be applied. The fog seal shall be applied to the recycled surface at a uniform application rate of 0.06 gal/yd2 (0.04 gal/yd2 residual).  . A light grit shall be applied at a rate of 2 to 3 lbs/yd2 to the fog seal to aide in the reduction of CCPRM pickup and raveling. After fog sealing, no traffic, including the Contractor’s equipment, will be permitted on the completed CCPRM for at least 2 hours.  After 2 hours rolling traffic may be permitted on the recycled material. Rolling traffic means wheeled vehicles that do not start, stop, or turn while on the recycled material. This time may be adjusted by the Engineer to allow establishment of sufficient cure so traffic will not initiate raveling. After opening to traffic, the surface of the CCPRM shall be maintained in a condition suitable for the safe movement of traffic. All loose particles that may develop on the CCPRM surface shall be removed without damaging the surface.

  - Any damage to the completed CCPRM, such as raveling or other surface imperfections, shall be repaired by the Contractor before the placement of any additional asphalt layers or other applicable surface treatment, to the Engineer’s satisfaction according to Section 105.14 of the Specifications at no additional cost to the Department.

  - Before placing any asphalt layers, additional CCPRM layers or other applicable surface treatment, the CCPRM shall be allowed to cure until the moisture of the material is a maximum of 50% of the optimum moisture content or until approval of the Engineer is received. Moisture content shall be measured in accordance with AASHTO T 329 on samples (immediately placed in sealed plastic bag) taken from two stratified random locations as determined by the Engineer per each production day. Other methods and sampling rates may be used if supplied in the Contractor’s Quality Control Plan and approved by the Engineer. Split samples may be taken at the direction of the Engineer. Split samples may be part of the stratified random locations or at additional locations determined by the Engineer. A tack coat shall be applied prior to any additional asphalt layers.

- Acceptance

  - Field Compaction: A nuclear density gauge conforming to VTM 10 shall be used for determining CCPRM density by Backscatter when the CCPRM layer depth is 3.0 inches or less, or the Direct Transmission method when the CCPRM layer depth  is greater than 3.0 inches. The Contractor’s nuclear density gauge shall have been calibrated within the previous 12 months by an approved calibration service.  The Contractor shall maintain documentation of such calibration service for the 12-month period from the date of the calibration service and furnish the same to the Engineer if requested. The Contractor shall determine a roller pattern and construct a control strip at the beginning of work on the project, in accordance with VTM 10. Density test locations shall be marked and labeled according to VTM 76.  The control strip (CS) will be acceptable if both the field proctor (AASHTO T 180, Method D) and the CS nuclear density average is at least 98% of the maximum dry l density (MDD) from the approved job mix formula (JMF). A single moisture sample shall be taken from the uncompacted CCPRM in the CS and tested in accordance with VTM 10. Moisture contents shall be calculated as defined in VTM 10    The Contractor shall construct an additional roller pattern and control strip when a change in the source of material is made, when a change in compaction equipment is made, when a significant change occurs in the composition of the material being placed from the same source, or when there is a failing test section.

  - Test section (lot) – For the purposes of acceptance, each day’s production will be considered a lot unless the paving length is less than 3,000 feet or greater than 7,500 feet.  When paving is less than 3,000 feet, it shall be combined with the previous day’s production or added to the next day’s production to create a lot as described below.

The standard size of a lot shall be 5,000 feet, with 1,000 foot sublots, of any pass 6 feet or greater made by the paving train for the thickness of the course. If the Engineer approves, the lot size may be increased to 7,500 feet with five 1,500 foot sublots when the Contractor’s normal daily production exceeds 7,500 feet. Pavers traveling in echelon will be considered as two passes. When a partial lot occurs at the end of a day’s production or upon completion of the project, the lot shall be added to the previous lot if the partial lot contains one or two complete sublots or redefined to be an entire lot if the partial lot contains three or four complete sublots.

The Contractor shall test each lot for acceptance for density by taking a nuclear density reading from two random test sites selected by the Engineer within each sublot.  Test sites will not be located within 18 inches of the edge of any application width of CCPRM.

The average of the sublot density measurements will be compared to the target density established by the control strip to determine the acceptability of the lot. Once the average density of the lot has been determined, the Contractor will not be permitted to provide additional compaction to raise the average. If two consecutive sublots produce density results less than 98% of the CS target density, the Contractor shall immediately notify the Engineer and institute corrective action to bring lot density into conformance.One moisture sample will be taken from two test locations per lot, from the uncompacted CCPRM in close proximity to where the test site will be. The average moisture content of these two samples will be used to correct the nuclear readings to dry densities for the entire lot. Moisture correction is as defined in VTM 10.

By the end of each day’s operations, the Contractor shall furnish the test data developed during the day’s recycling to the Engineer. The Contractor shall verify the results of every lot by performing a field proctor in accordance with AASHTO T180, Method D. The field proctor shall be at least 98 percent of the JMF proctor’s MDD.

The tonnage of each lot will be based on the lot’s width and length and the mixture thickness as designated in the Contract or as revised by the Engineer. Payment will be made according to Table 1. Percent of payment will be calculated based on the unit cost of Cold Central Plant Recycling Material (CCPRM).

| Table 1 Payment Schedule for Lot Densities |  |
| --- | --- |
| % of Target Control Strip Density | % of Payment |
| 98.0 or greater | 100 |
| 97.0 to less than 98.0 | 95 |
| 96.0 to less than 97.0 | 90 |
| Less than 96.0 | 75 |

  - Depth Checks shall be performed by the Contractor at a rate of twice per 5,000 feet after compaction according to VTM 38, Method B. Depth checks shall be taken at locations selected by the Engineer. In the event that a slit trench cannot be created according to VTM 38, Method B, the Contractor may remove the CCPRM by use of a core rig and depth measurements taken according to VTM 38, Method B.

Acceptance of CCPRM course for depth will be based on the mean result of measurements of samples taken from each lot of material placed.

A lot will be considered acceptable for depth if the mean result of the tests is within the tolerance of the plan depth for the number of tests taken as shown in Table 2.

| Table 2 Process Tolerance for Depth Checks |  |  |  |
| --- | --- | --- | --- |
| Plan Depth, inches | Tolerance, inches (Plus or Minus) |  |  |
|  | 2 tests | 3 tests | 4 tests |
| ≤ 4 | 0.45 | 0.35 | 0.30 |
| >4 ≤ 8 | 0.65 | 0.50 | 0.40 |
| >8 ≤ 12 | 0.90 | 0.70 | 0.50 |
| >12 | 1.00 | 0.80 | 0.60 |

If the mean depth of a lot of material is in excess of the tolerance, the Contractor will not be paid for that material in excess of the tolerance throughout the length and width represented by the tests. For excessive depth CCPRM courses, the rate of deduction from the tonnage allowed for payment as CCPRM course will be calculated based on the JMF weight per square yard per inch of depth in excess of the tolerance for the plan depth and the number of tests taken as specified in Table 2 or the Department may require excessive material to be removed at the Contractor’s expense.

If the mean depth of a lot of material is deficient by more than the allowable tolerance for the plan depth specified, correction will be required and the Contractor will be paid for the quantity of material that has been placed in the lot. For sections of CCPRM course that are deficient in depth beyond the tolerance, the Contractor shall furnish and place material specified for the subsequent course or as approved by the Engineer to bring the deficient CCPRM course depth within the tolerance of the specified plan depth. This additional material shall be placed at the Contractor’s expense.

  - Density and Depth Check Construction Records: The Contractor shall prepare and submit to the Engineer separate test reports for density and depth testing meeting the requirements of AASHTO R 18 or may use the current appropriate VDOT forms.

- Trial Section

At least one week but not more than 30 days before the start of production, the Contractor shall construct a 1,000 foot long trial section, one-lane wide, at the designated thickness and designed optimal stabilizing agent content provided in the approved JMF. The trial section will be constructed at a location approved by the Engineer on the project using the same construction procedures and equipment intended for the entire project. Production will cease after construction of the trial section until the trial section is evaluated and accepted by the Engineer according to the requirements herein and the Special Provision for Cold Central Plant Recycling Material. The Trial Section shall be considered a lot and payment will follow the payment tables established in this specification and the Special Provision for Cold Central Plant Recycling Material.

Should the initial trial section fail, the Contractor shall construct a second trial section on the project site and shall have a Technical Representative present during mixing and placing operations for the second trial section. When a Technical Representative is required, they shall remain present during mixing and placement of any additional trial sections until acceptance has been made by the Department. The Technical Representative shall also be present for the next day of production to oversee the mixing and placing operation. If during the next production day, the materials meet the mixture and placement acceptance criteria, the Technical Representative will no longer be required on the project site. If additional trial sections beyond the first two are needed, the Contractor shall construct the trial section at sites approved by the Engineer.

The Technical Representative shall meet the following criteria:

- Have 2 years minimum experience with the CCPRM process

- Have personally supervised a minimum of 5 successful CCPRM projects

- Have personal experience in developing CCPRM mix designs

- Have the experience to perform and supervise field process control testing

- Submit a list of references, with current telephone numbers, of persons who are able to verify the experience required herein

The Contractor may use consultants or manufacturers’ representatives to satisfy the technical representative requirements listed above.

- Measurement and Payment

Cold Central Plant Recycling Material (CCPRM) will be measured in tons of the completed sections and will be paid for at the Contract ton price.  This price shall be full compensation for removal, hauling and processing of the existing pavement (if RAP from the same project is used) or existing RAP stockpiles; for additional aggregate; for preparing, hauling, placing and compacting of all materials; furnishing stabilizing agents, fog seal, grit and additives; for all freight involved; for all manipulations, rolling and brooming; for testing and documentation; for asphalt supplier services; and for all labor, tools, equipment and incidentals necessary to complete the work. Net weight information shall be furnished with each load of material delivered according to Section 211 of the Specifications. Batch weights will not be permitted as a method of measurement unless the Contractor’s plant is equipped according to Section 211 of the Specifications, in which case the cumulative weight of the batches will be used for payment.

The initial trial section will be paid for at the contract unit price for CCPRM, to include price adjustments. If needed, the Department will pay for up to one additional trial section of CCPRM at the contract unit price, to include price adjustments. The Department will pay for a maximum of two trial sections at the contract unit price. If more than two trial sections are needed, the Contractor shall bear all costs associated with producing and placing the material at a site approved by the Engineer.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Cold Central Plant Recycling Material (CCPRM) | Ton |