GUIDELINES – Use when requested by the Designer for asphalt projects. {2007-S315AC0}

SP315-000410-01

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

Cold In-Place Recycling (CIR)

March 17, 2020

- DESCRIPTION

Cold In-place Recycling (CIR) is defined as a process in which a portion of existing asphalt concrete pavement layers are pulverized, stabilized, and repaved in place.  This is most commonly performed using foamed asphalt or emulsified asphalt as the primary stabilizing additive.  The pavement may be milled, stabilized, and repaved using the same machine or machine train, or paved from a stabilized, windrowed material using traditional practices.

The Contractor shall furnish all labor, materials and equipment required for completing the work.  The Contractor shall select the final job mix formula (JMF) and construction methods to meet the performance requirements specified herein.

- MATERIALS

- Stabilizing agent (Emulsified or Foamed Asphalt): Emulsified asphalts shall conform to Section 210 of the Specifications; liquid asphalts shall be a neat (i.e. not modified) asphalt that meets the requirements of Section 211.02 of the Specifications.  Emulsion shall not be used for night-time work when the lanes will be opened to traffic the next morning.

- Water used for mixing shall conform to Section 216 of the Specifications.

- CIR material shall conform to Table 3.

- Other Additives may be used to meet the requirements in Table 4. In the case where an additional additive is used, the type and dosage shall be described in the JMF(s) submitted to the Department.

- Additional Crushed Reclaimed Asphalt Pavement (RAP) Material (other than that reclaimed from the project) may be added by the Contractor and shall conform to Section 211.02(j) of the Specifications and Table 1.

| Table 1 Additional Crushed RAP |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Deleterious Materials: Clay Lumps and Friable Particles in Aggregate | AASHTO T 112 | 0.2% maximum |
| Maximum Sieve Size, 1.5 inches | AASHTO T 27 | 100% Passing, |

- Fog Seal shall be a CSS-1h or CQS-1h conforming to Section 210 of the Specifications.

- Fine Aggregate for Grit Application shall conform to Section 202 of the Specifications.

- Tack Coat shall be Non-Tracking tack conforming to Section 310 of the Specifications.

- Additional aggregate: Based on the results of the job mixt designs or other requirements of this provision, the Contractor shall determine if additional aggregate is required. If the Contractor determines additional aggregate is needed, any additional aggregate shall conform to Section 203 of the Specifications and Table 2, and it shall be graded to produce a product that conforms to Table 3.

| Table 2 Additional Aggregate |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Los Angeles Abrasion Value | AASHTO T 96 | 45% maximum loss |
| Sand Equivalent | AASHTO T 176 | 45% minimum |
| Maximum size, 100% Passing, Sieve Size | AASHTO T 27 | 1.5 in |
| Water absorption | AASHTO T 85 | 3% maximum |

- QUALITY CONTROL PLAN

The Contractor shall develop and implement a Quality Control Plan to ensure that operational techniques and activities under their control provide a homogeneous and finished material of acceptable quality. Contractor sampling and testing shall be performed to control the processes and ensure material compliance with the Contract.  The Contractor shall provide the Quality Control Plan  and the JMF(s) they intend to use to accomplish the work to the District Materials Engineer for approval at least 30 calendar days before the start of CIR operations.

For each CIR project, a project specific Quality Control Plan is required, and shall include the following (minimum) information:

  - A description of the Contractor’s Quality Control organization, including the number of full-time equivalent employees or Sub-Contractors with specific Quality Control responsibilities, including an organizational chart showing lines of authority and reporting responsibilities.

  - A list of Cold Asphalt Recycling Plant and Field Technicians conforming to Section 200.06 of the Specifciations who will work on the project.A Quality Control Sampling, Testing and Analysis Plan with methods that include a description of how random locations for testing and sampling are determined.

  - Identification and description (Accreditation) of the laboratories to be used for each type of testing.

  - Specific list of documentation for Quality Control activities.

  - Procedures to meet contract requirements for corrective action when QC criteria are not met.

  - Procedures to protect stabilized material from receiving excessive moisture from weather events (e.g. rain, fog, etc.) and corrective actions when criteria are not met.

  - Contingency Plan including:

- Inclement weather

- Equipment breakdowns

- Materials shortages

- Excessive fluff - (greater than approximately 10 percent).  Fluff is defined as the increase in material thickness of the recycled layer over the specified recycling depth due to remixing in place.

- Deficient density of installed CIR

- Material doesn’t break or cure in timely manner, as established by the job-mix design

- Gradation is outside tolerances

- Production modifications based on changes in ambient or material temperature

- Job Mix Formula

CIR mix designs in the form of a JMF shall be submitted to the District Materials Engineer for approval at least 30 calendar days before the start of CIR operations. More than one JMF may be required. The gradation of each JMF shall fall within the bands shown in Table 3.  The Contractor’s contingency plan should address actions to be taken if gradation fails to meet the requirements. The Department at its discretion reserves the right to require appropriate measures that may include stopping the work.

| Table 3 Design Range |  |  |
| --- | --- | --- |
| Sieve Size | Gradation Band1 (Percent Passing) |  |
|  | Lower | Upper |
| 1.5” | 100 | 100 |
| 3/8” | -- | 55 |
| 1Based on pulverized materials, prior to stabilization, washed, following AASHTO T 27 |  |  |

JMF’s shall be created using existing materials obtained directly from the project site prior to the start of construction and any additional RAP or aggregate that is needed to meet the requirements herein. Sampling shall be conducted at a minimum of once per 2500 lane-feet.  Each JMF shall provide, as a minimum, the following mix design parameters:

  - Maximum Dry Density at Optimum Moisture Content

  - Percent by weight of all stabilizing agents to be added to the recycled mix

  - Percent by weight of water (at room temperature) required

  - Expansion ratio and half-life characteristics and temperature of asphalt binder at the time of dosage into foaming chamber (for mixtures using foamed asphalt)

  - Minimum curing time/cure time for the emulsified asphalt

  - Temperature of emulsified asphalt at the time of dosage into the mixture (for mixtures using emulsified asphalt)

  - Target gradation (including any aggregate to be added).

If a change in source materials is made during construction, new JMFs shall be created, submitted to the Engineer and approved prior to use on the project.

JMFs shall conform to Tables 4A and 4B at the approved stabilizing agents’ content.

| Table 4A CIR Mix Design Requirements Emulsified Asphalt Stabilized Materials |  |  |  |
| --- | --- | --- | --- |
| Item | Property | Test Method | Criteria |
| 1 | Moisture Density Relations | AASHTO T 180, Method D | Determined by Design; Used to Establish Target Field Density |
| 2 | Marshall Stability Test1,2 | ASTM D5581 or AASHTO T 245 | 2945 lbs. minimum (ASTM) 1475 lbs. minimum (AASHTO) |
| 3 | Retained Stability1,3 | ASTM D5581 or AASHTO T 245 | Minimum 70% of results of #2 |
| 4 | Raveling Stability4 | ASTM D7196 | Maximum 6% |
| 5 | Materials Gradation Test prior to stabilization | AASHTO T 27, washed | Gradation to control field production. |
| 1The Contractor may test this property using either ASTM D5581 or AASHTO T 245 and compare to the criteria corresponding to that test. 2Three specimens shall be produced at 75 blows per side (or 30 gyrations per AASHTO T 312), cured at 140ºF to constant mass, and held at 104ºF for 2 hours in a forced draft oven immediately before testing. 3An additional three specimens shall be produced at cured at 140ºF to constant mass. Specimens shall then be vacuum saturated to 55-65% in a 77ºF water bath for 23 hours and 104ºF water bath for an additional hour immediately before testing. 4Specimens shall be produced using a gyratory at 20 gyrations and cured at 50ºF for 4 hours at 50% humidity. |  |  |  |

| Table 4B CIR Mix Design Requirements Foamed Asphalt Stabilized Materials |  |  |  |
| --- | --- | --- | --- |
| Item | Properties | Test Method | Criteria |
| 1 | Moisture Density Relations | AASHTO T 180, Method D | Determined by Design; Used to Establish Target Field Density |
| 2 | Dry Indirect Tensile Strength (ITS)1 | AASHTO T 283 Section 11 | 53 psi minimum |
| 3 | Retained Indirect Tensile Strength2 | AASHTO T 283 Section 11 | Min 70% of the Dry ITS from Item 2 |
| 4a | Expansion Ratio (Aggregate temperature is 50ºF to 77ºF) | Wirtgen 2012 Cold Recycling Manual | 10 times |
| 4b | Expansion Ratio (Aggregate temperature is greater than 77ºF) | Wirtgen 2012 Cold Recycling Manual | 8 times |
| 5 | Half-Life | Wirtgen 2012 Cold Recycling Manual | 6 second minimum |
| 6 | Materials Gradation Test prior to stabilization | AASHTO T 27, washed | Gradation to control field production. |
| 1Three specimens shall be produced using 75 blows per side (or 30 gyrations per AASHTO T 312) compacted at or below OMC and oven dried at 104ºF for 72 hrs and cool to ambient temperature for 24 hrs;. 2An additional three specimens shall be produced and cured according to Item 2, Dry Indirect Tensile Strength. Specimens shall be oven dried at 104ºF for 72 hrs and then submerged in 77ºF water bath for 24 hours before testing |  |  |  |

- EQUIPMENT

- CIR shall be completed with a self-propelled machine with a down cutting milling head that is capable of pulverizing and recycling the existing asphalt concrete pavement to a maximum depth of 6 inches, uniformly incorporating the stabilizing agents and water, and mixing the materials to produce a homogeneous product. The machine shall be capable of pulverizing and recycling the full lane width in no more than two passes (with the longitudinal joint located between the anticipated wheel paths).  The machine shall have the ability to meter dosage rates for stabilizing agents and water relative to the machine’s ground speed. Individual valves on the spray bar shall be capable of being turned off as necessary to minimize stabilizing agents and water overlap on subsequent passes. The equipment shall be operated according to the manufacturers’ recommendations.

The self-propelled machine may also have a screed attached to the milling and mixing unit.  The screed shall have slope control and the ability to convey material out to the side of the screed if there is a surge of material between the mixing chamber and the screed. The mixing unit and screed combination shall have electronic grade controls. In lieu of a screed attachment, the material may be placed by means of a material transfer device or windrow into an asphalt paver that conforms to Section 315.03(b) of the Specifications

Any additives such as water, lime slurry, etc. added by the equipment at the milling head or mixing unit shall be controlled through liquid metering devices capable of automatically adjusting for the variation in bituminous material going into the mixing unit, by means of weighing device or proportional control systems.

The metering devices shall be capable of delivering the amount of additive to within +/- 0.2% of the required amount, except that a capability of adding up to 5% water by weight of the pulverized bituminous material is mandatory. The Department will not require metering of the water added at the milling machine to control dust in the screens, belts, or crusher/material sizing unit.

A pozzolonic material distributor truck shall be used if dry stabilizing agents are applied directly to the asphalt concrete pavement prior to CIR operations.  The pozzolonic material distributor truck shall have the ability to uniformly apply the stabilizing agents at the specified rate.

- Rollers – All rollers shall conform to Section 315.03(c) of the Specifications.  Additionally, at least one pneumatic tire roller shall have a minimum gross operating weight of at least 50,000 pounds. At least one double steel-wheeled vibratory roller shall have a gross operating weight of at least 24,000 pounds and a width of 78 inches. All rollers must have properly working scrapers and water spraying systems.

- TRIAL SECTION

Before planned start of full production, stabilize a 2,500 foot long trial section, one-lane wide, at the designated thickness and designed optimal stabilizing agents content provided in the approved JMF. Construct the trial section on the Project at an approved location, using construction procedures intended for the entire Project. Cease production after construction of the trial section until the trial section is evaluated and accepted.  Trial section acceptance will be determined according to Section VII.  The trial section shall be considered a lot and payment will follow the payment tables established in this Special Provision.

Should the initial trial section fail, the Contractor shall construct a second trial section on the Project site at a location approved by the Engineer and shall have a Technical Representative present during mixing and placing operations for the second trial section. The Technical Representative shall remain present during mixing and placement of any additional trial sections until acceptance has been made by the Department. In addition, the Technical Representative shall also be present for the next day of production to oversee the mixing and placing operation. If during the next production day, the materials meet the mixture and placement acceptance criteria, the Technical Representative will no longer be required on the Project site. If additional trial sections beyond the first two are needed, the Contractor shall construct the trial section at sites approved by the Engineer.

The Technical Representative shall meet the following criteria:

•	Have 2 years minimum experience with the CIR process

•	Have personally supervised a minimum of 5 successful CIR projects

•	Have personal experience in developing CIR mix designs

•	Have the experience to perform and supervise field process control testing

•	Submit a list of references, with current telephone numbers, of persons who are able to verify the experience required herein

The Contractor may use Consultants or Manufacturers’ representatives to satisfy the technical representative requirements listed above.

- CONSTRUCTION METHODS

  - Grass and other vegetation shall be removed from the edge of the existing pavement to prevent contamination of the pulverized asphalt concrete material during the milling operation.

  - The existing asphalt concrete pavement shall be milled to the required depth and width as indicated on the plans. CIR shall be performed in a manner that minimizes disturbance of the underlying material in the existing roadway. The milling operation shall be conducted so that the amount of fines occurring along the vertical faces of the cut shall not prevent bonding of the CIR materials. If needed, the CIR materials shall be processed by crushing or sizing to the required gradation specified in Table 3.  When a paving fabric is encountered during the CIR operation, the Contractor shall make the necessary adjustments in equipment or operations so that at least 90% of the shredded fabric in the CIR is no more than the maximum particle size specified in TableABLE 3. These changes may include, but shall not be limited to: adjusting the forward machine speed, milling rate, the milling depth, or adding or removing screens in order to obtain the specified CIR. The Contractor will be required to waste material containing over-sized pieces of paving fabric as directed by the Engineer. The Contractor will not receive additional payment for the necessary adjustments to equipment or CIR operations to accommodate the presence and processing of the paving fabric.

  - Adjacent CIR passes shall overlap by a minimum 4 inches. The stabilizing agents shall be controlled such that it is not applied at the joint overlap location more than the dosage rate in the approved JMF by the total of the passes. Transverse joints between successive CIR operations during the same day of placement shall be overlapped a minimum of 2 feet. The beginning of each day’s CIR operation shall overlap the previous day’s operation a minimum of 50 feet unless otherwise approved by the Engineer.

  - Compaction of the CIR shall be completed using rollers conforming to Section V-2. The Contractor shall establish a rolling pattern and control strip to determine the maximum achievable density . The testing will be conducted using backscatter for CIR layer depth of 3.0 inches or less, or direct transmission mode for CIR layer depth greater than 3.0 inches, with the nucleargauge . Final rolling to eliminate pneumatic tire marks and to achieve density shall be done by double drum steel rollers, either operating in a static, oscillating, or vibratory mode at the highest frequency and lowest amplitude. Oscillating and vibratory modes should only be used if it is shown to not damage the pavement.

Rolling shall start no more than 30 minutes after initiation of paving. Finish rolling shall be completed no more than one hour after paving is completed, unless otherwise approved by the Engineer. When possible, rolling shall not be started or stopped on uncompacted material but performed with rolling patterns established so that they begin or end on previously compacted material or the existing pavement.

  - After compaction of theCIR, a fog seal shall be applied to the recycled surface at a uniform application rate of 0.06 gal/yd2 (0.04 gal/yd2 residual).  .  A light grit shall be applied at a rate of 2 to 3 lbs/yd2 to reduce raveling.  After fog sealing, no traffic, including the Contractor’s equipment, will be permitted on the completed CIR until the water content of the CIR material is a maximum of 50 percent of the optimum water content when measured as described in Section VII-7.  After this “curing” period, rolling traffic may be permitted on the CIR. Rolling traffic means wheeled vehicles that do not start, stop, or turn while on the recycled material. This time may be adjusted by the Engineer to allow establishment of sufficient cure so traffic will not initiate raveling. After opening to traffic, the surface of the CIR shall be maintained in a condition suitable for the safe movement of traffic. All loose particles that may develop on the CIR surface shall be removed without damaging the surface.

  - Any damage to the completed CIR material, such as raveling or other surface imperfections, shall be repaired by the Contractor before the placement of the asphalt concrete surface courses, or other applicable surface treatment , to the Engineer’s satisfaction according to Section 105.14 of the Specifications, at no additional cost to the Department.

  - Before placing the asphalt concrete surface courses, or other applicable surface treatment, the CIR material shall be allowed to cure until the moisture of the CIR is a maximum of 50 percent of the optimum water content or until approval of the Engineer is received. Moisture content shall be measured in accordance with AASHTO T 329 on samples  taken from two stratified random locations and immediately placed in a sealed plastic bag, as determined by the Engineer for each production day. Other methods and sampling rates may be used if supplied in the Contractor’s Quality Control Plan and approved by the Engineer. Split samples may be taken at the direction of the Engineer. A tack coat, shall be applied prior to any additional asphalt layers.

- ACCEPTANCE TESTING

  - Field Compaction – A nuclear density gauge conforming to VTM 10 shall be used for determining CIR density by Backscatter if the CIR layer depth is 3 inches or less, or the Direct Transmission method for CIR layers greater than 3 inches. The Contractor’s nuclear density gauge shall have been calibrated within the previous 12 months by an approved calibration service. The Contractor shall maintain documentation of such calibration service for the 12-month period from the date of the calibration service and furnish the same to the Engineer if requested. The Contractor shall determine a roller pattern and construct a control strip according to VTM 10. Density test locations shall be marked and labeled by the Contractor according to VTM 76. The control strip (CS) will be acceptable if both the field proctor (AASHTO T 180, Method D) and the CS nuclear density average is at least 98 percent of the maximum dry density (MDD) from the approved JMF. A single moisture sample shall be taken from the uncompacted CIR in the CS and tested in accordance with VTM 10.  Moisture contents shall be calculated as defined in VTM 10.   The Contractor shall construct an additional control strip when a change in the source of material is made, when a change in compaction equipment is made, when a significant change occurs in the composition of the material being placed from the same source, or when there is a failing test section.

  - Test section (lot): For the purposes of acceptance, each day’s production will be considered a lot unless the paving length is less than 3,000 feet or greater than 7,500 feet. When paving is less than 3,000 feet, it shall be combined with the previous day’s production or added to the next day’s production to create a lot as described below.

The standard size of a lot shall be 5,000 feet, with 1,000-foot sublots, of any pass 6 feet or greater made by the paving train for the thickness of the course. If the Engineer approves, the lot size may be increased to 7,500 feet with five 1,500-foot sublots when the Contractor’s normal daily production exceeds 7,500 feet. When a partial lot occurs at the end of a day’s production or upon completion of the project, the lot shall be either added to the previous lot if the partial lot contains one or two complete sublots or redefined to be an entire lot if the partial lot contains three or four complete sublots.

Each lot shall be tested for density by taking a nuclear density reading from two random test sites selected by the Engineer within each sublot used for acceptance. Test sites shall not be located within 18 inches of the edge of any application width for CIR mixes.

The average of the sublot density measurements will be compared to the target density established by the control strip to determine the acceptability of the lot. Once the average density of the lot has been determined, the Contractor will not be permitted to provide additional compaction to raise the average. If two consecutive sublots produce density results less than 98 percent of the control strip, the Contractor shall immediately notify the Engineer and institute corrective action to bring lot density into conformance. One moisture sample will be taken from two test locations per lot from the uncompacted CIR in close proximity to each density test location. The average moisture content of these two samples will be used to correct the nuclear readings to dry densities for the entire lot. Moisture correction is as defined in VTM 10.

By the end of each day’s operations, the Contractor shall furnish the test data developed during the day’s production to the Engineer. The Contractor shall verify their results for every lot by performing a field proctor (AASHTO T180, Method D). The field proctor shall be at least 98 percent of the JMF proctor’s MDD.

The tonnage or square yards of each lot will be based on the lot’s width and length and the mixture application rate as designated in the Contract or as revised by the Engineer. Payment will be made according to Table 5.  Percent of Payment will be calculated based on the unit cost of Cold In-Place Recycling (CIR) (Depth), Liquid Asphalt (Emulsion) and Liquid Asphalt (Foamed).

| Table 5 Payment Schedule for Lot Densities |  |
| --- | --- |
| % of Target Control Strip Density | % of Payment |
| 98.0 or greater | 100 |
| 97.0 to less than 98.0 | 95 |
| 96.0 to less than 97.0 | 90 |
| Less than 96.0 | 75 |

  - Gradation: The Contractor shall verify that the unstabilized gradation conforms to the JMF twice per production day. One test shall be at the beginning of each production day.  In addition, the Contractor shall verify the unstabilized gradation wherever there are changes in the pavement structure being recycled. Should the gradation not meet the JMF, the Contractor shall immediately take corrective actions.

  - Depth Check shall be performed by the Contractor according to VTM 38, Method B at a minimum rate of twice per 5,000 feet after compaction. Depth checks shall be taken at locations selected by the Engineer. In the event that a slit trench cannot be created according to VTM 38, Method B, the Contractor may remove the CIR materials by use of a core rig and depth measurements taken according to VTM 38, Method B.

Acceptance of CIR course for depth will be based on the mean result of measurements of samples taken from each lot of material placed.

A lot will be considered acceptable for depth if the mean result of the tests is within the tolerance of the plan depth for the number of tests taken as shown in TableABLE 6.

| Table 6 Process Tolerance for Depth Checks |  |  |  |
| --- | --- | --- | --- |
| Plan Depth (in) | Tolerance (in, ±) |  |  |
|  | 2 tests | 3 tests | 4 tests |
| ≤ 4 | 0.45 | 0.35 | 0.30 |
| >4 ≤ 6 | 0.65 | 0.50 | 0.40 |

If the mean depth of a lot of material is in excess of the tolerance, the Contractor will not be paid for that material in excess of the tolerance for the plan depth specified throughout the length and width of the lot of material represented by the tests. For excessive depth CIR courses, the rate of deduction from the square yardage allowed for payment as CIR course will be calculated by prorating the mean depth measured based on the plan depth specified or the Department may require excessive material to be removed at the Contractor’s expense.

If the mean depth of a lot of material is deficient by more than the allowable tolerance for the plan depth specified, correction will be required and the Contractor will be paid for the quantity of material that has been placed in the lot. For sections of CIR course that are deficient in depth beyond the tolerance, the Contractor shall furnish and place material specified for the subsequent course or as approved by the Engineer to bring the deficient CIR course depth within the tolerance of the specified plan depth. This additional material shall be placed at the Contractor’s expense.

  - Stabilizing Agent Dosage Rate: The Contractor shall verify the stabilizing agent dosage rate by reading a calibrated meter ten times per lot. The dosage rate shall be within 0.20 percentage points of the approved JMF. If the dosage rate is outside 0.20 percentage points, then paving and production shall stop and the Contractor shall take corrective measures to bring the dosage rate within tolerance. The Engineer will calculate the yield at the end of each production day.

  - Construction Records: The Contractor shall prepare separate test reports conforming to AASHTO R 18 or may use the current appropriate VDOT forms.  Records documenting the dosage rate of stabilizing agents and other test results from Tables 4A or 4B shall be provided to the Engineer, unless specified otherwise.

- WEATHER LIMITATIONS

CIR operations shall be completed when both the atmospheric temperature and material to be processed (measured in the shade and away from artificial heat) is a minimum 50°F.  CIR operations shall not begin when the weather forecast calls for freezing temperatures within 48 hours after placement of CIR on any portion of the project.

- MEASUREMENT AND PAYMENT

Cold In-Place Recycling will be measured in square yards of the completed sections for the depth specified and will be paid for at the Contract square yard price. This price shall include removal and processing of the existing pavement; preparing, hauling, and placing of all materials;, fog seal, grit and additives (including all freight involved); all manipulations including removal of grass and other vegetation, rolling, and brooming; testing and documentation; asphalt supplier services; and all labor, tools, equipment and incidentals necessary to complete the work.

Liquid Asphalt (Emulsion) will be measured in tons and paid for at the Contract ton price. This price shall include furnishing and incorporating the emulsion into the mixture. An emulsion content of 2.5% by weight of the milled bituminous material shall be used for bidding purposes before the JMF is approved. The actual emulsion content will be adjusted based on the quantity necessary to conform to Tables 4A and 4B.

Liquid Asphalt (Foamed) will be measured in tons and paid for at the Contract ton price. This price shall include furnishing and incorporating the foamed asphalt into the mixture. A foamed asphalt content of 2.5% by weight of the milled bituminous material shall be used for bidding purposes before the JMF is approved. The actual foamed asphalt content will be adjusted based on the quantity necessary to conform to Tables 4A and 4B.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Cold In-Place Recycling (Depth) | Square Yard |
| Liquid Asphalt (type) | Ton |

Additional Crushed RAP if required to meet the contract requirements will be measured in tons and paid for at $ fill in amount per ton. This price shall include furnishing and incorporating the additional RAP into the mixture. The additional RAP shall conform to Section IV for payment purposes.

Additional Aggregate, if required, according to the JMF and other Contract requirements, will be measured in tons and paid for at $ fill in amount per ton. This price shall include furnishing and incorporating the additional aggregate material into the mixture. The additional aggregate material shall conform to Section IV for payment purposes.