GUIDELINES – Use when requested by the Designer for asphalt projects. {2007-S315AD0}

SP315-000420-01

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

FULL-DEPTH RECLAMATION (FDR)

March 9, 2020

- DESCRIPTION

Full-depth reclamation (FDR) is defined as those processes in which all or a portion of the existing pavement structure is  pulverized, stabilized, and compacted in place; If the portion which is to be pulverized includes all of the existing asphalt pavement layers then a portion of the underlying bound and unbound layers may also be included. This operation is most commonly performed using hydraulic cement, lime, foamed asphalt or asphalt emulsion as the primary stabilizing additives.

The Contractor shall furnish all labor, materials, and equipment required for completing the work.  The Contractor shall select the job mix formulae (JMF) and construction methods to meet the performance requirements specified herein.

- MATERIALS

  - Stabilizing Agents: The amount of stabilizing agents to be used shall be determined by the Contractor by means of a mixture design process.

    - Hydraulic cement shall conform to Section 214 of the Specifications.

    - Lime shall conform to Section 240 of the Specifications.

    - Fly ash shall conform to Section 241 of the Specifications.

    - Asphalt emulsions shall conform to Section 210 of the Specifications

    - Liquid asphalts shall conform to Section 211.02(a) of the Specifications.

  - Water used for mixing shall conform to Section 216 of the Specifications.

  - FDR: material shall meet the gradation requirements of Table 3 before adding any stabilizing agents.

  - Other Additives, if necessary, may be used by the Contractor to meet the requirements in Table 4.  In the case where an additional additive is used, the type and dosage shall be described in the JMFs submitted to the Engineer.  For FDR using asphalt emulsion, hydrated lime shall be added according to Section 211.02(i) of the Specifications.

  - Crushed Reclaimed Asphalt Pavement (RAP) Material conforming to Section 211.02(j) and Table 1 may be added by the Contractor.

| Table 1 Additional Crushed RAP |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Deleterious Materials: Clay Lumps and Friable Particles in Aggregate | AASHTO T 112 | 0.2% maximum |
| Maximum Sieve size, 2.0 in | AASHTO T 27 | 100% passing |

  - Additional aggregate, conforming to Section 203 of the Specifications and Table 2, may be used if the Contractor determines it is necessary based on the mixture design or other requirements to produce a product which meets the mixture requirements specified in Table 4 and final mix gradation specified in Section IV-1.

| Table 2 Additional Aggregate |  |  |  |
| --- | --- | --- | --- |
| Tests | Method | Limit |
| Los Angeles Abrasion Value | AASHTO T 96 | 45% maximum loss |
| Sand Equivalent | AASHTO T 176 | 45% minimum |
| Maximum size, 100% Passing, Sieve Size | AASHTO T 27 | 2.0 in |
| Water absorption | AASHTO T 85 | 3% maximum |

  - Handling and Storage: Store cement to prevent moisture degradation and partial hydration.  Do not use cement that has become hard, caked, or lumpy.  Store aggregates and RAP so that segregation and inclusion of foreign materials are prevented.  Do not use the bottom 6 inches of aggregate or RAP piles in contact with the ground.

- QUALITY CONTROL PLAN

The Contractor shall develope and implement a Quality Control Plan to ensure that operational techniques and activities provide integral and finished material of acceptable quality. Contractor sampling and testing shall be performed to control the processes and ensure material compliance with the requirements of the Contract.  The Contractor shall provide their Quality Control Plan and JMFs to the District Materials Engineer for approval at least 30 Days before the start of FDR operations.

For each FDR project, the Contractor is required to furnish a project specific Quality Control Plan that shall include, at a minimum, the following information:

  - A description of the Contractor’s Quality Control organization, including the number of full-time equivalent employees or Sub-Contractors with specific Quality Control responsibilities, including an organizational chart showing lines of authority and reporting responsibilities

  - A list of Full Depth Reclamation Technicians  conforming to Section 200.06 of the Specifciations.

  - A Quality Control Sampling, Testing and Analysis Plan with methods that include a description of how random locations for testing and sampling are determined

  - Identification and description of qualifications of the laboratories to be used for each type of testing

  - Specific listing of documentation for Quality Control activities

  - Procedures to meet contract requirements for corrective action when Quality Control criteria are not met

  - Procedures to protect stabilized material from receiving excessive moisture from weather events (e.g.. rain, fog, etc.) and corrective actions when criteria are not met

  - Contingency Plan including but not limited to:

- Inclement weather

- Equipment breakdowns

- Materials shortages

- Excessive fluff - (greater than approximately 10%).  Fluff is defined as the increase in material thickness of the recycled layer over the specified recycling depth due to remixing in place.

- Deficient density of installed FDR

- Material doesn’t break or cure in timely manner

- Gradation is outside tolerances

- Production modifications based on changes in ambient or material temperature.

- Job Mix Formula (JMF)

  - Mixture Designs in the form of a job-mix formula (JMF) shall be submitted to the District Materials Engineer for the Department’s approval at least 30 Days before the start of FDR operations. More than one JMF may be required.  The gradation of each JMF shall fall within the bands shown in Table 3.

| Table 3 Design Range |  |  |
| --- | --- | --- |
| Sieve Size | Percentage by Weight Passing Square Mesh Sieves (in) |  |
|  | Lower | Upper |
| 2.0” | 100 | 100 |
| 3/8” |  | 55 |

The Contractor shall obtain sufficient samples of the material to be reclaimed directly from each roadway within the project for laboratory testing and mix analysis. Samples shall be obtained from every 2500 linear feet, within each lane and to the proposed total recycling depth, with a minimum of six locations for each job mix formula.  Sample locations from each lane may be offset or adjacent from each other.  Additional locations may also be selected based on pavement conditions and variability.

  - Mixture Design Submittal – The designs shall be performed by the Contractor according to these specifications and submitted to the District Materials Engineer for approval 30 working days before the planned start of the work.  The JMF submittal shall include, at a minimum, the following information:

    - Maximum Dry Density at Optimum Moisture Content

    - Percent by weight of all stabilizing agents to be added to the recycled mix

    - Percent water content (at room temperature) required

    - Expansion ratio and half-life characteristics and temperature of asphalt binder at the time of injection into foaming chamber (for mixtures using foamed asphalt)

    - Minimum curing time or set time of the asphalt emulsion for mixtures using asphalt emulsion

    - Temperature of asphalt emulsion at the time of incorporating into the mixture (for mixtures using asphalt emulsion)

    - Target gradation (including any aggregate to be added)

| Table 4 Full-Depth Reclamation JMF Requirements |  |  |
| --- | --- | --- |
| Test | Test Method | Criteria |
| Liquid Limit, Plastic Limit, and Plasticity Index of Soil | VTM-7 | Report |
| Dry Preparation and Mechanical Analysis of Soils, Select Material, Subbase and Aggregate Bases | VTM-25 | Report |
| Classification of Soils | AASHTO M 145 | Report |
| Moisture-Density Relations of Soil-Cement Mixtures | AASHTO T 134 | Report |
| Moisture Density Relations for Bituminous Stabilizing Agents | AASHTO T 180 | Report |
| Compressive Strength of Soil-Cement Cylinders | ASTM D 1633 | 250 - 450 psi at 7 days1 |
| Determining the Strength of Soil-Lime Mixtures (Minimum) | VTM-11 | 150 psi |
| Dry Indirect Tensile Strength (ITS) for Foamed Asphalt Stabilizing Agent (Minimum) | AASHTO T 283, Section 112 | 45 psi |
| Marshall Stability Test for Asphalt Emulsion Stabilizing Agent (Minimum) | ASTM D5581 AASHTO T 2453 | 2500 lbs 1250 lbs |
| 1Three specimens shall be produced and tested for each JMF. The average strength of the specimens shall be within the specified range with no individual specimen having a strength value that varies more than 100 psi from the minimum or maximum value. 2Three specimens shall be produced using either 75 blows per side (per VTM-57) for AASHTO T 245 or 30 gyrations (per AASHTO T 312) for ASTM D5581, compacted at or below Optimum Moisture Content and cured as follows: oven dry at 104ºF (40°C) for 72 hrs and cool to ambient air temperature for 24 hrs. 3 Three specimens shall be produced at 75 blows per side (or 30 gyrations per AASHTO T 312) and cured at 140ºF (60°C) to constant mass, hold specimens at 104ºF (40°C) for 2 hours in a forced draft oven immediately prior to testing. |  |  |

If a change in source materials is made during construction, new JMFs shall be created and approved by the District Materials Engineer prior to use on the project.  The JMFs shall meet the above criteria at the approved stabilizing agents content.

- EQUIPMENT

  - Pulverizing equipment used to reclaim existing pavements shall be capable of pulverizing existing pavement, as well as any additional materials, to meet the gradation provided in the approved JMF, for the widths provided in the Plans, and to the depth specified.

  - Stabilizing equipment shall be capable of incorporating the stabilizing agents at the rate provided in the approved JMF, automatically metering dosage and mixing the full depth and width of pulverized material to a homogenous mixture.

  - Grading equipment shall be capable of working within the constraints of the excavation and grading the full width of stabilized material in conformance with the lines and grades provided in the Plans.

  - Compacting equipment shall be capable of working within the constraints of the excavation and compacting the stabilized material in conformance with the lines and grades provided in the Plans, as well as in conformance with the density requirements provided in the approved JMF.

- TRIAL SECTION

One week before planned start of full production, the Contractor shall stabilize a 2,500-foot long trial section, one lane wide, at the designated thickness and designed optimal stabilizing agents content provided in the approved JMF. Construct the trial section on the project at a location approved by the Engineer .

Construct the trial section using the same construction procedures intended for the entire project.  Cease production after construction of the trial section until the trial section is evaluated and accepted by the Engineer. The trial section shall be considered a lot and payment will follow the payment tables established in this specification.

Should the initial trial section fail, the Contractor shall construct a second trial section on the Project site at a location approved by the Engineer and shall have a Technical Representative present during mixing and placing operations for the second trial section. The Technical Representative shall remain present during mixing and placement of any additional trial sections until acceptance has been made by the Department. In addition, the Technical Representative shall also be present for the next day of production to oversee the mixing and placing operation.  If during the next production day, the materials meet the mixture and placement acceptance criteria, the Technical Representative will no longer be required on the project site.  If additional trial sections beyond the first two are needed, the Contractor shall construct the trial section at sites approved by the Engineer.

The Technical Representative shall meet the following criteria:

- Have 2 years minimum experience with the FDR process

- Have personally supervised a minimum of 5 successful FDR projects

- Have personal experience in developing FDR mix designs

- Have the experience to perform and supervise field process control testing

- Submit a list of references, with current telephone numbers, of persons who are able to verify the experience required herein

The Technical Representative does not have to be an employee of the Contractor.

- CONSTRUCTION METHODS

  - Grass and Other Vegetation shall be removed from the edge of the existing pavement to prevent contamination of the pulverized bituminous material during the milling operation.

  - FDR shall be performed to the depth provided in the Plans, while incorporating stabilizing agents, mineral filler, additional aggregate and water.  Mixing shall continue until a homogenous mixture of the above materials and pulverized materials is achieved.  As needed, the speed of the recycling unit shall be adjusted to ensure a homogenous mixture,

    - Pre-cutting, grading and light compaction of the recycled material shall be performed prior to incorporation of the stabilizing agent.

    - The application rate of all stabilizing agents shall be continuously monitored using calibrated, automatic meters. The application rate shall be within 0.20 percentage points of the optimal stabilizing agents content provided in the approved JMF. If the measured application rate falls outside the above tolerance, then the recycling operations shall be stopped and corrected before proceeding.

    - The water content of the stabilized material shall be monitored closely to ensure conformance with the approved JMF ± 2 percentage points of optimum and to ensure proper compaction.

    - Longitudinal joints between adjacent stabilization passes shall be overlapped by at least 4 inches.  Transverse joints created by the recycling process shall be saw-cut, if necessary, to provide a vertical, clean face to ensure proper compaction.

  - Final Grading and Compacting shall be performed within the constraints of the excavation and the stabilized material shall be compacted in conformity with the lines and grades provided in the Plans. Compaction shall progress across the full width of the stabilized area until the established target density is achieved.

    - Once the entire working width (full lane width plus affected shoulder width) has been stabilized, and only after primary compaction has been completed, the entire working width shall be graded to the required profile and cross-slope. Disturbance to the stabilized and primarily compacted material shall be kept to a minimum during this grading and shaping operation.

    - Any additional water required to achieve the established target density shall be applied by spraying the surface of the stabilized material with light applications.  Care shall be taken not to over-apply additional water to any areas of stabilized material.

  - Surfacing: The surface of the compacted material shall be kept moist until covered with an asphalt-based layer in the case of cement stabilized materials.  For bituminous stabilized materials, the FDR shall be allowed to cure until the moisture of the material is a maximum of 50% the optimum moisture content or until approval of the Engineer is received.  Subsequent asphalt-based layers can be placed any time after finishing, as long as the FDR is sufficiently able to support the required construction equipment without marring or permanent distortion of the surface.

- ACCEPTANCE TESTING

  - Density shall be determined with a nuclear gauge operating in direct transmission mode conforming to VTM 10 to the full depth of the FDR layer.  The Contractor shall have had the gauge calibrated within the previous 12 months by an approved calibration service.  The Contractor shall maintain documentation of such calibration service for the 12-month period from the date of the calibration service.

The project will be divided into lots by the Engineer for the purpose of defining areas represented by each series of tests.

  - Lot: For the purposes of acceptance, each day’s production shall be considered a lot unless the paving length is less than 3,000 linear feet or greater than 7,500 linear feet.  When paving is less than 3,000 feet, it shall be combined with the previous day’s production or added to the next day’s production to create a lot as described below.

For the purposes of acceptance, the standard size of a lot shall be 5,000 linear feet, with 1,000 foot sublots, including the full width of the lane (including any affected shoulder width).  If the Engineer approves, the lot size may be increased to 7,500 linear foot lots with five 1,500 foot sublots when the Contractor’s normal daily production exceeds 7,500 feet.  When a partial lot occurs at the end of a day’s production or upon completion of the project, the lot shall be either  added to the previous lot if the partial lot contains one or two complete sublots, or redefined to be an entire lot if the partial lot contains three or four complete sublots.

Each lot shall be tested for density by taking a nuclear density reading from two stratified-random test sites selected by the Engineer within each sublot.  Test sites shall not be located within 18 inches of any longitudinal joint.

The average of the sublot density measurements will be compared to the maximum density from the approved JMF to determine the acceptability of the lot.  Once the average density of the lot has been determined, the Contractor will not be permitted to provide additional compaction to raise the average.  If two consecutive sublots produce density results less than 97.0 percent of the target density, the Contractor shall immediately notify the Engineer and institute corrective action.  By the end of the day’s operations, the Contractor shall furnish the test data developed during the day’s production to the Engineer.

Payment will be made according to Table 5.

| Table 5 Payment Schedule For Lot Densities |  |
| --- | --- |
| % of Density from Approved JMF | % of Payment |
| 97.0 or greater | 100 |
| 96.0 to less than 97.0 | 95 |
| 95.0 to less than 96.0 | 90 |
| Less than 95.0 | 75 |

  - Depth Check – Depth checks shall be performed by the Contractor in accordance with VTM 38, Method B twice per lot after compaction and prior to the placement of the next pavement layer.

Acceptance testing of FDR for depth for each lot will be based on the mean result of measurements of samples taken from that lot of material placed.

A lot will be considered acceptable for depth if the mean result of the tests is within the tolerance of the plan depth for the number of tests taken as shown in Table 6.

| Table 6 Process Tolerance for Depth Checks |  |  |  |  |
| --- | --- | --- | --- | --- |
| Plan Depth, inches | Tolerance, inches (Plus or Minus) |  |  |  |
|  | 1 test | 2 tests | 3 tests | 4 tests |
| >6 ≤ 8 | 0.9 | 0.65 | 0.5 | 0.4 |
| >8 ≤ 12 | 1 | 0.9 | 0.7 | 0.5 |
| >12 | 1.2 | 1 | 0.8 | 0.6 |

If an individual depth test is in excess of the tolerance for one test, that portion of the lot represented by that test will be excluded from the lot. If an individual test result indicates that the depth of material represented by the test is more than the tolerance for one test, the Contractor will not be paid for that amount of material in excess of the tolerance throughout the length and width represented by the test. The Department may require excessive material to be removed at the Contractor’s expense. If an individual test result indicates that the depth of the material represented by the test is deficient by more than the tolerance for one test, correction of the base course represented by that test shall be made by the Contractor as specified hereinafter.

If the mean depth of a lot of material is less than the allowable tolerance, correction will be required and the Contractor will be paid for the quantity of material that has been placed in the lot. The Contractor will be required to furnish and place material specified for the subsequent course to bring the deficient FDR course depth within the tolerance. This additional material will be placed at the Contractor’s expense.

  - Gradation shall be checked twice per day.

  - Stabilizing Agent Dosage Rate shall be verified at the start of a day’s production and twice per 1,000 linear feet . If using a dry stabilizing agent, the dosage rate shall be determined in accordance with VTM 141. The dosage rate shall be within 0.20 percentage points of the approved JMF. If the dosage rate is beyond this tolerance, then paving shall stop and the Contractor shall take corrective measures.

If testing of 2,000 linear feet meets the dosage rate within 0.20 percentage points of the approved JMF, the Engineer may reduce the frequency of testing to 1 test per 1,000 feet. However, if the dosage rate is beyond the tolerance at any time during an approved reduced frequency, testing shall resume at a rate of twice per 1,000 linear feet. The Engineer reserves the right to require verification of the dosage rate by the Contractor at any time.

  - Construction Records: The Contractor shall prepare separate test reports meeting the requirements of AASHTO R 18 or may use the current appropriate VDOT forms. Records documenting the dosage rate of stabilizing agents and other test results from Table 4 shall be provided to the Engineer, unless specified otherwise.

- WEATHER LIMITATIONS

Recycling operations shall be completed when both the atmospheric temperature and material to be processed (measured in the shade and away from artificial heat) is at least 40°F when cement stabilizing agent is used or 50°F when foamed asphalt or emulsion is used. Recycling operations shall not begin when the weather forecast calls for freezing temperature within 48 hours after placement of any portion of the project.

- MEASUREMENT AND PAYMENT

Full Depth Recycling (FDR) will be measured in square yards of the completed sections for the depth specified in the Plans and paid for at the Contract square yard price. This price shall be full compensation for removal and processing of the existing pavement; for preparing, hauling, and placing all materials; furnishing additives (not including stabilizing agents); for all freight involved; for all manipulations, including removal of grass and other vegetation; rolling and brooming; testing and documentation; stabilizing agent supplier services; and for all labor, tools, equipment and incidentals necessary to complete the work.

Stabilizing agents will be paid as follows:

Liquid Asphalt (Emulsion) will be measured in tons and paid for at the Contract ton price. This price shall be full compensation for furnishing and incorporating the emulsion into the mixture. An emulsion content of 3.0% by weight of the reclaimed material shall be used for bidding purposes prior to the completed design. The actual emulsion content will be adjusted based on the quantity necessary to meet the design requirements in Table 4.

Liquid Asphalt (foamed) will be measured in tons and paid for at the Contract ton price.  This price shall be full compensation for furnishing and incorporating the foamed asphalt into the mixture. A foamed asphalt content of 2.5% by weight of the reclaimed material shall be used for bidding purposes prior to the completed job mix formula. The actual foamed asphalt content will be adjusted based on the quantity necessary to meet the design requirements in Table 4.

Hydraulic Cement will be measured in tons and paid for at the Contract ton price. This price shall be full compensation for furnishing and incorporating the hydraulic cement into the mixture. A cement content of 5.0% by weight of the reclaimed material shall be used for bidding purposes prior to the completed design. The actual cement content will be adjusted based on the quantity necessary to meet the design requirements in Table 4.

Lime will be measured in tons and paid for at the Contract ton price. This price shall be full compensation for furnishing and incorporating the lime into the mixture. A lime content of 5.0% by weight of the reclaimed material shall be used for bidding purposes prior to the completed design. The actual lime content will be adjusted based on the quantity necessary to meet the design requirements in Table 4.

Other Cementitious Material will be measured in tons and paid for at the Contract ton price. This price shall be full compensation for furnishing and incorporating the cementitious material into the mixture. A cementitious content of 5.0% by weight of the reclaimed material shall be used for bidding purposes prior to the completed design. The actual cementitious content will be adjusted based on the quantity necessary to meet the design requirements in Table 4.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Full-Depth Reclamation (Depth) | Square Yard |
| Liquid Asphalt (Emulsion) | Ton |
| Liquid Asphalt (Foamed) | Ton |
| Hydraulic Cement | Ton |
| Lime | Ton |
| Other Cementitious Materials | Ton |

Additional Crushed RAP if required to meet the contract requirements will be measured in tons and paid for at $ fill in amount per ton per ton. This price shall be full compensation for furnishing and incorporating the additional RAP into the mixture. The additional RAP shall conform to Section II-4 for payment purposes.

Additional Aggregate, if required, according to the JMF and other Contract requirements, will be measured in tons and paid for at $ fill in amount per ton per ton.  This price shall be full compensation for furnishing and incorporating the additional aggregate material into the mixture.  The additional aggregate material shall conform to Section II-5 for payment purposes.