GUIDELINES — Use when requested by the District Materials Engineer.  When this provision applies include the following in the proposal:{2007-S315V01}

SP315-DB0160-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

BM-25.0D WITH INCREASED ASPHALT CONTENT

November 14, 2018

I.	DESCRIPTION

The work described in this special provision is specifically intended for supplying, testing and installing asphalt concrete base with additional asphalt cement.  BM-25.0D+0.4 and/or BM-25.0D+0.8 shall be placed at locations identified in the Contract.

II.	MATERIALS

The Design-Builder shall furnish, test and install BM-25.0D with additional asphalt cement content according to this special provision.  The mix(es) shall conform to all of the requirements of a standard BM-25.0D in Section 211 of the Specifications except as noted herein.

Construction and Acceptance of one or more courses of asphalt concrete consisting of BM-25.0D+0.4 or BM-25.0D+0.8 asphalt concrete base shall be according to BM-25.0D in Section 315 of the Specifications and the density specified in Table 5 herein.

An equivalent single axle load (ESAL) will be established by the Engineer and the mix types may be specified as one of the types listed in Table 1 herein.

| TABLE 1 |  |  |  |
| --- | --- | --- | --- |
| Mix Type | Equivalent Single Axle Load (ESAL)Range (millions) | Final Asphalt Performance Grade (PG) | Aggregate Nominal Maximum Size* |
| BM-25.0D+0.4 | All ranges | 64H-16 | 1” |
| BM-25.0D+0.8 | All ranges | 64H-16 | 1” |
| Asphalt concrete shall conform to the requirements for the type designated. *Nominal Maximum Size is defined as one sieve size larger than the first sieve to retain more than 10 percent aggregate. |  |  |  |

Job-Mix Formulas

To determine the AC content for the BM-25.0D plus additional asphalt cement, an approved BM-25.0D per Section 211 will be used to determine the optimum AC content and aggregate gradations.  While the optimum AC content for the BM-25.0D will be selected at 2.5 percent per Section 211, the initial AC content for the BM-25.0D+0.4 and/or BM-25.0D+0.8 will be selected using the 3.5 percent air voids for the BM-25.0D.  The additional asphalt cement (0.4% or 0.8%) will be added to the initial AC content at 3.5 percent air voids in order to establish the design AC content.

During production the BM-25.0D+0.4 and BM-25.0D+0.8 mixes shall be controlled according to Table 2 herein.

| TABLE 2 PRODUCTION CRITERIA |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mix Type | VTM Production (%) | VFA (%) | Min. VMA (%) | Fines/Asphalt Ratio | Number of Gyrations |  |
|  |  |  |  |  | N Design | N Initial |
| BM-25.0D+0.4 | 1.0 – 4.0 | 67 – 92 | 12.0 | 0.6 – 1.3 | 65 | 7 |
| BM-25.0D+0.8 | 0.5 – 3.5 | 67 – 92 | 12.0 | 0.6 – 1. 3 | 65 | 7 |

1.	The Laboratory mixing temperature shall be 310 oF to 320 oF and the compaction temperature shall be 295 oF to 300 oF for both testing and design.

2.	Field correction factor.  The field correction factor is determined by subtracting the bulk specific gravity of the aggregate from the effective specific gravity of the aggregate determined at the JMF AC content achieved.

| TABLE 3 RECOMMENDED PERFORMANCE GRADE OF ASPHALT |  |  |
| --- | --- | --- |
|  | Percentage of Reclaimed Asphalt Pavement (RAP) in Mix |  |
| Mix Type | %RAP < 25.0 | 35.0 ≥ %RAP ≥ 25.0 |
| BM-25.0D (+0.4 and +0.8) | PG 64H-22 | PG 64S-22 |

III.	TESTING

When asphalt cement is extracted and recovered according to AASHTO T170, the recovered asphalt cement shall meet the required grade specified in Table 1 herein.

IV.	ACCEPTANCE AND ADJUSTMENTS

Acceptance shall be in accordance with the requirements for BM-25.0D in Section 211.08 of the Specifications.  If the material does not meet the applicable requirements, the Engineer may elect to accept the material at a reduced price, an extended warranty, or both in accordance with Part 5 Section 105.18.

V.	DENSITY

Density shall be determined in accordance with Section 315.05(e) of the Specifications.  The minimum density requirements for BM-25.0D+0.4 and BM-25.0D+0.8 shall be as specified in Table 4 herein. If the density testing results do not meet the applicable requirements, the Engineer may elect to accept the material at a reduced price, an extended warranty, or both in accordance with Part 5 Section 105.18.

| T A B L E 4 |  |
| --- | --- |
| DENSITY REQUIREMENTS |  |
| Mixture Type | Minimum Control Strip Density (%)¹ |
| BM-25.0D+0.4 | 94.0 |
| BM-25.0D+0.8 | 96.0 |
| ¹ The control strip density requirement is the percentage of theoretical maximum density of the job mix formula by SUPERPAVE® mix design or as established by the Engineer based on two or more production maximum theoretical density tests. |  |