GUIDELINES – Use when requested by the Designer for asphalt projects. {2007-S315AC0}

SP315-DB0410-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

Cold In-Place Recycling (CIR)

December 19, 2018

- DESCRIPTION

Cold In-place Recycling (CIR) is defined as a process in which a portion of existing asphalt concrete pavement layers are pulverized, stabilized, and repaved in place. This is most commonly performed using foamed asphalt or emulsified asphalt as the primary stabilizing additive. The Design-Builder shall select the final mix design (job mix formula- JMF) and construction methods to meet the performance requirements specified herein. The pavement may be milled, stabilized, and repaved using the same machine or machine train, or paved from a stabilized, windrowed material using traditional practices.

- MATERIALS

- Stabilizing agent (Emulsified or Foamed Asphalt) – All liquid asphalts used as recycling agents shall be emulsions and PG binders (Lists Nos. 50 and 50.1) on the VDOT Materials Division’s Approved List. Emulsified asphalts shall conform to Section 210 of the Specifications; liquid asphalts shall be a neat (i.e. not modified) asphalt that meets the requirements of Section 211.02 of the Specifications. Emulsion shall not be used for night-time work.

- Water – Any water used for mixing shall meet the requirements of Section 216 of the Specifications.

- CIR – The CIR material shall meet the gradation requirements in TABLE 3 in this special provision.

- Other Additives – If necessary, additional additives may be used to meet the requirements in TABLE 4 in this special provision. In the case where an additional additive is used, the type and dosage must be described in the Job Mix Formulae submitted to the Department.

- Addition of Crushed Reclaimed Asphalt Pavement (RAP) Material – Additional RAP material (other than that reclaimed from the project) may be added by the Design-Builder and, if added, shall meet the requirements of Section 211.02(j) of the Specifications and TABLE 1 herein.

| TABLE 1 – ADDITIONAL CRUSHED RAP |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Deleterious Materials: Clay Lumps and Friable Particles in Aggregate | AASHTO T 112 | 0.2% maximum |
| Maximum Sieve Size, 1.5 inches (37mm) | AASHTO T 27 | 100% Passing, |

- Additional aggregate – Based on the results of the job mixture designs or other requirements of this provision, the Design-Builder shall determine if additional aggregate is required. If the Design-Builder determines additional aggregate is needed, any additional aggregate shall meet the requirements of Section 203 of the Specifications and TABLE 2 herein, and it shall be graded to produce a product that meets the requirements of TABLE 3 in this special provision.

| TABLE 2 – ADDITIONAL AGGREGATE |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Los Angeles Abrasion Value | AASHTO T 96 | 45% maximum loss |
| Sand Equivalent | AASHTO T 176 | 45% minimum |
| Maximum size, 100% Passing, Sieve Size | AASHTO T 27 | 1.5 inches (37mm) |
| Water absorption | AASHTO T 85 | 3% maximum |

- QUALITY CONTROL PLAN

The Design-Builder shall develop and implement a CIR Quality Control Plan to ensure that operational techniques and activities under their control provide a homogeneous and finished material of acceptable quality. Design-Builder sampling and testing shall be performed to control the processes and ensure material compliance with the requirements of this special provision. The Design-Builder shall provide their Quality Control Plan (in accordance with this special provision) and the Job Mix Formulae they intend to accomplish the work to the District Materials Engineer for approval no less than thirty (30) calendar days prior to the start of CIR operations.

For each CIR project, a project specific CIR Quality Control Plan is required, and shall include the following (minimum) information:

  - A description of the Design-Builder’s Quality Control organization, including the number of full-time equivalent employees or Sub-Contractors with specific Quality Control responsibilities, including an organizational chart showing lines of authority and reporting responsibilities.

  - A listing by discipline with the name, qualifications, duties, responsibilities and authorities for all persons proposed to be responsible for Construction Quality Control.

  - A Quality Control Sampling, Testing and Analysis Plan with methods that include a description of how random locations for testing and sampling are determined.

  - Identification and description (Accreditation) of the laboratories to be used for each type of testing.

  - Specific list of documentation for Quality Control activities.

  - Procedures to meet contract requirements for corrective action when QC criteria are not met.

  - Procedures to protect stabilized material from receiving excessive moisture from weather events (i.e. rain, fog, etc.) and corrective actions when criteria are not met.

  - Contingency Plan including:

- Inclement weather

- Equipment breakdowns

- Materials shortages

- Excessive fluff - (greater than approximately 10 percent). Fluff is defined as the increase in material thickness of the recycled layer over the specified recycling depth due to remixing in place.

- Deficient density of installed CIR

- Material doesn’t break or cure in timely manner, as established by the job-mix design

- Gradation is outside tolerances

- Production modifications based on changes in ambient and/or material temperature

The Design-Builder is required to have a technical representative at the project site during mixing and placement operations. At a minimum, this person must:

●	Have 2 years minimum experience with the CIR process

●	Have personally supervised a minimum of 5 successful CIR projects

●	Have personal experience in developing CIR mix designs

●	Have the experience to perform and supervise field process control testing

●	Submit a list of references, with current telephone numbers, of persons who are able to verify the experience required herein

The Design-Builder may use consultants or manufacturers’ representatives to satisfy the technical representative requirements of this section provided these individuals meet the requirements listed above and are on-site at all times construction operations are being performed.

- Job Mix Formula

Mixture Designs – CIR mix designs in the form of a job-mix formulae (JMF’s) shall be submitted to the Engineer for approval no less than 30 calendar days prior to the start of CIR operations More than one JMF may be required. The gradation of each JMF shall fall within the bands shown in TABLE 3 herein. The Design-Builder’s contingency plan should address actions to be taken if gradation fails to meet the requirements The Department at its discretion reserves the right to require appropriate measures that may include stopping the work.

TABLE 3 – DESIGN RANGE

| Sieve Size | Gradation Band* (Percent Passing) |  |
| --- | --- | --- |
|  | Lower | Upper |
| 1.5” | 100 | 100 |
| 3/8” | -- | 55 |

*based on pulverized materials, prior to stabilization, washed, following AASHTO T 27

The JMF’s shall be created using existing materials obtained directly from the project site prior to the start of construction. Sampling shall be conducted at a minimum of once per 2500 lane-feet. Each JMF shall provide, as a minimum, the following mix design parameters:

  - Target field density

  - Percent by weight of all stabilizing agents to be added to the recycled mix

  - Percent by weight of water (at room temperature) required

  - Expansion ratio and half-life characteristics and temperature of asphalt binder at the time of dosage into foaming chamber (for mixtures using foamed asphalt)

  - Minimum curing time/cure time for the emulsified asphalt

  - Temperature of emulsified asphalt at the time of dosage into the mixture (for mixtures using emulsified asphalt)

  - Target gradation (including any aggregate to be added).

If a change in source materials is made during construction, new JMF’s shall be created, submitted to the Engineer, and approved prior to use on the project.

The JMF’s shall meet the criteria of TABLE 4 herein at the approved stabilizing agents’ content.

| TABLE 4 – CIR MIX DESIGN REQUIREMENTS |  |  |  |
| --- | --- | --- | --- |
| Item | Test Method | Criteria | Fabrication / Conditioning Procedure |
| Emulsified Asphalt Stabilized Materials |  |  |  |
| 1 | Moisture Density Relations AASHTO T 180, Method D | Determined by Design; Used to Establish Target Field Density |  |
| 2 | Marshall Stability Test ASTM 5581 (6 in. specimens), AASHTO T 245 (4 in. specimens) | 2500 lbs. minimum (6 in. (150mm) diameter specimen), or 1250 lbs. minimum (4 in. (100mm) diameter specimen) | Three specimens shall be produced at 75 blows per side (or 30 gyrations per AASHTO T 312) and cured at 140ºF (60°C) to constant mass, hold specimens at 104ºF (40°C) for 2 hours in a forced draft oven immediately prior to testing. |
| 3 | Retained Stability ASTM 5581 (6 in. specimens), AASHTO T 245 (4 in. specimens) | Minimum 70% of results of #2 | An additional three specimens shall be produced at cured at 140ºF (60°C) to constant mass. Specimens shall then be vacuum saturated to 55-65% moisture content, 77ºF (25°C) water bath for 23 hours and 104ºF (40°C) water bath for an additional hour immediately prior to testing |
| 4 | Raveling Stability (ASTM D 7196) | Maximum 2% | Specimens shall be produced using a gyratory at 20 gyrations and cured at 50ºF (10°C) for 4 hours at 50% humidity. |
| 5* | Thermal Cracking (Indirect Tensile Test, AASHTO T 322) | The critical cracking temperature must be less than or equal to the pavement temperature given for the project climate area and pavement depth by LTPPBind1. | See Notes 1 through 7 below. |
| Foamed Asphalt Stabilized Materials |  |  |  |
| 1 | Moisture Density Relations AASHTO T 180, Method D | Determined by Design; Used to Establish Target Field Density |  |
| 2 | Dry Indirect Tensile Strength (ITS), AASHTO T 283 Section 11 | 45 psi minimum | Three specimens shall be produced using 75 blows per side (or 30 gyrations per AASHTO T 312) compacted at or below OMC and cured as follows: 4 inch (100 mm) diameter specimens, oven dry at 104ºF (40°C) for 72 hrs and cool to ambient temperature for 24 hrs; 6 inch (150 mm) diameter specimens, air dried for 24 hours, then an additional 48 hours at 104ºF (40ºC) in sealed plastic bag, cool to ambient temperature for 24 hrs. |
| 3 | Retained Indirect Tensile Strength, AASHTO T 283 Section 11 | Minimum, 70% of the Dry ITS from Item 9 | An additional three specimens shall be produced and cured according to Item 9, and then submerged in 77ºF (25ºC) water bath for 24 hours prior to testing. |
| 4 | Expansion Ratio. Wirtgen 2012 Cold Recycling Manual | 10 times when Aggregate Temperature is 50ºF to 77ºF (10ºC to 25ºC) 8 times when Aggregate Temperature is greater than 77ºF (25ºC) |  |
| 5 | Half-Life – Wirtgen 2012 Cold Recycling Manual | 6 second minimum |  |
| All materials (emulsified asphalt and foamed asphalt) shall be controlled following Item 1. |  |  |  |
| 1 | Materials Gradation Test (AASHTO T 27), prior to stabilization | Gradation to control field production. |  |
| Notes: 1. Specification temperature shall be chosen using current FHWA LTPPBind software, using the weather station closest to the project. The required temperature shall be the coldest temperature at the top of the recycled layer, using 98% reliability. 2. Samples shall be compacted to 150 mm (6 in.) diameter and at least 115 mm height, compacted to within 1% of design air voids at the design stabilizing agent content. Compacted samples shall be cured at 140ºF (60ºC) no less than 48 hours. Before testing, sample mass shall be checked every two hours until change in mass between successive checks does not exceed 0.05%. After curing, two specimens shall be saw-cut from each compacted sample to 50 mm (2 in.) in height. Perform bulk density testing after saw-cutting. 3. Three specimens are required at each of the three testing temperatures. 4. Select two testing temperatures that bracket the specification temperature above. For example, if the specification temperature is -13ºF (-25ºC), then two of the selected testing temperatures shall be -4ºF and -22ºF (-20ºC and -30ºC). A temperature of 14ºF or -40ºF (-10ºC or -40ºC) shall be used as the third testing temperature. 5. The tensile strength test shall be performed on each specimen directly after the tensile creep test (at the same temperature as the creep test). 6. The critical cracking temperature is defined as the temperature at the intersection of the thermal stress curve (derived from the creep data) and the tensile strength line (the line connecting the average tensile strengths at the three testing temperatures). 7. To meet this specification, the critical cracking temperature predicted by the Indirect Tensile Test must be less than or equal to the pavement temperature given for the project climate area and pavement depth by LTPPBind. |  |  |  |

- EQUIPMENT

- CIR – The CIR work shall be completed with a self-propelled machine with a down cutting milling head that is capable of pulverizing and recycling the existing asphalt concrete pavement to a maximum depth of 6 inches, uniformly incorporating the stabilizing agent(s) and water, and mixing the materials to produce a homogeneous product. The machine shall be capable of pulverizing and recycling the full lane width in no more than two passes (with the longitudinal joint located between the anticipated wheel paths). The machine shall have the ability to meter dosage rates for stabilizing agent(s) and water relative to the machine’s ground speed. Individual valves on the spray bar shall be capable of being turned off as necessary to minimize stabilizing agent(s) and water overlap on subsequent passes. The equipment shall be operated according to the manufacturers’ recommendations.

The self-propelled machine may also have a screed attached to the milling and mixing unit. The screed shall have slope control and the ability to convey material out to the side of the screed if there is a surge of material between the mixing chamber and the screed. The mixing unit and screed combination must have electronic grade controls. In lieu of a screed attachment, the material may be placed into an asphalt paver that meets the requirements of Section 315.03(b) of the Specifications by means of a material transfer device.

Any additives such as water, lime slurry, etc. added by the equipment at the milling head or mixing unit shall be controlled through liquid metering devices capable of automatically adjusting for the variation in bituminous material going into the mixing unit, by means of weighing device or proportional control systems.

The metering devices shall be capable of delivering the amount of additive to within +/- 0.2 percent of the required amount, except that a capability of adding up to 5 percent water by weight of the pulverized bituminous material is mandatory. The Department will not require metering of the water added at the milling machine to control dust in the screens, belts, or crusher/material sizing unit.

A pozzolonic material distributor truck shall be used if dry stabilizing agents is/are applied directly to the asphalt concrete pavement prior to CIR operations. The pozzolonic material distributor truck shall have the ability to uniformly apply the stabilizing agent(s) at the specified rate.

- Rollers – All rollers shall be self-propelled. At least one pneumatic tire roller shall have a minimum gross operating weight of not less than 50,000 lbs. At least one double steel-wheeled vibratory roller shall have a gross operating weight of not less than 24,000 lbs. and a width of 78 inches. All rollers must have properly working scrapers and water spraying systems.

- Test Strip

Before planned start of full production, stabilize a 2,500 foot long test strip, one-lane wide, at the designated thickness and designed optimal stabilizing agent(s) content provided in the approved job mix design. Construct the test strip on the project at an approved location, using construction procedures intended for the entire project. Cease production after construction of the test strip until the test strip is evaluated and accepted. Test strip acceptance will be determined according to Section VII below. The test strip shall be considered a lot.

- CONSTRUCTION METHODS

  - Grass and other vegetation shall be removed from the edge of the existing pavement to prevent contamination of the pulverized asphalt concrete material during the milling operation.

  - The existing asphalt concrete pavement shall be milled to the required depth and width as indicated on the plans. Recycling shall be performed in a manner that minimizes disturbance of the underlying material in the existing roadway. The milling operation shall be conducted so that the amount of fines occurring along the vertical faces of the cut shall not prevent bonding of the CIR materials. If needed, the CIR materials shall be processed by crushing or sizing to the required gradation specified in TABLE 3 in this special provision. When a paving fabric is encountered during the CIR operation, the Design-Builder shall make the necessary adjustments in equipment or operations so that at least ninety percent (90 percent) of the shredded fabric in the recycled material is no more than the particle size specified in TABLE 3 herein. These changes may include, but shall not be limited to: adjusting the forward machine speed, milling rate, the milling depth, and/or adding or removing screens in order to obtain the specified recycled material. The Design-Builder will be required to waste material containing over-sized pieces of paving fabric as directed by the Engineer.

  - Adjacent CIR passes shall overlap by a minimum 4 inches. The stabilizing agent shall be controlled such that it is not applied at the joint overlap location more than the dosage rate in the approved mix design by the total of the passes.

  - Compaction of the recycled mix shall be completed using rollers meeting the requirements of Section V-2 herein. The Design-Builder shall establish rolling patterns to achieve the density target as determined by nuclear density testing. Final rolling to eliminate pneumatic tire marks and to achieve density shall be done by double drum steel roller(s), either operating in a static, oscillating or vibratory mode. Oscillating and vibratory mode should only be used if it is shown to not damage the pavement. Rolling shall be performed until the material reaches a density of 98 percent the maximum theoretical density as measured via a nuclear density gauge. Rolling shall start no more than 30 minutes after initiation of paving. Finish rolling shall be completed no more than one hour after paving is completed, unless otherwise approved by the Engineer. When possible, rolling shall not be started or stopped on uncompacted material but performed with rolling patterns established so that they begin or end on previously compacted material or the existing pavement.

  - After compaction of the recycled material, a fog seal shall be applied to the recycled surface at a uniform application rate of 0.06 gal/sy (0.04 gal/sy residual). The fog seal shall be a CSS-1h, CQS-1h, or Non-Tracking Tack Coat conforming to Section 310 of the Specifications. A light grit conforming to Section 202 of the Specifications, Grading A, shall be applied to reduce raveling. After fog sealing, no traffic, including the Design-Builder’s equipment, will be permitted on the completed recycled material until the water content of the CIR material is a maximum of 50 percent of the optimum water content according to paragraph 7 below. After this “curing” period, rolling traffic may be permitted on the recycled material. This time may be adjusted by the Quality Assurance Manager or Engineer to allow establishment of sufficient cure so traffic will not initiate raveling. After opening to traffic, the surface of the recycled pavement shall be maintained in a condition suitable for the safe movement of traffic. All loose particles that may develop on the pavement surface shall be removed without damaging the surface.

  - Any damage to the completed CIR material, such as raveling or other surface imperfections shall be repaired by the Design-Builder to the Engineer’s satisfaction in accordance with Part 5 Section 105.18 requirements, prior to the placement of the asphalt concrete surface course(s), or other applicable surface treatment.

  - Before placing the asphalt concrete surface courses, or other applicable surface treatment, the CIR material shall be allowed to cure until the moisture of the material is a maximum of 50 percent of the optimum water content or until approval of the Engineer is received. Moisture content shall be measured per AASHTO T 329 on samples taken from two stratified random locations and immediately placed in a sealed plastic bag, as determined by the Quality Assurance Manager or Engineer for each lot. Other methods and sampling rates may be used if supplied in the Design-Builder’s Quality Control Plan and approved by the Engineer. Split samples may be taken at the direction of the Engineer. A tack coat, according to Section 310 of the Specifications for Non-tracking Tack Coat, shall be applied prior to any additional asphalt layers.

- ACCEPTANCE TESTING

  - Field Compaction – A nuclear density gauge conforming to the requirements of VTM-10 shall be used for determining mat density by the Direct Transmission method. The Design-Builder’s nuclear density gauge shall have been calibrated within the previous 12 months by an approved calibration service. In addition, the Design-Builder shall maintain documentation of such calibration service for the 12-month period from the date of the calibration service and furnish the same to the Quality Assurance Manager or Engineer. The Design-Builder shall determine a roller pattern and construct a control strip according to VTM 10. Density test locations shall be marked and labeled by the Design-Builder according to VTM-76. The control strip will be acceptable if the field proctor (AASHTO T 180, Method D) is at least 98 percent of the target density from the approved job mix designs. The required density of the compacted CIR course shall not be less than 98.0 percent of the target density from the approved job mix designs.

  - Test section (lot) – For the purposes of acceptance, each day’s production will be considered a lot unless the paving length is less than 3,000 linear feet or greater than 7,500 linear feet. When paving is less than 3,000 feet, it shall be combined with the previous day’s production or added to the next day’s production to create a lot as described below.

The standard size of a lot shall be 5,000 linear feet, with 1,000 linear foot sublots, of any pass 6 feet or greater made by the paving train for the thickness of the course. If the Engineer approves, the lot size may be increased to 7,500 linear foot lots with five 1,500 foot sublots when the Design-Builder’s normal daily production exceeds 7,500 feet. When a partial lot occurs at the end of a day’s production or upon completion of the project, the lot shall be either added to the previous lot if the partial lot contains one or two complete sublots or redefined to be an entire lot if the partial lot contains three or four complete sublots.

Each lot shall be tested for density by taking a nuclear density reading from two random test sites selected by the Quality Assurance Manager within each sublot used for acceptance. Test sites shall not be located within 18 inches of the edge of any application width for CIR mixes.

The average of the sublot density measurements will be compared to the target nuclear density established by the approved mix design to determine the acceptability of the lot. Once the average density of the lot has been determined, the Design-Builder will not be permitted to provide additional compaction to raise the average. If two consecutive sublots produce density results less than 98 percent of the target density, the Design-Builder shall immediately notify the Engineer and institute corrective action. By the end of the day’s operations, the Design-Builder shall furnish the test data developed during the day’s recycling to the Engineer. The Design-Builder shall verify their results for every lot by performing a field proctor (AASHTO T180, Method D). The field proctor shall be at least 98 percent of the target density from the approved mix design. If the density results are less than 98.0%, but more than 96%, of the maximum theoretical density from the approved job mix design, the Engineer may elect to accept the Work at a reduced price, an extended warranty, or both in accordace with Part 5 Section 105.18. The tonnage or square yards of each lot will be based on the lot’s width and length and the mixture application rate as designated in the Plans or as revised by the Design-Builder Design Manager.

  - Gradation – For CIR, the Design-Builder shall verify that the unstabilized gradation conforms to the JMF at the beginning of each production day and wherever there are changes in the pavement structure being recycled. Gradation bands shall be established for the day by operating the machine at two distinct forward speeds and sampling the associated unstabilized material for field gradation testing.

  - Depth Check – Depth checks shall be performed by the Design-Builder according to VTM-38, Method B at a minimum rate of twice per 5,000 linear feet after compaction. Depth checks shall be taken at the Quality Assurance Manager’s direction. In the event that a slit trench cannot be created according to VTM-38, Method B, the Design-Builder may remove the CIR materials by use of a core rig and depth measurements taken according to VTM-38, Method B.

Acceptance of CIR course for depth will be based on the mean result of measurements of samples taken from each lot of material placed.

A lot will be considered acceptable for depth if the mean result of the tests is within the tolerance of the plan depth for the number of tests taken as shown in TABLE 5 herein.

| TABLE 5 – PROCESS TOLERANCE FOR DEPTH CHECKS |  |  |  |
| --- | --- | --- | --- |
| Plan Depth, inches | Tolerance, inches (Plus or Minus) |  |  |
|  | 2 tests | 3 tests | 4 tests |
| ≤ 4 | 0.45 | 0.35 | 0.30 |
| >4 ≤ 6 | 0.65 | 0.50 | 0.40 |

If the mean depth of a lot of material is in excess of the tolerance, the Engineer can require excessive material to be removed. If the mean depth of a lot of material is deficient by more than the allowable tolerance for the plan depth specified, correction will be required. For sections of CIR course that are deficient in depth beyond the tolerance, the Design-Builder shall furnish and place material specified for the subsequent course, or an alternate material approved by the Engineer, to bring the deficient CIR course depth within the tolerance of the specified plan depth.

  - Stabilizing Agent Dosage Rate – The Design-Builder shall verify the stabilizing agent dosage rate by reading a calibrated meter ten times per lot. The dosage rate shall be within 0.20 percentage points of the approved JMF. If the dosage rate is outside 0.20 percentage points, then paving/production shall stop and the Design-Builder shall take corrective measures to bring the dosage rate within tolerance. The Quality Assurance Manager will calculate the yield at the end of each production day.

  - Construction Records – The Design-Builder shall prepare separate test reports meeting the requirements of AASHTO R 18 or may use the current appropriate VDOT forms. Records documenting the dosage rate of stabilizing agent(s) and other test results from TABLE 4 in this special provision shall be provided to the Quality Assurance Manager, unless specified otherwise.

- WEATHER LIMITATIONS

Recycling operations shall be completed when both the atmospheric temperature and material to be processed (measured in the shade and away from artificial heat) is a minimum 50°F. The weather forecast shall not call for freezing temperatures within 48 hours after placement of CIR on any portion of the project.