GUIDELINES – Use when requested by the Designer for asphalt projects. {2007-S315AD0}

SP315-DB0420-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

FULL-DEPTH RECLAMATION (FDR)

December 12, 2018

I.	DESCRIPTION

Full-depth reclamation (FDR) is defined as those processes in which all of the asphalt pavement layers and some portion of the underlying bound and unbound layers are pulverized, stabilized, and compacted in place. The Design-Builder shall select the final mix design (job mix formula- JMF) and construction methods to meet the performance requirements specified herein. This is most commonly performed using hydraulic cement, lime, foamed asphalt or asphalt emulsion as the primary stabilizing additives.

II.	MATERIALS

Stabilizing Agent(s) – The amount of stabilizing agents to be used shall be determined by the Design-Builder by means of a mixture design process. Hydraulic cement shall conform to Section 214 of the Specifications. Lime shall conform to Section 240 of the Specifications. Fly ash shall conform to Section 241 of the Specifications. All liquid asphalts used for stabilizing agents shall be emulsions and PG binders on the VDOT Approved List for emulsions and PG binders, Approved List 50 and 50.1. Liquid asphalts not currently on the Approved List shall be submitted to VDOT for approval. Asphalt emulsions shall conform to Section 210 of the Specifications; liquid asphalts shall meet the requirements of Section 211.02 (a) of the Specifications.

1.	Water – Any water used for mixing shall meet the requirements of Section 216 of the Specifications.

2.	FDR – The FDR material shall have 100% of all particles passing the 2.0 inch (50mm) sieve size and 55% of all particles passing the 3/8 inch (9.5mm) sieve size prior to the addition of any stabilizing agents.

3.	Other Additives – If necessary, additional additives may be used by the Design-Builder to meet the requirements in TABLE 4. In the case where an additional additive is used, the type and dosage must be described in the JMF’s submitted to the Engineer. For FDR using asphalt emulsion, hydrated lime shall be added according to Section 211.02(i) of the Specifications.

4.	Addition of Crushed Reclaimed Asphalt Pavement (RAP) Material – RAP material may be added by the Design-Builder and shall meet the requirements of Section 211.02(j) of the Specifications and TABLE 1.

| TABLE 1 – ADDITIONAL CRUSHED RAP |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Deleterious Materials: Clay Lumps and Friable Particles in Aggregate | AASHTO T 112 | 0.2% maximum |
| Maximum Sieve size, 2.0 in. (50 mm) | AASHTO T 27 | 100% passing |

5.	Additional aggregate – Based on the results of the mixture design or other requirements, the Design-Builder shall determine if additional aggregate is required. If the Design-Builder determines additional aggregate is required any additional aggregate shall meet Section 203 of the Specifications and TABLE 2, and it shall produce a product which meets the mixture requirements given in TABLE 4 and final mix gradation specified in Section IV-1.

| TABLE 2 – ADDITIONAL AGGREGATE |  |  |
| --- | --- | --- |
| Tests | Method | Limit |
| Los Angeles Abrasion Value | AASHTO T 96 | 45% maximum loss |
| Sand Equivalent | AASHTO T 176 | 45% minimum |
| Maximum size, 100% Passing, Sieve Size | AASHTO T 27 | 2.0 in. (50 mm) |
| Water absorption | AASHTO T 85 | 3% maximum |

6.	Handling and Storage – Store cement to prevent moisture degradation and partial hydration. Do not use cement that has become hard, caked or lumpy. Store aggregates and RAP so that segregation and inclusion of foreign materials are prevented. Do not use the bottom six (6) inches of aggregate or RAP piles in contact with the ground.

III.	QUALITY CONTROL PLAN

The Design-Builder shall develop and implement a Quality Control Plan to ensure that operational techniques and activities provide integral and finished material of acceptable quality. Design-Builder sampling and testing shall be performed to control the processes and ensure material compliance with the requirements of the Contract. The Design-Builder shall provide their Quality Control Plan and Job Mix Formulae to the District Materials Engineer for approval no less than 30 calendar days prior to the start of FDR operations.

For each FDR project, a project specific FDR Quality Control Plan is required, and shall include, at a minimum, the following information:

1.	A description of the Design-Builder’s Quality Control organization, including the number of full-time equivalent employees or Sub-Contractors with specific Quality Control responsibilities, including an organizational chart showing lines of authority and reporting responsibilities

2.	A listing by discipline with the name, qualifications, duties, responsibilities and authorities for all persons proposed to be responsible for Construction Quality Control

3.	A Quality Control Sampling, Testing and Analysis Plan with methods that include a description of how random locations for testing and sampling are determined

4.	Identification and description of qualifications of the laboratory(s) to be used for each type of testing

5.	Specific listing of documentation for Quality Control activities

6.	Procedures to meet contract requirements for corrective action when Quality Control criteria are not met

7.	Procedures to protect stabilized material from receiving excessive moisture from weather events (i.e. rain, fog, etc.) and corrective actions when criteria are not met

8.	Contingency Plan including but not limited to:

●	Inclement weather

●	Equipment breakdowns

●	Materials shortages

●	Excessive fluff - (greater than approximately 10%). Fluff is defined as the increase in material thickness of the recycled layer over the specified recycling depth due to remixing in place.

●	Deficient density of installed FDR

●	Material doesn’t break or cure in timely manner

●	Gradation is outside tolerance(s)

●	Production modifications based on changes in ambient and/or material temperature.

The Design-Builder shall have a technical representative at the project site during the mixing and placement operations for the trial section and first day of production. At a minimum, this person must:

●	Have 2 years minimum experience with the FDR process

●	Have personally supervised a minimum of 5 successful FDR projects

●	Have personal experience in developing FDR mix designs

●	Have the experience to perform and supervise field process control testing

●	Submit a list of references, with current telephone numbers, who are able to verify the experience required herein

The Design-Builder may use consultants or manufacturers’ representatives to satisfy the requirements of this section provided they meet the requirements above and are on-site or available for contact while construction operations are being performed.

IV.	Job Mix Formula (JMF)

1.	Mixture Designs – FDR mix designs in the form of a job-mix formula (JMF) shall be submitted to the Engineer for the Department’s approval no less than 30 calendar days prior to the start of FDR operations. More than one JMF may be required. The gradation of each JMF shall fall within the bands shown below.

| TABLE 3 - DESIGN RANGE |  |  |
| --- | --- | --- |
| Sieve Size | Percentage by Weight Passing Square Mesh Sieves (in) |  |
|  | Lower | Upper |
| 2.0” | 100 | 100 |
| 3/8” | 55 | -- |

The Design-Builder shall obtain sufficient samples of the material to be reclaimed directly from each roadway within the project for laboratory testing and mix design analysis. Samples shall be obtained from every 2500 linear feet, within each lane and to the proposed total recycling depth, with a minimum of six locations for each mix design. Sample locations from each lane may be offset or adjacent from each other. Additional locations may also be selected based on pavement conditions and variability.

2.	Mixture Designs Submittal – The design shall be performed by the Design-Builder according to these specifications and submitted to the Engineer for approval thirty (30) working days prior to the planned start of the work. The mix design submittal shall include, at a minimum, the following information:

A.	Target field density

B.	Percent by weight of all stabilizing agents to be added to the recycled mix

C.	Percent water content (at room temperature) required

D.	Expansion ratio and half-life characteristics and temperature of asphalt binder at the time of injection into foaming chamber (for mixtures using foamed asphalt)

E.	Minimum curing time/set time for the asphalt emulsion

F.	Temperature of asphalt emulsion at the time of incorporating into the mixture (for mixtures using asphalt emulsion)

G.	Target gradation (including any aggregate to be added)

| TABLE 4 – FULL-DEPTH RECLAMATION MIX DESIGN REQUIREMENTS |  |  |
| --- | --- | --- |
| Test | Test Method | Criteria |
| Liquid Limit, Plastic Limit, and Plasticity Index of Soil | VTM-7 | Report |
| Dry Preparation and Mechanical Analysis of Soils, Select Material, Subbase and Aggregate Bases | VTM-25 | Report |
| Classification of Soils | AASHTO M 145 | Report |
| Moisture-Density Relations of Soil-Cement Mixtures | AASHTO T 134 | Report |
| Moisture Density Relations for Bituminous Stabilizing Agents | AASHTO T 180 | Report |
| Compressive Strength of Soil-Cement Cylinders | ASTM D 1633 | Min. 250 psi (Max. 450 psi) at seven (7) days |
| Determining the Strength of Soil-Lime Mixtures | VTM-11 | Min. 150 psi |
| Dry Indirect Tensile Strength (ITS) for Foamed Asphalt Stabilizing Agent | AASHTO T 283 Section 11* | 45 psi minimum |
| Marshall Stability Test for Asphalt Emulsion Stabilizing Agent | ASTM 5581 (6 inch specimens), AASHTO T 245 (4 inch specimens)** | 2500 lbs minimum (6 inch (150mm) diameter specimen), or 1250 lbs (4 inch (100mm) diameter specimen) |

* Three specimens shall be produced using either 75 blows per side (per VTM-57) or 30 gyrations (per AASHTO T 312) compacted at or below Optimum Moisture Content and cured as follows: 4 inch (100 mm) diameter specimens, oven dry at 104ºF (40°C) for 72 hrs and cool to ambient air temperature for 24 hrs; 6 inch (150 mm) diameter specimens, air dried for 24 hours, then an additional 48 hours at 104ºF (40ºC) in sealed plastic bag, cool to ambient air temperature for 24 hrs.

** Three specimens shall be produced at 75 blows per side (or 30 gyrations per AASHTO T 312) and cured at 140ºF (60°C) to constant mass, hold specimens at 104ºF (40°C) for 2 hours in a forced draft oven immediately prior to testing.

If a change in source materials is made during construction, a new JMF’s shall be created and approved by the Engineer prior to use on the project. The JMF’s shall meet the above criteria at the approved stabilizing agents content.

V.	EQUIPMENT

1.	Pulverizing – The equipment used to reclaim existing pavements shall be capable of pulverizing existing pavement, as well as any additional materials, to meet the gradation provided in the approved job mix design, for the widths provided in the Plans, to the depth specified in the approved pavement design.

2.	Stabilizing – The equipment used to stabilize the pulverized materials shall be capable of incorporating the stabilizing agents at the rate provided in the approved job mix design, automatically metering dosage and mixing the full depth and width of pulverized material to a homogenous mixture.

3.	Grading – The equipment used to grade the stabilized material shall be capable of working within the constraints of the excavation and grading the full width of stabilized material in conformity with the lines and grades provided in the Plans.

4.	Compacting – The equipment used to compact the stabilized material shall be capable of working within the constraints of the excavation and compacting the stabilized material in conformity with the lines and grades provided in the Plans, as well as in conformity with the density requirements provided in the approved job mix design.

VI.	TRIAL SECTION

One week before planned start of full production, stabilize a 2,500 foot long trial section, one-lane wide, at the designated thickness and designed optimal stabilizing agents content provided in the approved job mix design. Construct the trial section on the project at a location approved by the Engineer.

Construct the trial section using construction procedures intended for the entire project. Cease production after construction of the trial section until the trial section is evaluated and accepted by the Engineer.

VII.	CONSTRUCTION METHODS

1.	Grass and Other Vegetation – All grass and other vegetation shall be removed from the edge of the existing pavement to prevent contamination of the pulverized bituminous material during the milling operation.

2.	FDR – Recycling shall be performed to the depth provided in the plans, while incorporating stabilizing agents, mineral filler, additional aggregate and water. Mixing shall continue until, and the speed of the recycling unit adjusted to ensure, a homogenous mixture of the above materials and pulverized materials is achieved.

A.	Pre-cutting, grading and light compacting of the recycled material shall be performed prior to incorporation of the stabilizing agent.

B.	The application rate of all stabilizing agents shall be continuously monitored using calibrated, automatic meters. The application rate shall be within 0.20 percentage points of the optimal stabilizing agents content provided in the approved job mix design. If the measured application rate falls outside the above tolerance, then the recycling operations shall be stopped and corrected before proceeding.

C.	The water content of the stabilized material shall be monitored closely to ensure conformance with the approved job mix design within ± 2 percentage points of optimum and to ensure proper compaction.

D.	Longitudinal joints between adjacent stabilization passes shall be overlapped at least 4 inches. Transverse joints created by the recycling process shall be saw-cut, if necessary, to provide a vertical, clean face to ensure proper compaction.

3.	Final Grading and Compacting – The final grading and compacting shall be performed within the constraints of the excavation and the stabilized material shall be compacted in conformity with the lines and grades provided in the Plans. Compaction shall progress across the full width of the stabilized area until maximum density is achieved.

A.	Once the entire working width (full lane width plus affected shoulder width) has been stabilized, and only after primary compaction has been completed, the entire working width shall be graded to the required profile and cross-slope. Disturbance to the stabilized and primarily compacted material shall be kept to a minimum during this grading and shaping operation.

B.	Any additional water required to achieve maximum density shall be applied by spraying the surface of the stabilized material with light applications. Care shall be taken not to over-apply additional water to any areas of stabilized material.

4.	Surfacing – The surface of the compacted material shall be kept moist until covered with an asphalt-based layer in the case of cement stabilized materials. For bituminous stabilized materials, the FDR shall be allowed to cure until the moisture of the material is a maximum of 50% the optimum moisture content or until approval of the Engineer is received. Subsequent asphalt-based layers can be placed any time after finishing, as long as the FDR is sufficiently able to support the required construction equipment without marring or permanent distortion of the surface.

VIII.	ACCEPTANCE TESTING

1.	Field Compaction – Density shall be determined with a nuclear gauge operating in direct transmission mode conforming to VTM-10 to the full depth of the FDR layer. The Design-Builder shall have had the gauge calibrated within the previous 12 months by an approved calibration service. In addition, the Design-Builder shall maintain documentation of such calibration service for the 12-month period from the date of the calibration service and furnish the same to the Quality Assurance Manager.

The project will be divided into lots by the Quality Assurance Manager for the purpose of defining areas represented by each series of tests.

2.	Lot – For the purposes of acceptance, each day’s production shall be considered a lot unless the paving length is less than 3,000 linear feet or greater than 7,500 linear feet. When paving is less than 3,000 feet, it shall be combined with the previous day’s production or added to the next day’s production to create a lot as described below.

For the purposes of acceptance, the standard size of a lot shall be 5,000 linear feet, with 1,000 foot sublots, the full width of the lane (including any affected shoulder width). If the Engineer approves, the lot size may be increased to 7,500 linear foot lots with five 1,500 foot sublots when the Design-Builder’s normal daily production exceeds 7,500 feet. When a partial lot occurs at the end of a day’s production or upon completion of the project, the lot shall be either added to the previous lot if the partial lot contains one or two complete sublots, or redefined to be an entire lot if the partial lot contains three or four complete sublots.

Each lot shall be tested for density by taking a nuclear density reading from two stratified-random test sites selected by the Quality Assurance Manager within each sublot. Test sites shall not be located within 18 inches of any longitudinal joint.

The average of the sublot density measurements will be compared to the maximum density from the approved mix design to determine the acceptability of the lot. Once the average density of the lot has been determined, the Design-Builder will not be permitted to provide additional compaction to raise the average. If two consecutive sublots produce density results less than 97.0 percent of the target density, the Design-Builder shall immediately notify the Quality Assurance Manager and institute corrective action. By the end of the day’s operations, the Design-Builder shall furnish the test data developed during the day’s production to the Quality Assurance Manager.

3.	Depth Check – Depth checks shall be performed by the Design-Builder twice per lot after compaction and prior to the placement of the next pavement layer. The depth checks shall be performed twice per lot following VTM-38, Method B.

Acceptance testing of FDR for depth will be based on the mean result of measurements of samples taken from each lot of material placed.

A lot will be considered acceptable for depth if the mean result of the tests is within the tolerance of the plan depth for the number of tests taken as shown in TABLE 5.

| TABLE 5 – PROCESS TOLERANCE FOR DEPTH CHECKS |  |  |  |  |
| --- | --- | --- | --- | --- |
| Plan Depth, inches | Tolerance, inches (Plus or Minus) |  |  |  |
|  | 1 test | 2 tests | 3 tests | 4 tests |
| >6 ≤ 8 | 0.9 | 0.65 | 0.5 | 0.4 |
| >8 ≤ 12 | 1 | 0.9 | 0.7 | 0.5 |
| >12 | 1.2 | 1 | 0.8 | 0.6 |

If an individual depth test is in excess of the tolerance for one test, that portion of the lot represented by that test will be excluded from the lot. If an individual test result indicates that the depth of the material represented by the test is deficient by more than the tolerance for one test, correction of the base course represented by that test shall be made by the Design-Builder as specified hereinafter.

If an individual test result indicates that the depth of material represented by the test is more than the tolerance for one test or if the mean depth of a lot of material is in excess of the tolerance, the Engineer can require excessive material to be removed.

If the mean depth of a lot of material is deficient beyond the allowable tolerance, correction will be required. The Design-Builder shall furnish and place material specified for the subsequent course, or an alternate material approved by the Engineer,

to bring the deficient FDR course depth within the tolerance.

4.	Gradation – The Design-Builder will check the unstabilized gradation twice per day.

5.	Stabilizing Agent Dosage Rate – Design-Builder shall verify the dosage rate ten times per lot. The dosage rate shall be within 0.20 percentage points of the approved mix design. If the dosage rate is beyond this tolerance, then paving shall stop and the Design-Builder shall take corrective measures.

6.	Construction Records – The Design-Builder shall prepare separate test reports meeting the requirements of AASHTO R 18 or may use the current appropriate VDOT forms. Records documenting the dosage rate of stabilizing agents and other test results from Table 4 shall be provided to the Quality Assurance Manager, unless specified otherwise.

IX.	WEATHER LIMITATIONS

Recycling operations shall be completed when both the atmospheric temperature and material to be processed (measured in the shade and away from artificial heat) is a minimum 40°F (4 °C). The weather forecast shall not call for freezing temperature within 48 hours after placement of any portion of the project.