SP315-DB0710-01

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

# RIDEABILITY FOR DESIGN-BUILD PROJECTS

November 19, 2018

# SECTION 315—ASPHALT CONCRETE PAVEMENT and SECTION 316 – HYRDAULIC CEMENT CONCRETE PAVEMENT of the Specifications are amended as follows:

Section 315.07 Pavement Tolerances and Section 316.05 Thickness and Finished Grade Tolerances are amended to include the following:

For all travel lanes, excluding ramps, that are designated in the contract to be constructed by the Design-Builder, the final ride quality acceptance will be based on the lowest average International Roughness Index (IRI) for each 0.01-mile section produced by a minimum of two test runs, using a South Dakota style road profiling device and reported for each travel lane. Testing will be conducted in accordance to VTM – 106. Testing equipment shall conform to VTM-106 and shall measure both wheelpaths with laser height sensing instruments. The Department will conduct the testing within 30 calendar days from the date of receipt of the Design-Builder’s written request, provided the Design-Builder can arrange unimpeded access to the paved surface for constant highway speed test runs.

The Design-Builder shall submit a written request for testing to the Engineer following the completion of the final surface course and final pavement striping over the designated section. The designated section is defined as all travel lanes specified for the Project that have been constructed by the Design-Builder. The Design-Builder may request alternate limits for testing of the designated section as previously defined provided the request is submitted to the Engineer for review at least 30 calendar days prior to placement of final paving course. The Engineer will have 10 calendar days to review and approve or deny the request. The minimum length of the designated section the Design-Builder can request is 0.5 continuous lane mile.

If temporary pavement marking is placed and the lanes are clearly delineated over the completed final surface course, the Design-Builder may submit a written request for Rideability testing to the Engineer. The Department will conduct testing within 30 calendar days from the written request provided the Design-Builder can arrange unimpeded access to the paved surface for constant highway speed test runs.

# Acceptance

For all sections designated in the contract for Ride, an IRI number in inches per mile will be established for each 0.01-mile increment for each designated lane. The last 0.01-mile (52 feet) increment before a bridge, the first 0.01-mile (52 feet) increment after a bridge, and the beginning and end 0.01-mile (52 feet) increments of the final surface will not be subject to a pay adjustment.

Areas excluded from testing by the road profiling device will be tested using a 10-foot straightedge. The variation of the surface from the testing edge of the straightedge between any two contacts with the surface shall not be more than 1/4 inch. Humps and depressions exceeding the specified tolerance shall be subject to correction as directed by the Engineer, at the Design-Builder’s expense.

  - Positive and Negative Quality Rate Adjustment

    - Asphalt and Hydraulic Cement Concrete Pavement Construction

For sections identified as “Positive and Negative Quality Rate Adjustment”, Tables A and B provide the acceptance quality of asphalt and hydraulic cement concrete pavement based on the finished rideability for interstate, limited access, non-interstate, and non-limited access roadways.

| TABLE A – POSITIVE AND NEGATIVE QUALITY RATE ADJUSTMENT INTERSTATE OR LIMITED ACCESS SYSTEM |  |  |
| --- | --- | --- |
| IRI After Completion (Inches Per Mile) | Stone Matrix Asphalt Surface or Hydraulic Cement Concrete Quality Rate Adjustment (Per Square Yard) | Superpave Asphalt Surface Quality Rate Adjustment (Per Square Yard) |
| 45.0 and Under | $1.60 | $1.40 |
| 45.1-55.0 | $1.10 | $0.95 |
| 55.1-70.0 | $0.00 | $0.00 |
| 70.1-80.0 | -$1.10 | -$0.95 |
| 80.1-90.0 | -$2.15 | -$1.85 |
| 90.1-100.0 | -$3.20 | -$2.75 |
| 100.1-120.0 | -$4.25 or Subject To Corrective Action | -$3.70 or Subject to Corrective Action |
| 120.1-140.0 | -$6.35 or Subject to Corrective Action | -$5.50 or Subject to Corrective Action |
| 140.1-160.0 | -$8.50 or Subject to Corrective Action | -$7.35 or Subject to Corrective Action |
| Over 160.1 | -$10.60 or Subject to Corrective Action | -$9.15 or subject to Corrective Action |

| TABLE B – POSITIVE AND NEGATIVE QUALITY RATE ADJUSTMENT NON- INTERSTATE AND NON-LIMITED ACCESS SYSTEM |  |  |
| --- | --- | --- |
| IRI After Completion (Inches Per Mile) | Stone Matrix Asphalt Surface or Hydraulic Cement Concrete Quality Rate Adjustment (Per Square Yard) | Superpave Asphalt Surface Quality Rate Adjustment (Per Square Yard |
| 55.0 and Under | $1.60 | $1.40 |
| 55.1-65.0 | $1.10 | $0.95 |
| 65.1-80.0 | $0.00 | $0.00 |
| 80.1-90.0 | -$1.10 | -$0.95 |
| 90.1-100.0 | -$2.15 | -$1.85 |
| 100.1-110.0 | -$3.20 | -$2.75 |
| 110.1-130.0 | -$4.25 or Subject To Corrective Action | -$3.70 or Subject to Corrective Action |
| 130.1-150.0 | -$6.35 or Subject to Corrective Action | -$5.50 or Subject to Corrective Action |
| 150.1-170.0 | -$8.50 or Subject to Corrective Action | -$7.35 or Subject to Corrective Action |
| Over 170.1 | -$10.60 or Subject to Corrective Action | -$9.15 or Subject to Corrective Action |

A quality rate adjustment calculation will be made at each 0.01-mile increment and summed over each 0.1 mile length. The sum of all 0.1 mile lengths for the designated section will be the total quality rate adjustment. However, if sections are subject to corrective action in accordance with Table A and B, the Design-Builder shall submit proposed method(s) of correction to the Engineer within 14 calendar days of notification from the Department that corrective action is required. It is the Engineer’s sole discretion to determine if the Design-Builder shall perform corrective action or be assessed the corresponding negative Quality Rate Adjustment. The method of correction shall be reviewed and approved by the Engineer prior to corrective action being performed. If corrective action is approved by the Engineer, the correction shall be performed at the Design-Builder’s expense. The Engineer may require correction of any or all adjoining traffic lanes or shoulders at the Design-Builder’s expense to assure uniform cross section.

Where corrections are made after the initial Department rideability test, the pavement will be retested by the Department to verify that corrections have produced an acceptable ride surface. The maximum Quality Rate Adjustment for 0.01-mile increments on which corrective actions have been required by the Engineer will be $0.00 per square yard. Additional corrections may be required by the Engineer at the Design-Builder’s expense based on the retested IRI measurements. In the event the corrective action(s) do not result in 100 percent payment, and not subject to further corrective action, the Design-Builder will be assessed the corresponding negative Quality Rate Adjustment.

This rideability specification does not relieve the Design-Builder from responsibility concerning workmanship in accordance with the requirements of the contract.

    - Single-Lift Asphalt Construction

Where only one AC layer shall be placed on existing paved travel lanes as part of the contract and designated for “Positive and Negative Quality Rate Adjustment”, the Department will test those lanes prior to work by the Design-Builder. Upon request by the Design-Builder, the Engineer will provide the IRI testing results. If this IRI testing is conducted more than 180 calendar days prior to the scheduled beginning of the work, the Design-Builder may request new IRI testing.

A quality rate adjustment calculation will be made at each 0.01-mile increment and summed over each 0.1 mile length. Based on the average IRI (original surface and completed overlay) for each 0.1-mile length of each travel lane subject to this special provision, no corrective action will be required if the completed surface for the 0.1 mile length has IRI test results which indicate a 30 percent or more improvement in the ride quality. This percent improvement is based on the 0.1- mile paved section average IRI and not the individual 0.01-mile increments. When the 30 percent improvement is achieved for a 0.1-mile length, the payments (positive, negative and full payment) for the individual 0.01-mile increments will be summed. The Design-Builder will then be paid the greater of the total adjusted payments or 100 percent for that 0.1-mile length. For 0.1 mile lengths that do not achieve 30% or more improvement, pay adjustment in accordance with Table A or B of section A.1 of this specification will be applied for the designated contract section(s). The sum of all 0.1 mile lengths for the designated section will be the total quality rate adjustment.

This rideability specification does not relieve the Design-Builder from responsibility concerning workmanship in accordance with the contract requirements.

  - Positive Quality Rate Adjustment Only

For contract sections designated as “Positive Quality Rate Adjustment Only”, Table C will be applied for calculating quality rate adjustment. A quality rate adjustment calculation will be made at each 0.01-mile increment and summed over each 0.1 mile length. Any negative quality rate adjustments, calculated at each 0.1 mile length, will be waived. Only quality rate adjustment calculation producing a positive quality rate adjustment for each 0.1 mile (if any) length will be summed to determine the total positive quality rate adjustment. Therefore, no negative quality rate adjustment will be assessed over the entire designated “Positive Quality Rate Adjustment Only” contract section. The Design-Builder will be paid the greater of the total positive quality rate adjustment or 100 percent payment for the designated section.

| TABLE C – POSITIVE QUALITY RATE ADJUSTMENT ONLY |  |  |
| --- | --- | --- |
| IRI After Completion (Inches Per Mile) | Stone Matrix Asphalt Surface or Hydraulic Cement Concrete Quality Rate Adjustment (Per Square Yard) | Superpave Asphalt Surface Quality Rate Adjustment (Per Square Yard) |
| 60.0 and Under | $1.60 | $1.40 |
| 60.1-70.0 | $1.10 | $0.95 |
| 70.1-85.0 | $0.00 | $0.00 |
| 85.1-95.0 | -$1.10 | -$0.95 |
| 95.1-105.0 | -$2.15 | -$1.85 |
| 105.1-115.0 | -$3.20 | -$2.75 |
| 115.1-135.0 | -$4.25 | -$3.70 |
| 135.1-155.0 | -$6.35 | -$5.50 |
| 155.1-175.0 | -$8.50 | -$7.35 |
| Over 175.1 | -$10.60 | -$9.15 |

Positive Quality Rate Adjustment only sections will not be subject to corrective action as a result of the rideability results. Ride testing prior to paving by the Department is not required for these sections. Quality rate adjustments will be applied to the square yard of the pavement placed for the lane width and section length tested.

This rideability specification does not relieve the Design-Builder from responsibility concerning workmanship in accordance with the contract requirements.

# Application of Quality Rate Adjustments

Quality Rate Adjustments will be applied to each 0.01-mile increment tested, excluding the exemptions noted herein, based on the dollar amount per square yard shown in Table A, B or C. The Quality Rate Adjustment will be based on the Department’s initial acceptance rideability testing prior to any corrective action approved by the Engineer. For the section(s) where corrective action is required, the maximum positive Quality Rate Adjustment will be $0.00 per square yard. If after corrective action the pavement fails to meet the required rideability and not subject to corrective action, a negative Quality Rate Adjustment will apply.