GUIDELINES — Use when requested by the Designer. {2007-S404H01}

SP404-000120-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

SEALING LINEAR CRACKS IN CONCRETE DECKS AND

OVERLAYS USING EPOXY AND CARBON FIBER MESH

September 16, 2009c; Reissued July 12, 2016

I.	DESCRIPTION

This Special Provision specifies the requirements for sealing linear cracks and construction joints in hydraulic cement concrete bridge decks and overlays with epoxy and open grid carbon fiber mesh as directed by the Engineer.

Linear cracks, particularly transverse cracks, can be caused by thermal contraction, drying shrinkage, construction loads, continuous span deck construction sequence and live load induced tensile stress.  The width of the cracks may be a function of thermal contraction, drying shrinkage, crack spacing, concrete age, and loads applied to the deck.

The cracks get wider with age as the concrete under goes drying shrinkage.  This special provision does not apply to decks constructed with solid stainless reinforcing steel.

II.	MATERIALS

Epoxy and aggregate materials shall meet the requirements in Section 431 of the Specifications.  Carbon Fiber Mesh Materials shall conform to the following:

4-inch Carbon Fiber Strip Specs:

The carbon fiber mesh is comprised of a high tensile strength carbon fiber.  The mesh is not impregnated and is wet out and cured in place in epoxy resin overlay.

| General Information: |  |
| --- | --- |
| Constituent Materials: | 6K Carbon Fiber unidirectional tows |
| Primary Fiber Directions | Closed knit 0 X 90 |
| Color | Black |
| Packaging | 4” X 200 linear ft rolls |

| Carbon Material Properties |  |  |
| --- | --- | --- |
| Nominal Thickness | 0.030 inches |  |
| Nominal Tensile Strength per unit width | 400,000 psi | ASTM D3039-08 |
| Nominal Tensile Modulus | 33,000,000 psi | ASTM D3379-75(R-89) |
| Failure Strain | 1.3% | ASTM D3379-75(R-89) |
| Grid Spacing | 1/4” x 1/4” (inch) (longitudinal x transverse) |  |

III.	CONCRETE AGE AT TIME OF CRACK FILLING AND SEALING

Cracks shall be located and sealed at the oldest age that is practical as determined by the Engineer and prior to the final acceptance of the project and prior to opening the surface to traffic.

IV.	LOCATING CRACKS THAT SHALL BE FILLED AND SEALED

Crack width shall be measured using a transparent crack comparator placed on the surface of the concrete.  The width shall be at the oldest age that is practical as determined by the Engineer and prior to the final acceptance of the project and prior to opening the surface to traffic.  The width shall be measured and recorded prior to 3 hours past sun rise.  Cracks with a width equal to or greater than 0.2 millimeter shall be marked for sealing.

V.	SURFACE PREPARATION AND APPLICATION

The surface of the concrete on which the carbon fiber mesh will be placed shall be cleaned according to Section 431 of the Specifications.  The epoxy and aggregate shall be placed according to the requirements for the first layer in Section 431 of the Specifications.  Dump and spread the mixed epoxy resin on the designated area for the placement of the 4-inch Carbon Fiber strip.  Apply the epoxy at a minimum rate of 2 ½ gallons per 100 square feet.  Immediately place the 4-inch Carbon Fiber strip precut to the required length into the placed epoxy allowing the epoxy to wet into the carbon strip and to penetrate through the openings in the carbon strip to thoroughly encapsulate the strip.  A roller or squeegee may be used to assist penetration and to ensure the strip is pressed to the substrate and the epoxy is evenly spread.  Use a squeegee to move adjacent epoxy over the strip for complete encapsulation.  Broad cast aggregate to excess over all surfaces covered with epoxy.

The Contractor shall plan and prosecute the work in such a manner to protect persons, vehicles and the bridge structure from injury or damage.  In the event epoxy materials or solvents harm the appearance of bridge components, removal of such materials will be required as directed by the Engineer.  Traffic will not be permitted on the treated surface during the curing period which is specified in Section 431 of the Specifications.

VI.	MEASUREMENT AND PAYMENT

Crack sealing will be measured and paid for at the contract unit price per linear foot as specified.  The price bid for such work shall be full compensation for surface and crack preparation, for furnishing and applying the epoxy, carbon fiber mesh and aggregate, for vehicular and pedestrian protection, for protection of waterways and bridge surfaces and for all labor, tools and incidentals necessary to complete the work.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Crack sealing using epoxy and carbon fiber mesh | Linear foot |