Guidelines: For bridges with prestressed concrete adjacent members (voided slabs, box beams). Material for these components need to be shown on the Plans. The special provision SP217-000100 (VHPC) or SP217-000110 (ECC) shall be included.

SP404-000130-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

SHEAR KEYS AND BLOCK OUTS BETWEEN ADJACENT MEMBERS

March 25, 2021

- Description

This work shall consist of filling shear keys and Virginia Adjacent Member Connection block-outs in accordance with the Plans.

- Materials

Shear keys and Virginia Adjacent Member Connection block-outs will be constructed using the material shown on the Plans.

  - Engineered Cementitious Composite (ECC) shall conform to ECC-Shear Keys of the Special Provision for Engineered Cementitious Composite.

  - Very High Performance Concrete (VHPC) shall conform to the Special Provision for Very High Performance Concrete.

- Procedures

- Shear keys

All shear key surfaces shall be cleaned of all dirt, laitance, and loose aggregate by means of sandblasting, and then pre-wetted prior to filling. Material for shear keys shall be placed in one continuous operation without interruption using a method that will provide a neat, workmanlike joint using a trough sized for the shear key opening, and in accordance with Section 404 of the Specifications. Care shall be taken to prevent leakage of the material into precast holes for transverse tendons or from the bottom of shear keys. The method used to prevent leakage shall not protrude more than 1/4 inch into shear key. Material in the shear key shall be cured in accordance with Section 404.03(k) of the Specifications for seven days or until application of Epoxy Type EP-7 and joint fabric. The bridge shall not be overlaid or opened to traffic until the material has reached a minimum compressive strength of 4000 psi. Construction equipment weighing more than 1,000 pounds shall not be moved on or off the bridge until the minimum compressive strength is obtained.

- Virginia Adjacent Member Connection block-outs

All block-out and adjacent shear key surfaces shall be cleaned of all dirt, laitance, and loose aggregate by means of sandblasting, and then pre-wetted prior to filling. Filling block-outs and adjacent shear keys with Very High Performance Concrete shall be done in one continuous operation without interruption for each span using a method that will provide a neat, workmanlike joint. A trough sized for the shear key opening shall be used for material placement outside of the block outs. Care shall be taken to prevent leakage of the VHPC into precast holes for transverse tendons or from bottom of shear keys. The method used to prevent leakage shall not protrude more than 1/4 inch into shear key. Material in the block-outs shall be cured in accordance with Section 404.03(k) of the Specifications. Epoxy Type EP-7 and joint fabric shall not be placed until the VHPC has cured for a minimum of 24 hours. The bridge shall not be overlaid or construction equipment weighing more than 1,000 pounds moved on or off the bridge until the material has reached a minimum compressive strength of 4000 psi. The bridge shall not be opened to traffic until the 7-day compressive strength is reached.

- Measurement and Payment

Shear keys will be measured in cubic feet and will be paid for at the Contract cubic feet price. This price shall include preparing and testing the trial batch and furnishing, installing, and curing shear key material. The cost of Epoxy Type EP-7, sand and joint fabric are included in the cost of the Prestressed Members.

Virginia Adjacent Member Connection block-outs will be measured in cubic feet, including the volume in adjacent shear keys, and will be paid for at the Contract cubic feet price. This price shall include preparing and testing the trial batch and furnishing, installing, and curing block-out and shear key material. The cost of Epoxy Type EP-7, sand and joint fabric are included in the cost of the Prestressed Members. Reinforcing steel is paid for separately.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Shear Keys | Cubic Feet |
| Virginia Adjacent Member Connection Block-Outs | Cubic Feet |