SP520-000100-00

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

ARTICULATED CONCRETE BLOCK

April 26, 2022

# DESCRIPTION

This work shall consist of assembling, furnishing, and installing prefabricated articulated concrete block (ACB) as cellular concrete mats in accordance with the lines, grades, typical sections, and cross sections shown on the Plans, the manufacturer’s instructions, these Specifications, and as directed by the Engineer.

# MATERIALS

Each interconnected block shall minimize lateral displacement of the blocks within the mats when they are lifted by the longitudinal revetment cables. The surfaces must not protrude beyond the perimeter of the blocks to such an extent that they reduce the flexibility or articulation capability of the cellular mats, or become damaged or broken when the mats are lifted during shipment or placement. Once the mats are in place, lateral displacement of the blocks shall be minimized even if the cables and fittings should become damaged or removed.

Cellular concrete mats have the ability to be fabricated in various lengths, widths, and in combinations of lengths or widths, but shall not be fabricated larger than a width of 8 feet and a length of 40 feet.

Full-scale laboratory test results for cellular concrete mats, along with associated engineering calculations quantifying the hydraulic capacity of the proposed cellular concrete mat system, shall be provided in accordance with this Specification.

## Certification (Open-Channel Flow): Cellular concrete mats shall conform to ASTM D7277. All hydraulic performance testing shall be performed in a 2H:1V flume.

## Performance (Open-Channel Flow): The design of the cellular concrete mats shall have a minimum safety factor of 1.5 for the smallest block by utilizing the design methodology described in the following references:

## Design Guideline 8 – “Articulating Concrete Block System”, Bridge Scour and Stream Instability Countermeasures: Experience, Selection, and Design Guidance - Third Edition, Volume 2, Hydraulic Engineering Circular No. 23, September 2009, Publication No. FHWA-NHI-09-112.

- Standard Guide for Analysis and Interpretation of Test Data for Articulating Concrete Block (ACB) Revetment Systems in Open Channel Flow, ASTM D7276. ASTM International.

- ACB Revetment Design— Factor Of Safety Method, National Concrete Masonry Association, TEK 11-12A, Herndon, Virginia, revised 2011.

The analysis shall be performed based upon the stability of the mat due to gravity forces alone, neglecting conservative forces added by cabling, mechanical anchorage, contact with adjacent blocks, or other restraints not attributed to gravity-based forces. The analysis must account for a 1/2-inch block projection in accordance with ASTM D6884.

## Concrete Block: The concrete blocks shall be fabricated from a cementitious material and shall conform to Section 217 of the Specifications. At the time of delivery to the work site, the units shall conform to Table 1. ACB units shall be sampled and tested in accordance with ASTM D6684 and ASTM C1262.

| Table 1 Physical Requirements |  |  |  |
| --- | --- | --- | --- |
| Compressive Strength Net Area Min. psi |  | Water Absorption Max. lbs/ft3 |  |
| Avg. of 3 units | Individual Unit | Avg. of 3 units | Individual Unit |
| 4,000 | 3,500 | 9.1 | 11.7 |

## Visual Inspection

All units shall be sound and free of defects that would interfere with either the proper placement of the unit or impair the performance of the system.

Surface cracks incidental to the usual methods of manufacture, or surface chipping resulting from customary methods of handling in shipment and delivery, shall not be deemed grounds for rejection.

Cracks exceeding 0.25 inches in width and/or 1.0 inch in depth shall be deemed grounds for rejection. Chipping resulting in a weight loss exceeding 10% of the average weight of a concrete unit shall be deemed grounds for rejection. However, blocks rejected at the project site may be repaired at the discretion of the Engineer; repairs shall be made with 4000 psi non shrink grout at no additional cost to the Department.

Blocks that the Engineer determines cannot be repaired shall be replaced at no additional cost to the Department.

## Cable and fittings shall be made in a manner that ensures a design with a specified factor of safety for mats being lifted from both ends, thereby forming a catenary. Consideration shall be taken for the bending of the cables around hooks or pins during lifting. Revetment cable splicing fittings shall be selected so that the resultant splice shall provide a minimum of 60% rated cable strength for poly and a minimum of 75% rated cable strength for steel. Flexibility tolerances must equal a minimum of 18 degrees between rows and columns in the uplift direction and a minimum of 45 degrees in the downward direction. Fittings such as sleeves and stops shall be aluminum or stainless steel, and washers shall be galvanized or stainless steel unless otherwise specified in the Plans.

The revetment cable shall exhibit resistance to concentrated acids, alkalis, solvents, and acid forming soils. Cable shall be impervious to rot, mildew, and degradation associated with marine organisms. The materials used in the construction of the cable shall not be affected by continuous immersion in fresh or saltwater.

Cables shall be of the following characteristics:

### Polyester Revetment Cable and Fittings: Revetment cable shall be constructed of high tension, low elongation, and continuous filament polyester fibers. Cable shall consist of a core construction comprised of parallel fibers contained within an outer jacket or cover. The weight of the parallel core shall be 5% to 70% of the total weight of the cable. The revetment cable shall conform to Table 2.

| Table 2 Polyester Cable |  |  |  |  |
| --- | --- | --- | --- | --- |
| Nominal Cable Diameter (in) | Approximate Average Strength |  | Weight per Length |  |
|  | (lbs) | (kN) | (lbs)/100ft | (kg/m) |
| 1/4 | 3,000 | 13.3 | 2.2 | 0.03 |
| 5/16 | 7,000 | 31.1 | 4.4 | 0.07 |
| 3/8 | 10,000 | 44.5 | 5.5 | 0.08 |
| 1/2 | 15,000 | 66.7 | 9.7 | 0.14 |

Elongation requirements specified below are based upon stabilized new, dry cable. Stabilization refers to a process in which the cable is cycled 50 times between a load corresponding to 2000 lbs and a load equal to 10%, 20% or 30% of the cable’s approximate average breaking strength. The revetment cable elongation shall conform to Table 3 at the percent of breaking strength shown.

| Table 3 Elastic Elongation At Percentage of Break Strength |  |  |
| --- | --- | --- |
| 10% | 20% | 30% |
| 0.61 | 1.41 | 2.21 |
| 1The tolerance of these values is ± 5%. |  |  |

### Galvanized and Stainless Steel Revetment cable and Fittings: Revetment cable shall be constructed of preformed galvanized or stainless steel. Cable shall consist of a core construction comprised of seven wires wrapped within 7- or 19-wire strands. The revetment cable shall conform to Table 4.

| Table 4 Galvanized and Stainless Cable |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Nominal Cable Diameter (in) | Type | Approx. Average Strength |  | Weight per Length |  |
|  |  | (lbs) | (kN) | (lbs)/100ft | (kg/m) |
| 1/8 | 7x7 | 1,700 | 7.5 | 2.8 | 0.04 |
| 3/16 | 7x7 | 3,700 | 16.4 | 6.2 | 0.09 |
| 1/4 | 7x7 | 6,100 | 27.1 | 10.6 | 0.16 |
| 5/16 | 7x19 | 9,800 | 43.6 | 17.3 | 0.26 |
| 3/8 | 7x19 | 14,400 | 64.1 | 24.3 | 0.36 |

Depending on the material availability, the cable type (7x7 or 7x19) can be interchanged while providing the required factor of safety.

## Permanent anchors for mat stabilization may be required for slopes 2H:1V or steeper. Anchors shall be secured into earth or another structure through the lifting cable loops, or through open cells of the open-cell block in accordance with manufacturer instructions and as approved by the Engineer.

Where permanent anchoring is required (e.g. hanging mats on steep slopes without toe construction) the cables (polyester or steel) shall be attached to the anchoring system in accordance with manufacturer’s instructions and as approved by the Engineer. The design and layout of the anchored system shall be provided by the manufacturer and sealed by a Professional Engineer licensed in the Commonwealth of Virginia in accordance with Section 105 of the Specifications.

## Riprap bedding geotextile, as specified in Section 245 of the Specifications, shall not be affixed to the mattress (i.e. chemically bonded to the blocks) in a manner that would jeopardize the functionality of the geotextile. The geotextile shall be independent of the block system.

# PROCEDURES

All cellular concrete mats shall be prefabricated as an assembly of ACB, with specific hydraulic capacities, laced with revetment cables. Cellular concrete mats may be assembled on-site by hand placing the individual units either with subsequent insertion of cables or pre-assembled prior to delivery to the site.

Individual units in the system shall be staggered and interlocked for enhanced stability. The mats shall be constructed of open or closed cell units. The open cell units shall have vertical openings with sufficient wall thickness to resist breakage during shipping and installation.

## Submittals: The Contractor shall submit to the Engineer all manufacturers’ hydraulic calculations in support of the proposed cellular concrete mat system and geotextile. All calculations submitted shall be in accordance with this Specification.

### The Contractor shall furnish the manufacturer's certificates of compliance for cellular concrete blocks or mats, revetment cable, and any revetment cable fittings in accordance with this Specification.

### Only products from the VDOT Materials Division Approved Products List shall be used. The Contractor shall also furnish the manufacturer's instructions, literature, shop drawings for the layout of the mats, and any recommendations, if applicable, that are specifically related to the project.

### Submitted calculations and shop drawings shall be sealed by a Professional Engineer licensed in the Commonwealth of Virginia.

## Foundation Preparation:  Areas on which geotextile material and ACB will be placed shall be constructed in accordance with the Plans, the Specifications, and as directed by the Engineer.

Changes in grade that result in a discontinuous revetment surface in the flow direction shall require a 4000 psi non-shrink grout seam at the grade change locations to produce a continuous surface.

## Grading: In addition to the requirements of Section 303 of the Specifications, the slope shall be graded to a smooth plane surface and compacted in lifts as directed by the Engineer to ensure that contact is achieved between the slope face and the geotextile (filter fabric), and between the geotextile and the entire bottom surface of the ACB.

Slope deformities such as roots, grade stakes, and stones shall be removed. No holes, “pockmarks”, slope board teeth marks, footprints, or other voids greater than 1 inch in depth will be permitted. No grooves or depressions greater than 1/2 inch in depth or with a dimension exceeding 1 foot in any direction shall be permitted. Where such areas are evident, they shall be brought to grade by placing compacted homogenous material. The slope and slope face shall be uniformly compacted; and consistent layer depths, soil qualities, and compaction amounts shall be as directed by the Engineer.

## Trench Grading: Excavation and preparation for anchor trenches, flanking trenches, and toe trenches or aprons shall be in accordance with the Plans, the Specifications, and as directed by the Engineer. The width of the anchor trench hinge-point shall be graded uniformly to ensure contact between all cellular concrete blocks and the underlying grade at the hinge-point in accordance with the manufacturer’s instructions.

## Inspection: Before placing the geotextile and cellular concrete blocks, the prepared subgrade will be inspected by the Engineer. No fabric or blocks shall be placed thereon until that area has been approved by the Engineer. The Engineer's approval expires after one calendar day or after an adverse weather event, as determined by the Engineer. If the Engineer's approval expires, the Contractor shall prepare the subgrade for re-inspection by the Engineer, and the same approval expiration criteria shall apply.

## Placement of Geotextile Filter Fabric: At a minimum, the geotextile shall be placed directly on the prepared area, in contact with the subgrade, and free of folds or wrinkles. The geotextile shall not be walked on or disturbed after placement. The geotextile shall be placed so that the upstream strip of fabric overlaps the downstream strip, and the longitudinal and transverse joints shall be overlapped at least 2 feet. The geotextile shall extend at least 1 foot beyond the top and bottom revetment termination points. If cellular concrete blocks are pre-assembled and placed as large mattresses, the top lap edge of the geotextile should not occur in the same location as a joint between the cellular concrete mats unless the joint is concrete filled.

Geotextile placement shall be approved by the Engineer prior to placement of cellular concrete mats. If geotextile becomes displaced, ripped, or damaged in any way during the installation process, including placement of the blocks, reinstallation of geotextile shall be at no additional cost to the Department.

## Placement of ACB/Mats: Concrete blocks and cellular concrete mats shall be constructed in accordance with the lines and grades shown on the Plans, the manufacturer’s instructions, the Specifications, and as directed by the Engineer.

### Assembled in place ACB: The concrete blocks shall be placed on the geotextile in such a manner as to produce a smooth plane surface in contact with the geotextile. No individual block within the plane of placed blocks shall protrude more than 1/2 inch or as otherwise specified by the Engineer. To ensure that the concrete blocks are flush and in full contact with the subgrade, the blocks shall be “seated” with a roller, or other means recommended by the manufacturer and as approved by the Engineer. Hand placement of concrete block will be limited to specific locations as shown in the shop drawings and approved by the Engineer.

### Pre-assembled ACB Mat: If pre-assembled and placed as a large mat, the concrete mats shall be attached to a spreader bar or other approved device to aid in the lifting and placing of the mats in their proper position by the use of a crane or other approved equipment. The equipment used should have adequate capacity to place the mats without bumping, dragging, tearing or otherwise damaging the underlying geotextile fabric. The mats shall be placed side-by-side or end-to-end, so that the mats abut each other. Mat seams or openings between mats greater than 2 inches shall be filled with 4000 psi non-shrink grout.

## Anchor and Side Trenches: Trenches shall be backfilled and compacted flush with the top of the concrete blocks to maintain integrity for the service life of the mat. No more than 500 linear feet of placed cellular concrete blocks with non-completed anchor or toe trenches will be permitted at any time.

## Finishing: If cellular concrete mats are used, the cells shall be backfilled and compacted immediately with suitable material, as specified by the manufacturer, to ensure there are no voids and material extends from the geotextile fabric to 1 inch above the surface of the cellular concrete block. Backfilling and compaction shall be completed so that no more than 500 feet of exposed mats exist at any time.

## Warranty: The Contractor shall follow the manufacturer’s instructions for the installation of the cellular concrete blocks and mats. If a manufacturer’s representative is required to be present onsite during installation, the Contractor shall coordinate with the manufacturer to ensure one is present.

# MEASUREMENT AND PAYMENT

Articulated concrete block will be measured in square yards of surface area and will be paid for at the Contract square yard price. If limits are not shown on the Plans, measurements will be from the outside edge to outside edge, including anchor trenches, flanking trenches, and toe trenches or aprons as appropriate. This price shall include grading; preparing and providing submittals; and furnishing and installing geotextile fabric foundation course, grout, ACB, and treatment.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Articulated concrete block slope protection | Square yard |