SQ305-000100-00

GUIDELINES – Modified aggregate shoulder material (Loudoun county only). {2007-SU305000A}

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

MODIFIED AGGREGATE SHOULDER MATERIAL

(Northern Virginia District – Loudoun County Only)

October 2, 2008; Reissued February 23, 2022_

I.	DESCRIPTION

This work shall consist of furnishing and placing aggregate shoulder material according to the requirements herein and as directed by the Engineer.  Shoulder material shall consist of aggregate No. 21A mixed with topsoil for the purpose of establishing a vegetative cover on the roadway shoulder.

II.	MATERIALS

Aggregate No. 21A material shall conform to Section 208 of the Specifications.  Class B topsoil material shall conform to Section 244 of the Specifications.

III.	PROCEDURES

Modified aggregate shoulder material shall consist of 80 percent aggregate No. 21A and 20 percent Class B topsoil by weight.  Modified aggregate shoulder material shall be mixed mechanically to produce a well-blended and well-graded product.  The Contractor shall furnish a certified weigh ticket according to Section 109.01(b) of the Specifications upon delivery of the material.  Subbase and shoulder material shall be placed according to Section 305.03(e) of the Specifications.  The material shall be well compacted for stability, however, the density requirements are waived.

IV.	MEASUREMENT AND PAYMENT

Modified aggregate shoulder material will be measured in tons according to Section 109.01 of the Specifications and paid for at the contract unit price per ton.  The price bid for such work shall be full compensation for furnishing aggregate and Class B topsoil, mixing, placing and for all labor, tools and incidentals necessary to complete the work.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Modified Aggregate Shoulder Material | Ton |