SQ315-000200-24

VIRGINIA DEPARTMENT OF TRANSPORTATION

SPECIAL PROVISION FOR

Balanced Mix Design (BMD) Surface Mixtures Designed using Performance Criteria

April 24, 2023

I.	Description

This Specification covers the requirements and materials used to produce surface mixtures designed using performance criteria. Balanced Mix Design (BMD) surface mixtures shall be designed, produced, and placed as required by this Special Provision and Sections 211 and 315 of the Specifications.

II. 	Materials

All materials shall conform to Section 211.02 of the Specifications with the exception that Recycled Asphalt Shingles (RAS) will not be allowed in these mixes.

III.	Job-Mix Formula (JMF)

Mix Types SM-9.5A, SM-9.5D, SM-12.5A, and SM-12.5D shall be designed to meet the Performance + Volumetric Optimized (BMD P+VO) criteria included in this section. Each mix type used shall conform to Section 211 of the Specifications.  The Contractor shall submit the mix design at least two weeks before the mix is produced. Approval from the Engineer is required if the Contractor uses a  binder with a PG grade not recommended by Table II-14A of Section 211 of the Specifications.

Type Performance + Volumetric Optimized (BMD P+VO) asphalt mixtures shall be designed to conform to Section 211.03 of the Specifications as well as Table 1 herein, except that the following table shall replace Table II-13 in Section 211.03 of the Specifications:

| Asphalt Concrete Mixtures: Design Range |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Mix Type | Percentage by Weight Passing Square Mesh Sieves |  |  |  |  |  |  |  |
|  | ¾ in | ½ in | 3/8 in | No. 4 | No. 8 | No. 30 | No. 50 | No. 200 |
| SM-9.5 A,D |  | 1001 | 90-100 | 90 max. | 32-67 |  |  | 2-10 |
| SM-12.5 A,D | 100 | 90-100 | 90 max. |  | 28-58 |  |  | 2-10 |

The design binder content shall be selected within a range of 3.0% --4.5% air voids.

This mix shall conform to Table 1 at the design binder content.

The results of supplementary performance testing at different binder contents (informational purposes) in addition to the design binder content shall be reported as follows:

- Asphalt Pavement Analyzer (APA) rut testing (VTM-142): at design binder content and at 0.5% above the design binder content

- Indirect Tensile Test at High Temperature (IDT-HT) (VTM-145): at design binder content and at 0.5% above the design binder content

- Cantabro testing (VTM-144): at design binder content and at 0.5% below the design binder content

- Indirect Tensile Cracking Test at intermediate temperature (IDT-CT)  (VTM-143): at design binder content, at 0.5% above, and at 0.5% below the design binder content

The minimum design asphalt binder contents shall be based on the following unless otherwise approved by the Engineer:

| Bulk Specific Gravity of the Total Aggregate | Minimum Design Binder Content Mix Type (%) |  |
| --- | --- | --- |
|  | SM-9.5 | SM-12.5 |
| Less Than 2.65 | 5.5 | 5.3 |
| 2.65 - 2.74 | 5.4 | 5.2 |
| 2.74 - 2.85 | 5.3 | 5.1 |
| Greater Than 2.85 | 5.2 | 5.0 |

For the BMD P+VO mixtures, a set of five  IDT-CT pills with the final design JMF (only at the design binder content) shall be fabricated from long-term aged loose mix and tested in accordance with ASTM D8225. Test results shall be submitted with the JMF for the mix design review. Long-term aging shall be performed by aging loose laboratory produced mix for 8 hours at 135ºC, after short term oven aging is performed as required by Table 1. During long-term aging, the mix shall be uniformly placed in a pan such that the height of the loose mix shall not exceed the mixture nominal max aggregate size. Opening of the oven door shall be minimized during long-term aging. Specimens shall be heated to compaction temperature following aging and then compacted. The heating to compaction temperature shall not exceed 75 minutes.

The JMF shall meet the nominal max aggregate size of the designated mix type. The JMF shall establish a single percentage of aggregate passing each required sieve, a single percentage of binder  to be added to the mix, the SUPERPAVE volumetric properties defined by AASHTO R 35  and a temperature range at which the mixture is to be produced.

The Contractor shall have a Department-certified Asphalt Mix Design Technician with the BMD training certification approved by the Department for designing and adjusting mixes. The Asphalt Mix Design Technician or an Asphalt Plant Level II Technician with the BMD training certification approved by the Department shall be capable of conducting necessary performance tests. The Asphalt Mix Design Technician shall be responsible for producing a mixture that complies with the requirements of this Specification.

Table 1 Performance Testing Requirements for Mix Design Performance Property; Performance Test; Test Method; Criteria. Rutting; APA Rut depth; VTM-142; ≤ 8.0mm. IDT-HT; VTM-145; Strength ≥ 100 kPa. Durability; Cantabro Mass Loss; VTM-144; Mass loss ≤ 7.5%. Cracking; IDT-CT; VTM-143; CTindex ≥ 70 COV ≤ 18.3%1.

1. Single operator testing tolerance: Coefficient of Variance (COV) shall be applied for the mix design IDT-CT test for all short-term aged specimens.  For the long-term aged specimen test during design the COV shall be reported only for informational purposes.

The JMF shall indicate which type of specimen preparation will be used during production for Indirect Tensile Cracking Test at intermediate temperature (IDT-CT) testing for the mix: non-reheat or reheated mixture. Throughout the production of the approved JMF, the indicated method shall be followed for every IDT-CT sample, unless otherwise approved by the Engineer.

IV.	Production Testing

Lot sizes defined by Sections 211 and 315 of the Specifications shall be followed for all production testing.

The Contractor shall conduct testing as required by Sections 211.05 and 211.06 of the Specifications for both A and D designated mixes. If less than 300 tons of asphalt mixture is produced under a single JMF in a day, SUPERPAVE testing will not be required on that day. That day’s tonnage shall be added to subsequent production. When the accumulated tonnage exceeds 300 tons, minimum testing frequency for SUPERPAVE testing shall apply and results shall be reported.

In addition to all of the testing requirements for SUPERPAVE mixes, performance testing shall also be conducted on D designated mixes by the Contractor, in accordance with Table 2 and at the frequency shown in Table 3. The Contractor shall report BMD performance test results within 48 hrs of sampling to the Department unless otherwise approved by the appropriate District Materials Engineer

The approved asphalt concrete mixture shall also produce a tensile strength ratio (TSR) of not less than 0.80 in accordance with Section 211 of the Specification and as verified by the Contractor during the first lot of production.

Table 2

Performance Testing Requirements for Production

| Performance Property | Performance Test | Test Method | Criteria |
| --- | --- | --- | --- |
| Rutting | APA Rut depth1 | VTM-142 | ≤ 8.0mm |
|  | IDT-HT | VTM-145 | Report only COV report only |
| Durability | Cantabro Mass Loss | VTM-144 | Mass loss ≤ 7.5% |
| Cracking | IDT-CT | VTM-143 | CTindex2 ≥ 70, reheated CTindex2 ≥ 95, non-reheated COV report only |

- APA Rut will be performed during production by VDOT with specimens made by the Contractor at the request of the Engineer.

- IDT-CT specimens shall be prepared (reheat or non-reheat) in accordance with the method indicated on the JMF and VTM-143.

Table 3

Performance Testing Frequency

| Property/Test | Frequency (tons) |
| --- | --- |
| IDT-CT | 2,000 |
| Cantabro Mass Loss | 2,000 |
| IDT-HT1 APA Rut depth | 4,000 As requested by Engineer2 |

- IDT-HT shall be performed on the same sample as IDT-CT.

- APA test will be performed by VDOT, however, specimens shall be made by the Contractor at the request of the Engineer.

V. 	Acceptance

Lot acceptance for BMD P+VO shall be as required by Section 211.08 of the Specifications.

Although acceptance will be based on Section 211, should any performance test results (based on the average of required number of specimens tested) fail to meet the criteria as specified in Table 2, the Department may require that production be stopped until corrective actions are taken by the Contractor. The Engineer will investigate and determine the acceptability of material placed and represented by failing performance test results.

Field density shall be determined in accordance with Section 315 of the Specifications.

VI.	Adjustment System

The Department will determine adjustment points in accordance with Section 211.09 of the Specifications except for the following:

- If the total adjustment is 25 points or less and the Contractor does not elect to remove and replace the material, the unit price for the material will be reduced 3% of the unit price bid for each adjustment point the material is outside of the process tolerance.

- The Engineer will reduce the unit bid price by 1.0 % for each adjustment point applied for standard deviation.

- The Engineer will increase the unit bid price by 5% if the following criteria are met: 1) the standard deviation of the binder content is within the ranges of 0.0 – 0.15; 2) there are no adjustment points assigned for any sieve sizes as noted in Table II-16; and 3) the average binder  content is no less than 0.10% below and no more than 0.20% above the approved mix design binder  content.

VII. 	Initial Production

Mix type BMD P+VO shall be subject to Section 211.15 of the Specifications at the Engineer’s discretion.

VIII.	Measurement and Payment

Asphalt Concrete BMD P+VO will be measured in tons and will be paid for at the Contract ton price. Net weight information shall be furnished with each load of material delivered in accordance with Section 211 of the Specifications. Batch weights will not be permitted as a method of measurement unless the Contractor’s plant is equipped in accordance with Section 211 of the Specifications, in which case the cumulative weight of the batches will be used for payment. This price shall include all labor, equipment, and materials necessary to furnish, install, and finish the work described herein.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete BMD P+VO (mix type) | Ton |