SS200-002020-03	August 25, 2020

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 200 – GENERAL

SECTION 200 – GENERAL of the Specifications is amended as follows:

Section 200.04 – Acceptance Procedures for Aggregates is amended to replace the fourth paragraph with the following:

The No. 10 sieve shall be the dividing sieve for soils, select material, aggregate subbase material, and aggregate base material. The No. 8 sieve shall be the dividing sieve for asphalt concrete aggregates. That portion of the total aggregate retained on the sieves is defined as coarse aggregate, and that portion passing the sieves is defined as fine aggregate. Soundness tests will be performed according to the requirements of AASHTO T 104 without regard to these definitions of fine and coarse aggregate. Fine and coarse aggregates for hydraulic cement concrete are distinguishable by their conformity to the series of grading requirements specified in Sections 202 and 203, respectively, except that lightweight aggregate is specified in Section 206.

Section 200.06 – Technician and Batcher Certification is renamed Technician Certification is amended to replace the first paragraph with the following:

When the Contract requires a type of technician defined by this Section, the Contractor shall use a person certified by the Department. The Department will either certify technicians upon a candidate’s satisfactory completion of an examination or recognize third-party certifications as described herein. The Contractor shall ensure their technician is able to prove their certification status upon demand.

Section 200.06(e) – Concrete Batcher is deleted.

Section 200.06(h) – Concrete Field Technician is replaced with the following:

Concrete Field Technician: A Concrete Field Technician provides quality control of placement operations for hydraulic cement concrete in accordance with applicable requirements. The Department will recognize ACI Concrete Field Testing Technician Grade I, Washington Area Council of Engineering Laboratories (WACEL) Concrete I, or National Institute for Certification in Engineering Technologies (NICET) Construction Materials Testing Level II for Concrete for this certification.

Section 200.06(j) – Aggregate Properties Technician is deleted.

Section 200.06(m) – Soils and Aggregate Compaction Technician is inserted as follows:

Soils and Aggregate Compaction Technician: A Soils and Aggregate Compaction Technician conducts density, moisture content, and depth checks of soil placement and aggregate lifts during construction, including stabilized lifts. The Technician also monitors application rates of stabilizing chemicals used in soil and aggregate lifts in the field. The Department will recognize NICET Construction Materials Testing Level II for Soils for this certification.

Section 200.06(n) – Cold Asphalt Recycling – Plant Technician is inserted as follows:

Cold Asphalt Recycling – Plant Technician samples Cold In-place Recycling (CIR) or Cold Central Plant Recycling (CCPR) material during production and is capable of conducting any tests necessary to put the CIR equipment and CCPR plant into operation.

Section 200.06(o) – Cold Asphalt Recycling – Field Technician is inserted as follows:

Cold Asphalt Recycling – Field Technician provides quality control testing and inspection of the placement of CIR and CCPR materials.

Section 200.06(p) – Full Depth Reclamation (FDR) Technician is inserted as follows:

Full Depth Reclamation (FDR) Technician provides quality control testing, inspection of the placement of FDR, samples FDR material during production, and is capable of conducting any tests necessary to put the FDR equipment into operation.