SS210-002020-01	19 May 2020

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATION

SECTION 210 – ASPHALT MATERIALS

SECTION 210 – ASPHALT MATERIALS of the Specifications is amended as follows:

Section 210.04(e) – Thin Hot Mix Asphalt Concrete Overlay tack coat is inserted as follows:

Thin Hot Mix Asphalt Concrete Overlay tack coat shall conform to the following:

| Test on Emulsion | Method | Min | Max |
| --- | --- | --- | --- |
| Viscosity at 77° F, SSF | AASHTO T 59 | 20 | 100 |
| Sieve Test1, % | AASHTO T 59 | — | 0.05 |
| 24 hour storage stability2, % | AASHTO T 59 | — | 1 |
| Residue from distillation at 400° F3, % | AASHTO T 59 | 63 |  |
| Oil portion from distillation ml of oil per 100g emulsion |  |  | 2 |
| Demulsibility, % 35 ml 0.02 N CaCl2 or 35 ml 0.8% dioctyl sodium sulfosuccinate | AASHTO T 59 | 60 |  |
| 1The sieve test is waived if successful application of the material has been achieved in the field. 2After standing undisturbed for 24 hours, the surface shall show no white, milky colored substance, but shall be a smooth homogeneous color throughout. 3AASHTO T59 with modifications to include a 400° F +/- 10° F maximum temperature to be held for a period of 15 minutes. |  |  |  |

| Test on Residue From Distillation | Method | Min | Max |
| --- | --- | --- | --- |
| Elastic Recovery1, % | AASHTO T 301 | 60 | — |
| Penetration @ 77° F, 100 g, 5 sec. dmm. | AASHTO T 49 | 60 | 150 |
| 1With exception that the elongation is 20 cm and the test temperature is 50° F. |  |  |  |