GUIDELINES — For use on all projects.

SS223-002020-01	July 3, 2019

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 223 – STEEL REINFORCEMENT

SECTION 223 – STEEL REINFORCEMENT of the Specifications is amended as follows:

Section 223.02(a)3 – Welded wire fabric is replaced with the following:

Welded wire fabric shall conform ASTM A1064. When used in continuously reinforced hydraulic cement concrete pavement wire fabric shall be deformed, furnished in flat sheets, and shall conform to ASTM A497, high yield of 70,000 psi.