SS237-002020-01	July 27, 2020

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 237 – STRUCTURE BEDDING MATERIAL AND BEARING PADS

SECTION 237 – STRUCTURE BEDDING MATERIAL AND BEARING PADS of the Specifications is amended as follows:

## Section 237.02(a) – Elastomeric Bearing Pads is amended by replacing the fourth paragraph with the following:

Material having a nominal durometer hardness of 70 and 50 shall be used for nonlaminated pads and laminated pads, respectively. Test samples shall be prepared from finished pads. Samples of each thickness will be taken from 1 full-size pad from each shipment of 300 pads or less, with 1 additional pad for each additional increment of 300 pads or fraction thereof. Samples shall comply with the following physical requirements when tested in accordance with the ASTM methods designated.