SS245-002020-01	April 30, 2020

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 245 – GEOSYNTHETICS AND LOW PERMEABILITY LINERS

SECTION 245 – GEOSYNTHETICS AND LOW PERMEABILITY LINERS of the Specifications is amended as follows:

Section 245.03(a) – Geotextile Fabric for Use in Silt Fences is amended by replacing the second paragraph with the following:

The geotextile shall comply with the requirements of AASHTO M288, Table 8, Temporary Silt Fence Property Requirements, for grab strength and ultraviolet stability.

Section 245.03(c) – Geotextile Fabric for Use in Drainage Systems (Drainage Fabric) is amended by replacing the third paragraph with the following:

The geotextile shall comply with the requirements of AASHTO M288 Table 1-Geotextile Strength Property Requirements, Class 2, for grab strength.

Section 245.03(d) – Geotextile for Use in Stabilization is replaced with the following:

Geotextile for Use in Separation and Stabilization: Separation geotextiles are used as a permeable layer to separate fine-grained subgrades and aggregate base or subbase. Stabilization geotextiles are used in saturated or unstable conditions to provide the functions of separation and reinforcement.

1.	Subgrade Separation Fabric:

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Apparent opening size | ASTM D 4751 | Max. No. 70 sieve |
| Permittivity | ASTM D4491 | Min. 0.1 sec-1 |

The geotextile shall comply with the requirements of AASHTO M288 Table 1-Geotextile Strength Property Requirements, Class 2, for grab strength, tear strength, and puncture strength. Only nonwoven geotextiles shall be used as subgrade separation geotextiles.

2.	Subgrade Stabilization Fabric:

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Apparent opening size | ASTM D4751 | Max. No. 70 sieve |
| Permittivity | ASTM D4491 | Min. 0.1 sec-1 |

The geotextile shall comply with the requirements of AASHTO M 288 for strength property requirements, Table 1, Class 1, for grab strength, tear strength, and puncture strength. Geotextiles used for subgrade stabilization shall be woven or nonwoven.

3.	Embankment Stabilization Fabric Up to 6 Feet High:

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Apparent opening size | ASTM D 4751 | Max. No. 20 sieve |
| Seam strength | ASTM D 4632 | 90% specified grab strength |

The geotextile shall comply with the requirements of AASHTO M288 Table 1, Class 1 for grab strength, tear strength, and puncture strength.

Section 245.03(e) – Prefabricated Geocomposite Pavement Underdrain is replaced with the following:

Prefabricated Geocomposite Pavement Underdrain: Prefabricated geocomposite pavement underdrain shall consist of a polymeric drainage core encased in a nonwoven filter fabric envelope having sufficient flexibility to withstand bending and handling without damage. Prefabricated geocomposite pavement underdrain shall conform to the following:

  - Core: The drainage core shall be made from an inert, polymeric material resistant to commonly encountered chemicals and substances in the pavement environment and shall have a thickness of not less than 3/4 inch. Outer surfaces shall be smooth to prevent excessive wear of bonded filter fabric.

| Physical Properties | Test Method | Requirements |
| --- | --- | --- |
| Compressive strength panel vertical strain and core area change | ASTM D1621/ D2412/D6364 | Min. 40 psi at 20% deflection after 24 hrs at 0 deg F and at 125 deg F |
| Water flow rate (after 100 hr at 10 psi and normal confining pressure gradient of no more than 0.1) | ASTM D4716 | Min. 15 gal/min/ft width for 12-in specimen length |

  - Filter Fabric: Geotextile shall be bonded to and tightly stretched over both sides of the core. Geotextile shall not sag or block the flow channels, shall have a life equivalent to that of the core material, and shall conform to the requirements of (c) herein.

Section 245.03(h) – Dewatering Bag is replaced with the following:

Dewatering Bag: A nonwoven geotextile sewn together to form a bag that can be used in lieu of a de-watering basin for the purpose of filtering out suspended soil particles. The bag shall be capable of accommodating the water flow from the pump without leaking at the spout and seams.

| Physical Property | Test Method | Requirements |
| --- | --- | --- |
| Grab strength @ Elongation >50%(CRE/Dry) | ASTM D4632 | Min. 250 lb (min) |
| Seam strength | ASTM D4632 | 90% Specified grab strength |
| Puncture | ASTM D6241 | Min. 150 lb |
| Permittivity | ASTM D4491 | Min. 1.2 sec-1 |
| UV resistance | ASTM D4355 | Min. 70% at 500 hr |
| AOS | ASTM D4751 | Max. 100 sieve |

Section 245.03(i)1 – Paving Fabric, Type I & II is replaced with the following:

Paving Fabric, Type I & II:  All paving fabrics shall meet the requirements of the table below.

| Property | Test Method | Type I | Type II |
| --- | --- | --- | --- |
| Mass per unit area, min (oz/yd2) | ASTM D5261 | 4.5 | 4.1 |
| Grab Tensile Strength, min (lbs.) | ASTM D4632 | 120 | 101 |
| Grab Tensile Elongation, min (%) | ASTM D4632 | 50 | 50 |
| Melting point, min (F) | ASTM D276 | 3201 | 3201 |
| 1320 is the softening/melt point of polypropylene. |  |  |  |

Section 245.03(i)2 – Paving Mat; Type I, II, and III is replaced with the following:

Paving Mat; Type I, II, and III: Materials used for paving mat shall be a hybrid of two or more of the following material types: fiberglass, polyester, or polypropylene. Paving mat shall meet the requirements of the table below.

| Property | Test Method | Type I | Type II | Type III |
| --- | --- | --- | --- | --- |
| Tensile Strength, min (lbs) | ASTM D5035 (2C-E) | 280 | 140 | 45 |
| Ultimate Elongation, max (%) | ASTM D5035 (2C-E) | 5 | 5 | 5 |
| Melting Point, min (°F) | ASTM D276 | 3201 | 3201 | 3201 |
| Mass/Unit Area, min (oz/yd2) | ASTM D5261 | 7.0 | 4.0 | 4.0 |
| 1320 is the softening/melt point of polypropylene, which is lower than either polyester or fiberglass. |  |  |  |  |

Section 245.03(i)3 – Paving Grid: Type I, II, & III is replaced with the following:

Paving Grid: Type I, II, & III:  Materials used for paving grids shall be comprised of fiberglass and shall meet the requirements of the table below. Some paving grids are self-adhesive and some require nails for installation. Tack coat required for the installation of the overlay shall be specified with the paving grid. Refer to manufacturer’s recommendations for tack coat type and application rate.

| Property | Test | Type I | Type II | Type III |
| --- | --- | --- | --- | --- |
| Tensile Strength, min (lbs/in)1 | ASTM D6637, Method A, modified2 | 560 x 1,120 | 560 | 280 |
| Aperture size, min (in) | Calipered | 0.5 | 0.5 | 0.5 |
| Elongation, max (%) | ASTM D6637 Method A | 3 | 3 | 3 |
| Mass per area, min (oz/yd2) | ASTM D5261 | 16 | 10 | 5.5 |
| Melting Point, min (°F) (fabric component – if applicable) | ASTM D276 | 4203 | 4203 | 4203 |
| 1For Type I, machine and cross direction respectively. Strengths for Type II and III are in both directions 2Tensile Strength shall be converted to and reported in lbs/in. 3420 is the softening/melt point of fiberglass. |  |  |  |  |

Section 245.03(i)4 – Composite Paving Grids: Type I, II, & III is replaced with the following:

Composite Paving Grids: Type I, II, & III: Composite paving grids shall consist of a fiberglass, polyester, or polyvinyl alcohol (PVA) paving grid integrated with a nonwoven geotextile and meet the requirements of the table below.

| Property | Test | Type I | Type II | Type III |
| --- | --- | --- | --- | --- |
| Tensile Strength, Min (lbs/in)1 | ASTM D6637, Method A, modified2 | 560 x 1,120 | 560 | 280 |
| Aperture size, Min (in) | Calipered | 0.5 | 0.5 | 0.5 |
| Elongation, Max (%) | ASTM D6637 Method A | 5 | 5 | 10 |
| Mass per area, Min (oz/yd2) | ASTM D5261 | 16 | 10 | 5.5 |
| Melting Point, Min (°F) (fabric component) | ASTM D276 | 3203 | 3203 | 3203 |
| 1For Type I, machine and cross direction respectively. Strengths for Type II and III are in both directions. 2Tensile Strength should be converted to and reported in lbs/in. 3320 is the assumed softening/melt point of PVA. See Section 318.03 for more on placement temperature. |  |  |  |  |

Section 245.03(i)5 – Pavement Repair and Bridge Deck Waterproofing Strip Membrane is replaced by the following:

Pavement Repair and Bridge Deck Waterproofing Strip Membrane: Materials used for strip membranes shall be comprised of composite self-adhering rubberized asphalt attached to a pavingfabric, a paving mat, or a paving grid and meet the requirements of the table below.

| Property | Test Method | Type I |
| --- | --- | --- |
| Strip Tensile Strength, min (lbs/in) | ASTM D882 | 50 |
| Puncture Resistance, min (lbs) | ASTM E154 | 200 |
| Permeance-Perms, max | ASTM E-96 Method B | 0.05 |
| Pliability - 1/4" Mandrel 180⁰ Bend at -25 ⁰F | ASTM D146 | No cracks in fabric or rubberized asphalt |