SS320-002020-01	July 6, 2020

VIRGINIA DEPARTMENT OF TRANSPORTATION

2020 ROAD AND BRIDGE SUPPLEMENTAL SPECIFICATIONS

SECTION 320 – BM-25.0D WITH INCREASED ASPHALT CONTENT

SECTION 320 – BM-25.0D WITH INCREASED ASPHALT CONTENT of the Specifications is inserted as follows:

320.01 – Description

This work shall consist of supplying, testing and installing asphalt concrete base with additional asphalt binder. BM-25.0D with additional asphalt binder content (BM-25.0D+0.4 and BM-25.0D+0.8) shall conform to all of the requirements of a standard BM-25.0D in Section 211 except as provided herein.

Construction and Acceptance of one or more courses of asphalt concrete consisting of BM-25.0D+0.4 or BM-25.0D+0.8 asphalt concrete base shall be according to BM-25.0D in Section 315 and the density specified herein.

320.02 – Materials

Materials shall conform to Section 211 and 315.02.

320.03 – Job Mix Formula

The mixes shall conform to all of the requirements of a standard BM-25.0D in Section 211 except as noted herein.

An equivalent single axle load (ESAL) will be established by the Engineer and the mix types may be specified as one of the types listed in Table III-7.

| TABLE III-7 Mix Design Requirements |  |  |  |
| --- | --- | --- | --- |
| Mix Type | Equivalent Single Axle Load (ESAL) Range (millions) | Final Asphalt Performance Grade (PG) | NMAS1 |
| BM-25.0D (+0.4 and +0.8) | All ranges | 64H-16 | 1” |
| 1Nominal Maximum Aggregate Size (NMAS) is defined as one sieve size larger than the first sieve to retain more than 10 percent aggregate. |  |  |  |

To determine the asphalt binder content for the BM-25.0D plus additional asphalt binder, an approved BM-25.0D conforming to Section 211 will be used to determine the optimum asphalt binder content and aggregate gradations.  While the optimum asphalt binder content for the BM-25.0D will be selected at 2.5% in accordance with Section 211, the initial asphalt binder content for the BM-25.0D+0.4 or BM-25.0D+0.8 will be selected using the 3.5% air voids.  The additional asphalt binder (0.4% or 0.8%) will be added to the initial asphalt binder content at 3.5% air voids in order to establish the design asphalt binder content.

During production the BM-25.0D+0.4 and BM-25.0D+0.8 mixes shall be controlled according to Table III-8.

| TABLE III-8 Production Criteria |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Mix Type | VTM Production (%) | VFA (%) | Min. VMA (%) | Fines/Asphalt Ratio | Number of Gyrations |  |
|  |  |  |  |  | N Design | N Initial |
| BM-25.0D+0.4 | 1.0 – 4.0 | 67 – 92 | 12.0 | 0.6 – 1.3 | 65 | 7 |
| BM-25.0D+0.8 | 0.5 – 3.5 | 67 – 92 | 12.0 | 0.6 – 1.3 | 65 | 7 |

The Laboratory mixing temperature shall be 310°F to 320°F and the compaction temperature shall be 295oF to 300 oF for both testing and design.

Field correction factor. The field correction factor is determined by subtracting the bulk specific gravity of the aggregate from the effective specific gravity of the aggregate determined at the JMF asphalt binder content achieved.

| TABLE III-8A Recommended Performance Grade of Asphalt Binder |  |  |
| --- | --- | --- |
|  | Percentage of Reclaimed Asphalt Pavement (RAP) in Mix |  |
| Mix Type | %RAP < 25.0 | 25.0 ≤ %RAP ≤ 35.0 |
| BM-25.0D (+0.4 and +0.8) | PG 64H-22 | PG 64S-22 |

320.04 – Testing

When asphalt binder is extracted and recovered according to AASHTO T 170, the recovered asphalt binder shall meet the required grade specified in Table III-7.

320.05 – Aceptance and Adjustment

Acceptance and adjustments shall be according to BM-25.0D in Section 211.08 and 211.09.

320.06 – Density

Density shall be determined in accordance with Section 315.05(e).  The minimum density requirements for BM-25.0D+0.4 and BM-25.0D+0.8 are shown in Table III-9.

| TABLE III-9 DENSITY REQUIREMENTS |  |
| --- | --- |
| Mixture Type | Minimum Control Strip Density (%)1 |
| BM-25.0D+0.4 | 94.0 |
| BM-25.0D+0.8 | 96.0 |
| 1The control strip density requirement is the percentage of theoretical maximum density of the job mix formula by SUPERPAVE® mix design or as established by the Engineer based on two or more production maximum theoretical density tests. |  |

320.07 –  Measurement and Payment

BM-25.0D+0.4 and BM-25.0D+0.8 will be measured in tons and paid for at the Contract ton price.  This price shall include all materials and labor specified in Section 315 as modified in this Section for asphalt concrete base.

Payment will be made under:

| Pay Item | Pay Unit |
| --- | --- |
| Asphalt Concrete Base Course Type BM-25.0D+0.4 | Ton |
| Asphalt Concrete Base Course Type BM-25.0D+0.8 | Ton |